Supplementary Material

Focus on hydrochars produced from hydrothermal liquefaction of beech wood, soda lignin and black liquor

Maximilian Wörner a, Ursel Hornunga,*, Selhan Karagöz a,b *, Thomas Zevaco a, Nicolaus Dahmena

a Institut für Katalyseforschung und Technologie (IKFT), Karlsruher Institut für Technologie (KIT), Eggenstein-Leopoldshafen 76344, Germany.

bDepartment of Chemistry, Karabük University, 78050, Turkey.

*Corresponding Authors: ursel.hornung@kit.edu (U. Hornung)

skaragoz@karabuk.edu.tr (S.  Karagöz )

Table S1. Comparison of mass yields of hydrochars from hydrothermal liquefaction of various biomasses.

| Type of Lignocellulose | Temperature (C) | Residence Time (min) | The highest hydrochar mass yield (wt.%) | Literature |
| --- | --- | --- | --- | --- |
| White pine sawdust | 300 | 15 | 30.0 | (Cheng et al. 2010) |
| Chinese fir wood | 360 | 10 | 26.3 | (Zhong and Wei 2004) |
| Chinese fir wood | 300 | 10 | 29.8 | (Zhong and Wei 2004) |
| Lignin from empty fruit bunch | 300 | 30 | 35a (taken from Fig.) | (Jitpinit et al. 2024) |
| Oak wood | 330 | 30 | 24a (taken from Fig.) | (Tai et al. 2021) |
| Chicken manure | 300 | 30 | 24a (taken from Fig.) | (Vadlamudi et al. 2024) |
| Dried manure | 310 | 15 | 24.0 | (Rivas-Arrieta et al. 2024) |
| Natural hay | 310 | 30 | 22a (taken from Fig.) | (De Caprariis et al. 2017) |
| Oak wood | 310 | 30 | 36a (taken from Fig.) | (De Caprariis et al. 2017) |
| Walnut shell | 310 | 30 | 20a (taken from Fig.) | (De Caprariis et al. 2017) |
| Cellulose | 310 | 30 | 37a (taken from Fig.) | (De Caprariis et al. 2017) |
| Black liquor | 400 | 30 | 31b (calculated based on dry black liquor) | (Harisankar and Vinu 2023) |
| Beech wood | 300 | 20 | 31.1 | This study |
| Beech wood | 350 | 20 | 25.9 | This study |
| Soda lignin | 300 | 20 | 32.7 | This study |
| Soda lignin | 350 | 20 | 29.6 | This study |
| Black liquor | 300 | 20 | 31.4 | This study |
| Black liquor | 350 | 20 | 27.3 | This study |

REFERENCES

Cheng S, D’cruz I, Wang M, et al (2010) Highly Efficient Liquefaction of Woody Biomass in Hot-Compressed Alcohol−Water Co-solvents. Energy Fuels 24:4659–4667. https://doi.org/10.1021/ef901218w

De Caprariis B, De Filippis P, Petrullo A, Scarsella M (2017) Hydrothermal liquefaction of biomass: Influence of temperature and biomass composition on the bio-oil production. Fuel 208:618–625

Harisankar S, Vinu R (2023) Platform chemicals from hardwood black liquor via hydrothermal liquefaction: influence of process conditions on product yields and quality. Sustainable Energy & Fuels 7:4423–4441

Jitpinit S, Chisti Y, Rattanasak U, et al (2024) Hydrothermal liquefaction of oil-palm-derived lignin to bio-oils for use as antioxidants in biodiesel. Journal of Industrial and Engineering Chemistry 135:243–256

Rivas-Arrieta MJ, Torri C, Rombolà AG, Biller P (2024) Hydrochar fractionation and composition in batch and continuous hydrothermal liquefaction. Biomass and Bioenergy 183:107166

Tai L, De Caprariis B, Scarsella M, et al (2021) Improved Quality Bio-Crude from Hydrothermal Liquefaction of Oak Wood Assisted by Zero-Valent Metals. Energy Fuels 35:10023–10034. https://doi.org/10.1021/acs.energyfuels.1c00889

Vadlamudi DP, Pecchi M, Sudibyo H, Tester JW (2024) Direct and Two-Stage Hydrothermal Liquefaction of Chicken Manure: Impact of Reaction Parameters on Biocrude Oil Upgradation. ACS Sustainable Chem Eng 12:4300–4313. https://doi.org/10.1021/acssuschemeng.3c08579

Zhong C, Wei X (2004) A comparative experimental study on the liquefaction of wood. Energy 29:1731–1741