Supplementary information

Genesis of Devonian volcanic-associated Lahn-Dill-type iron ores – Part I: iron mobilisation and mineralisation style

Leanne Schmitt1,2*, Thomas Kirnbauer1, Thomas Angerer3, Rebecca Volkmann1,4, Vladimir Roddatis4, Richard Wirth4, Sabine Klein1,5

1Institute of Geology, Mineralogy and Geophysics, Ruhr University Bochum, 44801 Bochum, Germany

2Faculty of Georesources and Process Engineering, Technische Hochschule Georg Agricola, 44787 Bochum, Germany

3Department of Mineral Resources and Geoenergy, GeoSphere Austria, 1190 Wien, Austria

4GFZ German Research Centre for Geosciences, 14473 Potsdam, Germany

5 Deutsches Bergbau-Museum Bochum, 44791 Bochum, Germany

*corresponding author: Leanne Schmitt. Email: leanne.schmitt@ruhr-uni-bochum.de

1. WDXRF

Major element analysis of Si, Ti, Al, Fe, Mn, Mg, Ca, Na, K and P was conducted using WDXRF. For calibration, a selection of certified geological rock standards, which cover preferably most large concentration ranges of elements were measured. Statistically, linear regression lines were modelled for each element to re-calculate the concentrations in the unknown sample from detected intensities. Totals range between 98.01 and 100.53 wt.% for footwall volcaniclastic rocks. Additionally, Fe2+ was determined using potentiometric titration (method after Ungethüm 1965). For H2O determination, samples were heated in a high frequency heating apparatus coupled with an oven at 1000 °C, whereas for CO2 an Eltra CS-500 Carbon Determinator Anayser was used. However, for some footwall volcaniclastic rocks, loss on ignition (LOI) was determined at 1050 °C following standard procedure instead of separate CO2 and H2O determination, due to breakdown of the Carbon Determinator Analyser.

2. ICP-MS

Elements including Y, Zr, and Nb were analysed with ICP-MS. For analysis, mixed acid digestion was applied using 3 ml concentrated HCl, 1 ml concentrated HNO3 and 1 ml concentrated HF. Aliquots of 50 mg powder for each sample were placed in acid-cleaned PTFE (Teflon) vessels and digested in supra-pure acids under pressure with reagent blanks being constantly checked for contamination. After heating closed vessels up for 12h on a heating block, samples were opened, checked for complete digestion (no remaining residues) and put under a fume hood to evaporate acids. Samples were evaporated thrice until incipient dryness and filled twice with 5 ml concentrated HCl. After reaching incipient dryness for the third time, vessels with samples were filled with around 5 ml 0.5 M HNO3 and left on a hot plate for 30 min. Subsequently, each sample solution was transferred to a 60 ml bottle and filled up with 0.5 M HNO3. Trace amounts of HF were added to stabilize high field strength elements (HFSE) in solution. For ICP-MS analysis, sample solutions were further diluted and 1 ppb of Ru-Rh-Re-Bi internal standard was added to correct for matrix effects and instrumental drift.

References

Ungethüm H (1965) Eine neue Methode zur Bestimmung von Eisen(II) in Gesteinen und Mineralen, insbesondere auch in bitumenhaltigen Proben. Zeitschrift für angewandte Geologie 11:500–504