Supplementary Material

Table S1. Precursors and reactants used in previous investigations for ALD deposition.

| Material | Precursor | Reactant | Temperature | Reference |
| --- | --- | --- | --- | --- |
| Pt | MeCpPtMe3 | O2/H2 | 30 oC | [44] |
| Pd | PdII(hfac)2 | H2 | 80 oC | [45] |
| Cu | CuBu-amd | H2 | 150 – 190 oC | [46] |
| Cu | Cu(acac)2 | H2 | 165 oC | [47] |
| Co | Co(iPr-amd)2 | NH3, H2-N2 | 350 oC | [48] |
| Co | Co(MeCp)2 | NH3 | 200 oC | [49] |
| Ni | NiCp2 | H2O | 165 oC | [50] |
| Ni | Ni(dmamb)2 | NH3 | 300 oC | [51, 52] |
| Ag | Ag(fod)(PEt3) | H2 | 120-140 oC | [53] |
| Ru | Ru(EtCp)2 | NH3 | 270 oC | [54] |
| Ru | Ru(EtCp)2 | O2 - H2 | 200 oC | [55] |
| Ir | Ir(acac)3 | O3 + H2 | 165 – 200 oC | [56] |
| Ir | (MeCp)Ir(CHD) | O3/ O2 | 200/225 oC | [57] |
| MoO3 | t(BuN)2(NMe2)2Mo | O2 | 50 C – 350 oC | [58] |
| WO3 | t(BuN)2W(NMe2)2 | H2O | 250 C – 350 oC | [58] |
| WO3 | t(BuN)2W(NMe2)2 | O2 | 100 – 400 oC | [59] |
| WO3 | WO2(tBuamd)2 | H2O | 120 – 270 oC | [58] |
| Al2O3 | TMA | H2O | 180 oC | [58] |
| Al2O3 | TMA | O2 | 150 – 350 oC | [60] |
| TiO2 | TiCl4 | O2 | 30 – 180 oC | [58] |
| TiO2 | TDMAT | H2O | 250 oC | [58] |
| SiO2 | H2Si[N(C2H5)2]2 | O2 | 200 oC | [61] |
| ZnO | DEZ | H2O | 200 oC | [58] |
| ZnO | DEZ | O2 | RT | [62] |
| ZnS | DEZ | H2S/Ar | 60 – 300 oC | [63] |
| MoS2 | MoCl5 | H2S | 450 oC | [58] |
| MoS2 | Mo(CO)6 | Ozone | 165 oC | [58] |
| MoS2 | (NtBu)2(NMe2)2Mo | O2 | 150 oC | [58] |
| WSe2 | WCl5 | H2S | 390 oC | [58] |
| Bi2S3 | Bi(thd)3 | H2O | 300 oC | [58] |
| Bi2S3 | Bi(thd)3 | H2S | 125 – 300 oC | [58] |
| FeSx | Fe(amd)2 | H2S | 80 – 200 oC | [58] |
| GaS | Ga2(NMe2)6 | H2S | 125 – 225 oC | [58] |
| GaS | TMGa | H2S/Ar | 70 – 350 oC | [64] |
| Ga2O3 | TMGa | O2 | 80 – 250 oC | [65] |
| SnS | Sn(acac)2 | H2S | 80 – 160 oC | [58] |
| SnOx | TDMASn | Ar | 100 – 250 oC | [66] |

TM = trimethyl, TDMA = Tetrakisdimethylamido, DE = diethyl, dmamb = ¼ 1-dimethylamino-2-methyl-2-butanolate, fod = 1,1,1,2,2,3,3-heptafluoro-7,7-dimethyloctane-4,6-dione