Supplementary information

Study of the conductive ink wash-out during overmolding

e-mail corresponding author: epascualcuenca@gmail.com

journal: The International Journal of Advanced Manufacturing Technology

Enric Pascual Cuenca 1*, Miguel Sanchez Soto 2, Enric Fontdecaba Baig1, Lucia G. De la Cruz2

1Eurecat, Centre Tecnològic de Catalunya, Unit of Polymeric Materials and Processes, Av. Universitat Autònoma 23, 08290 Cerdanyola del Vallès, Spain

2Departament de Ciència I Enginyeria de Materials, Escola d’Enginyeria de Barcelona Est. (EEBE), Universitat Politècnica de Catalunya-Barcelona Tech (UPC), Campus Diagonal-Besòs, Av. D’Eduard Maristany, 16, 08019 Barcelona, Spain.

Fig. s 1. Experimental viscosity versus injection rate curves for edge gate. From this experimental analysis, the injection velocity at which the process reaches stability is determined, beyond which the process becomes insensitive to potential variations in the material's viscosity. The values of injection rates selected in this work were 50 mm/s and 120 mm/s

Fig. s 2. Experimental viscosity versus injection rate curves for fan gate. From this experimental analysis, the injection velocity at which the process reaches stability is determined, beyond which the process becomes insensitive to potential variations in the material's viscosity. The values of injection rates selected in this work were 50 mm/s and 120 mm/s

Fig. s 3. Experimental viscosity versus injection rate curves for submarine gate. From this experimental analysis, the injection velocity at which the process reaches stability is determined, beyond which the process becomes insensitive to potential variations in the material's viscosity. The values of injection rates selected in this work were 50 mm/s and 120 mm/s

Fig. s 4. PVT curve for Makrolon 2207