Table S 1. Series one thickness time-pressure data

| Test Data of Viscoelastic Materials with Various Thicknesses |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Material Characteristics |  |  | Waveform Data |  |  |  |  |
| Test No | Material Type | Thickness (mm) | Peak Pressure (kPa) | Duration (ms) | Rise Time (ms) | Decay Time (ms) | Impulse (kPa*ms) |
| 1 | Polyurethane-based Material | 1 | 184.3 | 0.204 | 0.101 | 0.103 | 21.42 |
| 2 |  | 1 | 190.9 | 0.199 | 0.109 | 0.090 | 20.99 |
| 3 |  | 1 | 197.1 | 0.199 | 0.101 | 0.098 | 21.82 |
| 4 |  | 3 | 218.2 | 0.256 | 0.147 | 0.109 | 25.08 |
| 5 |  | 3 | 221.9 | 0.253 | 0.148 | 0.105 | 24.99 |
| 6 |  | 3 | 214.1 | 0.255 | 0.149 | 0.106 | 24.68 |
| 7 |  | 5 | 184.8 | 0.310 | 0.195 | 0.115 | 27.76 |
| 8 |  | 5 | 169.8 | 0.310 | 0.185 | 0.125 | 26.53 |
| 9 |  | 5 | 169.9 | 0.307 | 0.183 | 0.124 | 26.26 |
| 10 |  | 7 | 191.0 | 0.339 | 0.213 | 0.126 | 28.35 |
| 11 |  | 7 | 195.7 | 0.333 | 0.203 | 0.130 | 29.03 |
| 12 |  | 7 | 202.9 | 0.330 | 0.200 | 0.130 | 29.03 |
| 13 |  | 9 | 201.5 | 0.335 | 0.220 | 0.115 | 31.14 |
| 14 |  | 9 | 192.5 | 0.358 | 0.218 | 0.140 | 30.61 |
| 15 |  | 9 | 197.1 | 0.351 | 0.220 | 0.131 | 31.92 |
| 16 | Silicone Rubber-based Material | 1 | 298.2 | 0.358 | 0.078 | 0.279 | 23.28 |
| 17 |  | 1 | 276.9 | 0.355 | 0.085 | 0.270 | 22.86 |
| 18 |  | 1 | 279.5 | 0.350 | 0.084 | 0.266 | 22.26 |
| 19 |  | 3 | 267.2 | 0.326 | 0.128 | 0.197 | 24.20 |
| 20 |  | 3 | 276.6 | 0.322 | 0.128 | 0.193 | 24.28 |
| 21 |  | 3 |  | 0.339 | 0.124 | 0.215 | 23.60 |
| 22 |  | 5 | 226.9 | 0.343 | 0.162 | 0.181 | 27.72 |
| 23 |  | 5 | 218.1 | 0.348 | 0.165 | 0.183 | 26.48 |
| 24 |  | 5 | 213.0 | 0.348 | 0.163 | 0.185 | 26.21 |
| 25 |  | 7 | 180.0 | 0.370 |  | 0.166 | 31.43 |
| 26 |  | 7 | 187.3 | 0.365 | 0.193 | 0.172 | 29.03 |
| 27 |  | 7 | 202.4 | 0.359 |  | 0.178 | 28.55 |
| 28 |  | 9 | 196.2 | 0.380 | 0.207 | 0.173 | 29.40 |
| 29 |  | 9 | 201.1 | 0.379 | 0.199 | 0.180 | 27.59 |
| 30 |  | 9 | 204.3 |  | 0.193 |  | 26.95 |

Figure S 1. Three trial comparison of 9 mm polyurethane-based material

Table S 2. Significance coefficients for thickness-based regression

| Material | Test Variable | R2 | ρ |
| --- | --- | --- | --- |
| Polyurethane | Peak Pressure (kPa) | 0.016 | 0.909 |
|  | Duration (ms) | 0.989 | < 0.001 |
|  | Rise Time (ms) | 0.990 | < 0.001 |
|  | Decay Time (ms) | 0.813 | < 0.001 |
|  | Impulse (kPa*ms) | 0.975 | < 0.001 |
| Silicone Rubber | Peak Pressure (kPa) | 0.913 | < 0.001 |
|  | Duration (ms) | 0.720 | 0.001 |
|  | Rise Time (ms) | 0.983 | < 0.001 |
|  | Decay Time (ms) | 0.942 | < 0.001 |
|  | Impulse (kPa*ms) | 0.790 | < 0.001 |

Table S 3. Series two GNP time-pressure data

| Test Data of Viscoelastic Materials Impregnated with GNPs by wt.% |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Material Characteristics |  |  | Waveform Data |  |  |  |  |
| Test No | Material Type | GNP (wt.%) | Peak Pressure (kPa) | Duration (ms) | Rise Time (ms) | Decay Time (ms) | Impulse (kPa*ms) |
| 1 | Polyurethane-based Material | 0.00% | 178.6 | 0.307 | 0.183 | 0.123 | 26.55 |
| 2 |  | 0.00% | 175.7 | 0.304 |  |  | 25.85 |
| 3 |  | 0.00% | 170.3 | 0.302 |  |  | 25.50 |
| 4 |  | 0.50% | 196.8 | 0.304 | 0.193 | 0.111 | 28.36 |
| 5 |  | 0.50% | 208.2 | 0.298 | 0.190 | 0.107 | 28.55 |
| 6 |  | 0.50% | 204.7 | 0.299 | 0.189 | 0.110 | 28.55 |
| 7 |  | 1.00% | 213.0 | 0.299 | 0.190 | 0.109 | 28.60 |
| 8 |  | 1.00% | 217.0 | 0.296 | 0.191 | 0.105 | 29.39 |
| 9 |  | 1.00% | 211.2 | 0.298 | 0.191 | 0.107 | 28.83 |
| 10 |  | 1.50% | 228.2 | 0.304 | 0.192 | 0.112 | 29.81 |
| 11 |  | 1.50% | 218.5 | 0.304 | 0.192 | 0.112 | 28.83 |
| 12 |  | 1.50% | 226.3 | 0.300 | 0.189 | 0.111 | 29.90 |
| 13 |  | 2.00% | 179.1 | 0.312 | 0.196 | 0.116 | 27.41 |
| 14 |  | 2.00% | 174.6 | 0.310 | 0.197 | 0.113 | 26.88 |
| 15 |  | 2.00% | 178.9 | 0.312 | 0.194 | 0.117 | 27.18 |
| 16 | Silicone Rubber-based Material | 0.00% | 218.7 | 0.331 | 0.165 | 0.166 | 25.84 |
| 17 |  | 0.00% | 213.0 | 0.332 | 0.165 | 0.167 | 26.33 |
| 18 |  | 0.00% | 215.3 | 0.330 | 0.164 | 0.166 | 24.61 |
| 19 |  | 0.50% | 208.2 | 0.330 | 0.172 | 0.158 | 25.38 |
| 20 |  | 0.50% | 204.2 | 0.327 | 0.174 | 0.152 | 26.92 |
| 21 |  | 0.50% | 197.4 | 0.333 | 0.174 | 0.159 | 27.03 |
| 22 |  | 1.00% | 193.9 | 0.312 | 0.168 | 0.144 | 28.19 |
| 23 |  | 1.00% | 186.5 | 0.313 | 0.169 | 0.144 | 27.29 |
| 24 |  | 1.00% | 187.0 | 0.311 | 0.166 | 0.144 | 27.09 |
| 25 |  | 1.50% | 179.8 | 0.316 | 0.176 | 0.139 | 27.32 |
| 26 |  | 1.50% | 186.5 | 0.316 | 0.172 | 0.144 | 27.93 |
| 27 |  | 1.50% | 173.7 | 0.319 | 0.176 | 0.143 | 25.97 |
| 28 |  | 2.00% |  |  |  |  |  |
| 29 |  | 2.00% |  |  |  |  |  |
| 30 |  | 2.00% |  |  |  |  |  |

Table S 4. Significance coefficients for GNP-based regression

| Material | Test Variable | R2 | ρ |
| --- | --- | --- | --- |
| Polyurethane | Peak Pressure (kPa) | 0.849 | < 0.001 |
|  | Duration (ms) | 0.845 | < 0.001 |
|  | Rise Time (ms) | 0.623 | 0.008 |
|  | Decay Time (ms) | 0.763 | 0.001 |
|  | Impulse (kPa*ms) | 0.882 | < 0.001 |
| Silicone Rubber | Peak Pressure (kPa) | 0.917 | < 0.001 |
|  | Duration (ms) | 0.679 | 0.006 |
|  | Rise Time (ms) | 0.415 | 0.089 |
|  | Decay Time (ms) | 0.944 | < 0.001 |
|  | Impulse (kPa*ms) | 0.476 | 0.055 |

Table S 5. Series three multilayered time-pressure data

| Test Data of Multilayered Viscoelastic Materials |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Material Characteristics |  | Waveform Data |  |  |  |  |
| Test No | Sample Layering | Peak Pressure (kPa) | Duration (ms) | Rise Time (ms) | Decay Time (ms) | Impulse (kPa*ms) |
| 1 | 3 mm Poly | 163.1 | 0.281 | 0.143 | 0.138 | 22.68 |
| 2 | 3 mm Poly | 163.0 | 0.273 | 0.141 | 0.132 | 22.20 |
| 3 | 3 mm Poly |  | 0.286 | 0.143 | 0.143 | 22.55 |
| 4 | 3 mm Poly | 163.7 | 0.286 |  | 0.130 | 22.69 |
| 5 | 3 mm Silicone | 174.4 | 0.343 | 0.141 | 0.202 | 23.53 |
| 6 | 3 mm Silicone | 162.5 | 0.342 | 0.140 | 0.202 | 23.83 |
| 7 | 3 mm Silicone |  |  |  |  |  |
| 8 | 3 mm Silicone | 174.2 | 0.339 | 0.140 | 0.199 | 23.77 |
| 9 | 5 mm Poly | 185.0 | 0.312 | 0.195 | 0.117 | 28.05 |
| 10 | 5 mm Poly | 197.9 | 0.304 | 0.186 | 0.118 |  |
| 11 | 5 mm Poly | 186.1 | 0.314 | 0.187 |  | 28.32 |
| 12 | 5 mm Poly | 191.2 | 0.306 | 0.193 | 0.113 | 28.28 |
| 13 | 5 mm Silicone | 194.0 | 0.349 | 0.165 | 0.184 | 26.23 |
| 14 | 5 mm Silicone | 187.2 | 0.344 | 0.168 | 0.176 | 25.66 |
| 15 | 5 mm Silicone | 194.8 | 0.346 | 0.156 | 0.190 | 26.58 |
| 16 | 5 mm Silicone |  | 0.337 | 0.156 | 0.181 | 25.73 |
| 17 | PSP |  | 0.293 | 0.152 | 0.141 | 24.59 |
| 18 | PSP | 157.7 | 0.299 | 0.151 | 0.148 | 24.10 |
| 19 | PSP | 154.5 | 0.297 | 0.151 | 0.146 | 22.37 |
| 20 | PSP | 158.8 | 0.299 | 0.155 | 0.144 | 23.28 |
| 21 | SPS | 158.0 | 0.354 | 0.155 | 0.199 | 24.80 |
| 22 | SPS | 165.3 | 0.330 | 0.143 | 0.187 |  |
| 23 | SPS | 172.9 | 0.307 | 0.145 | 0.162 | 24.67 |
| 24 | SPS | 157.0 | 0.366 | 0.151 | 0.215 | 24.71 |
| 25 | P3SP | 184.2 | 0.309 | 0.179 | 0.130 | 27.80 |
| 26 | P3SP | 172.4 | 0.315 | 0.182 | 0.133 | 26.52 |
| 27 | P3SP | 187.0 | 0.131 | 0.186 | 0.127 | 28.33 |
| 28 | P3SP | 182.0 | 0.315 | 0.194 | 0.121 | 27.52 |
| 29 | S3PS | 163.1 | 0.373 | 0.171 | 0.202 | 25.73 |
| 30 | S3PS | 159.8 | 0.351 | 0.164 | 0.187 | 26.35 |
| 31 | S3PS | 162.4 | 0.353 | 0.162 | 0.191 | 255.98 |
| 32 | S3PS | 153.4 | 0.367 | 0.157 | 0.210 | 26.06 |
| 33 | PSPSP | 153.4 | 0.329 | 0.179 | 0.150 | 25.98 |
| 34 | PSPSP | 168.3 | 0.321 | 0.180 | 0.141 | 27.32 |
| 35 | PSPSP | 166.5 | 0.319 |  | 0.142 | 26.09 |
| 36 | PSPSP | 157.0 | 0.328 | 0.179 | 0.149 | 26.51 |
| 37 | SPSPS | 168.1 | 0.373 | 0.165 | 0.208 | 25.61 |
| 38 | SPSPS | 172.8 | 0.373 | 0.163 | 0.210 | 25.58 |
| 39 | SPSPS | 174.3 | 0.376 | 0.167 | 0.209 | 26.33 |
| 40 | SPSPS |  | 0.379 | 0.157 |  | 25.96 |

Table S 6. Multilayered bartlett tests of variance results

| Bartlett Tests Assessing Multilayered Viscoelastic Materials |  |  |  |
| --- | --- | --- | --- |
| Waveform Characteristic | Combined Samples | External Layer Grouping |  |
|  |  | Polyurethane | Silicone Rubber |
| Peak Pressure (kPa) | 0.053 | 0.044 | 0.153 |
| Duration (ms) | < 0.001 | 0.658 | 0.002 |
| Rise Time (ms) | 0.027 | 0.023 | 0.174 |
| Decay Time (ms) | < 0.001 | 0.743 | < 0.001 |
| Impulse (kPa*ms) | 0.018 | 0.094 | 0.223 |

Table S 7. Generalized linear regression p-values for multilayered samples

| Sample Thickness | Samples Characteristic | Waveform Characteristic |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Peak Pressure (kPa) | Duration (ms) | Rise Time (ms) | Decay Time (ms) | Impulse (kPa*ms) |
| 3 mm | Number of Layers | 0.115 | 0.427 | 0.273 | 0.216 | 0.345 |
|  | Layering Pattern | 0.034 | < 0.001 | 0.492 | < 0.001 | 0.022 |
|  | Material Ratio | 0.414 | 0.258 | 0.628 | 0.186 | 0.946 |
|  | Number of Layers & Layering Pattern | NA | NA | NA | NA | NA |
|  | Number of Layers & Material Ratio | NA | NA | NA | NA | NA |
|  | Layering Pattern & Material Ratio | NA | NA | NA | NA | NA |
| 5 mm | Number of Layers | < 0.001 | 0.002 | 0.048 | < 0.001 | < 0.001 |
|  | Layering Pattern | 0.0417 | < 0.001 | 0.002 | < 0.001 | 0.002 |
|  | Material Ratio | 0.112 | 0.324 | 0.890 | 0.444 | 0.529 |
|  | Number of Layers & Layering Pattern | < 0.001 | 0.171 | 0.122 | 0.368 | 0.018 |
|  | Number of Layers & Material Ratio | NA | NA | NA | NA | NA |
|  | Layering Pattern & Material Ratio | 0.004 | 0.662 | 0.692 | 0.803 | 0.542 |