SUPPLEMENTARY INFORMATION FOR:

Development of a sample preparation procedure for Sr isotope analysis of Portland cements

Anera Kazlagić1, Francesco F. Russo1, Jochen Vogl1, Patrick Sturm2, Dietmar Stephan3, 
Gregor J. G. Gluth2

1 Federal Institute for Materials Research and Testing, Division 1.1 Inorganic Trace Analysis, Richard-Willstäter-Straße 11, 12489 Berlin, Germany

2 Federal Institute for Materials Research and Testing, Division 7.4 Technology of Construction Materials, Unter den Eichen 87, 12205 Berlin, Germany

3 Technische Universität Berlin, Department of Civil Engineering, Building Materials and Construction Chemistry, Gustav-Meyer-Allee 25, 13355 Berlin, Germany

Correspondence to: anera.kazlagic@bam.de

Contents

AbbreviationsS-2

EquationS-2

Fig. S1S-3

Fig. S2S-4

Fig. S3S-5

Fig. S4S-6

Fig. S5S-7

Table S1S-8

Table S2S-9

Table S3S-10

Table S4S-11

Table S5S-12

Table S6S-13

Table S7S-14

Abbreviations:

Sieving – sieving on 11-µm sieve

KOSH - potassium hydroxide/sucrose solution

Conc. acid - Concentrated hydrochloric acid/nitric acid dissolution

Dil. acid - Dilute nitric acid dissolution

Equation:

Δabs= 87Sr 86Srcement- 87Sr 86Srclinker#1

Legend:

Δabs - Absolute difference of processed cement from the clinker

(87Sr/86Sr)cement – Sr isotope ratio of processed cement

(87Sr/86Sr)clinker – Sr isotope ratio of the clinker

Fig. S1. X-ray diffractogram of non-treated cement (directly on top of the sample code) and sieved cement (on top of the respective non-treated pattern) for samples 3022, 3024, 3026, 3027 and 3028. G = Gypsum, A = Anhydrite.

Fig. S2. X-ray diffractogram of non-treated cement (directly on top of the sample code) and sieved cement (on top of the respective non-treated pattern) for samples 3029, 3030,3032, 3050 and 3062. G = Gypsum, A = Anhydrite.

Fig. S3. X- ray diffractogram of non-treated cement (directly on top of the sample code) and sieved cement (on top of the respective non-treated pattern) for samples 3063, 3064, 3075, and 3078. G = Gypsum, A = Anhydrite.

Fig. S4. X-ray diffractograms of the clinker samples 3022b, 3028b, 3050b, 3063b and 3078b after conc. acid treatment; A = anhydrite, z2 = zeolite-type phase.

Fig. S5. Comparison of 87Sr/86Sr isotope ratios from fifteen cement samples prepared with sieving and subsequent conc. acid treatment (purple) and fifteen corresponding clinker samples after conc. acid treatment (blue-green).

Table S1. 87Sr/86Sr isotope ratio of processed clinkers, and cements after the KOSH and sieving treatment and clinker. 2SE represents 2 x Standard Error (Standard Deviation divided by the square root of number of measured isotope ratios).

| Sample | 87Sr/86Sr (clinker) | 2SE x 10-5 (clinker) | 87Sr/86Sr (KOSH) | 2SE x 10-5 (KOSH) | 87Sr/86Sr (Sieving) | 2SE x 10-5 (Sieving) |
| --- | --- | --- | --- | --- | --- | --- |
| 3022 | 0.70807 | 1 | 0.70810 | 1 | 0.70807 | 1 |
| 3024 | 0.70798 | 1 | 0.70816 | 1 | 0.70811 | 1 |
| 3026 | 0.70818 | 3 | 0.70812 | 7 | 0.70809 | 1 |
| 3027 | 0.70814 | 1 | 0.70888 | 6 | 0.70886 | 1 |
| 3028 | 0.70826 | 1 | 0.70827 | 1 | 0.70825 | 2 |
| 3029 | 0.70792 | 1 | 0.70816 | 1 | 0.70785 | 1 |
| 3030 | 0.70802 | 1 | 0.70795 | 1 | 0.70794 | 1 |
| 3032 | 0.70880 | 1 | 0.70899 | 1 | 0.70858 | 1 |
| 3050 | 0.70783 | 1 | 0.70782 | 1 | 0.70783 | 1 |
| 3062 | 0.70803 | 3 | 0.70838 | 1 | 0.70824 | 1 |
| 3063 | 0.70910 | 1 | 0.70927 | 1 | 0.70918 | 1 |
| 3064 | 0.70867 | 1 | 0.70874 | 1 | 0.70849 | 1 |
| 3075 | 0.70898 | 1 | 0.70897 | 1 | 0.70863 | 1 |
| 3076 | 0.70919 | 1 | 0.70896 | 1 | 0.70880 | 1 |
| 3078 | 0.70936 | 1 | 0.71012 | 2 | 0.70951 | 1 |

Table S2.  87Sr/86Sr isotope ratio of processed cements after the dil. acid and conc. acid treatment.

| Sample | 87Sr/86Sr (Dil. Acid) | 2SE x 10-5 (Dil. Acid) | 87Sr/86Sr (Conc. Acid) | 2SE x 10-5 (Conc. Acid) |
| --- | --- | --- | --- | --- |
| 3022 | 0.70804 | 1 | 0.70803 | 1 |
| 3024 | 0.70811 | 1 | 0.70812 | 1 |
| 3026 | 0.70808 | 1 | 0.70808 | 1 |
| 3027 | 0.70881 | 1 | 0.70881 | 3 |
| 3028 | 0.70823 | 1 | 0.70824 | 1 |
| 3029 | 0.70783 | 1 | 0.70786 | 1 |
| 3030 | 0.70793 | 1 | 0.70795 | 2 |
| 3032 | 0.70856 | 1 | 0.70859 | 1 |
| 3050 | 0.70781 | 1 | 0.70783 | 1 |
| 3062 | 0.70821 | 1 | 0.70821 | 1 |
| 3063 | 0.70917 | 1 | 0.70917 | 3 |
| 3064 | 0.70848 | 1 | 0.70848 | 1 |
| 3075 | 0.70860 | 1 | 0.70861 | 1 |
| 3076 | 0.70879 | 1 | 0.70881 | 1 |
| 3078 | 0.70946 | 1 | 0.70948 | 1 |

Table S3. Absolute difference Δabs between the 87Sr/86Sr isotope ratio of the cement and the 87Sr/86Sr isotope ratio of the corresponding clinker for the four investigated preparation methods. Δabs was calculated using equation (1).

| Sample | Δabs (KOSH) x 10-5 | Δabs (sieving) x 10-5 | Δabs (dil. acid) x 10-5 | Δabs (conc. acid) x 10-5 |
| --- | --- | --- | --- | --- |
| 3022 | 2 | 0.03 | 4 | 4 |
| 3024 | 18 | 14 | 13 | 14 |
| 3026 | 6 | 10 | 11 | 10 |
| 3027 | 73 | 72 | 66 | 66 |
| 3028 | 2 | 1 | 3 | 2 |
| 3029 | 24 | 7 | 8 | 5 |
| 3030 | 7 | 8 | 9 | 7 |
| 3032 | 19 | 22 | 23 | 20 |
| 3050 | 1 | 0.3 | 2 | 1 |
| 3062 | 34 | 21 | 18 | 18 |
| 3063 | 18 | 8 | 7 | 7 |
| 3064 | 6 | 18 | 19 | 19 |
| 3075 | 1 | 36 | 39 | 37 |
| 3076 | 24 | 39 | 40 | 38 |
| 3078 | 76 | 16 | 10 | 12 |

Table S4. Results of the paired t-test for 87Sr/86Sr isotope ratios of clinker and KOSH 87Sr/86Sr isotope ratios of cements as calculated with Excel (Office 365).

| t-Test: Paired Two Sample for Means |  |  |
| --- | --- | --- |
|  | 87Sr/86Sr Clinker | 87Sr/86Sr KOSH |
| Mean | 0.708436 | 0.708592 |
| Variance | 2.74E-07 | 3.8E-07 |
| Observations | 15 | 15 |
| Pearson Correlation | 0.891731 |  |
| Hypothesized Mean Difference | 0 |  |
| df | 14 |  |
| t Stat | -2.15852 |  |
| P(T<=t) one-tail | 0.024369 |  |
| t Critical one-tail | 1.76131 |  |
| P(T<=t) two-tail | 0.048737 |  |
| t Critical two-tail | 2.144787 |  |

Table S5. Results of the paired t-test for clinker 87Sr/86Sr isotope ratios and sieving 87Sr/86Sr isotope ratios of cements as calculated with Excel (Office 365).

| t-Test: Paired Two Sample for Means |  |  |
| --- | --- | --- |
|  | 87Sr/86Sr Clinker | 87Sr/86Sr Sieved |
| Mean | 0.708436 | 0.708429 |
| Variance | 2.74E-07 | 2.48E-07 |
| Observations | 15 | 15 |
| Pearson Correlation | 0.865751 |  |
| Hypothesized Mean Difference | 0 |  |
| df | 14 |  |
| t Stat | 0.107146 |  |
| P(T<=t) one-tail | 0.458097 |  |
| t Critical one-tail | 1.76131 |  |
| P(T<=t) two-tail | 0.916194 |  |
| t Critical two-tail | 2.144787 |  |

Table S6. Results of the paired t-test for clinker 87Sr/86Sr isotope ratios and dil. acid 87Sr/86Sr isotope ratios of cements as calculated with Excel (Office 365).

| t-Test: Paired Two Sample for Means |  |  |
| --- | --- | --- |
|  | 87Sr/86Sr Clinker | 87Sr/86Sr Dil |
| Mean | 0.708436 | 0.708406 |
| Variance | 2.74E-07 | 2.41E-07 |
| Observations | 15 | 15 |
| Pearson Correlation | 0.873467 |  |
| Hypothesized Mean Difference | 0 |  |
| df | 14 |  |
| t Stat | 0.447992 |  |
| P(T<=t) one-tail | 0.330507 |  |
| t Critical one-tail | 1.76131 |  |
| P(T<=t) two-tail | 0.661014 |  |
| t Critical two-tail | 2.144787 |  |

Table S7. Results of the paired t-test for clinker 87Sr/86Sr isotope ratios and conc. acid 87Sr/86Sr isotope ratios of cements as calculated with Excel (Office 365).

| t-Test: Paired Two Sample for Means |  |  |
| --- | --- | --- |
|  | 87Sr/86Sr Clinker | 87Sr/86Sr conc |
| Mean | 0.708436 | 0.708419 |
| Variance | 2.74E-07 | 2.41E-07 |
| Observations | 15 | 15 |
| Pearson Correlation | 0.877963 |  |
| Hypothesized Mean Difference | 0 |  |
| df | 14 |  |
| t Stat | 0.259105 |  |
| P(T<=t) one-tail | 0.399662 |  |
| t Critical one-tail | 1.76131 |  |
| P(T<=t) two-tail | 0.799325 |  |
| t Critical two-tail | 2.144787 |  |

Each cement sample was loaded on a single filament, and the standard deviation was then calculated from minimum 100, maximum 200 measured isotope ratios.