Supporting Information

pH-Tuned Reversible Self-Assembly of Janus Particles for Enhanced Raman Imaging and Sensing

Maria Iftesum1, ‖, Mohan Kumar Dey1,†, Alisha Prasad2,†, Jin Gyun Lee3,‖, Ram Devireddy1, Bhuvnesh Bharti3, Manas Ranjan Gartia1,*

1Department of Mechanical and Industrial Engineering, Louisiana State University, Baton Rouge, LA 70803 USA

2Catalent Pharma, St. Petersburg, FL 33716 USA

3Cain Department of Chemical Engineering, Louisiana State University, Baton Rouge, LA 70803 USA

†, ‖Equal contribution authors

*Corresponding author: mgartia@lsu.edu

Table S1. Raman peak positions for the different components of the Janus Particles

|  | PS | 11-MUA | EDC | Lysozyme | Au + PS | Au + PS + MUA | Au + PS + MUA + EDC | Au + PS + MUA + EDC + Lys |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 450 - 550 |  |  |  | 471, 527 |  |  |  |  |
| 551 - 650 | 622 |  |  | 622, 648 | 624 |  | 624 | 624 |
| 651 - 750 |  | 738 |  |  |  |  |  |  |
| 751 - 850 | 798 |  | 827 | 755, 798 | 793 |  |  |  |
| 851 - 950 |  | 909 |  |  |  |  |  |  |
| 951 - 1050 | 1005, 1029 |  |  |  | 1004, 1033 | 1004, 1033 | 1004, 1033 | 1004, 1033 |
| 1051 - 1150 |  | 1060, 1107 | 1149 | 1122 |  | 1197 |  | 1191 |
| 1151 - 1250 | 1157, 1205 |  |  |  | 1201 |  | 1203 |  |
| 1251 - 1350 |  | 1290 |  | 1255 |  |  |  |  |
| 1351 - 1450 |  | 1436 |  |  |  |  |  |  |
| 1451 - 1550 | 1452 | 1457 | 1454 |  | 1451 |  |  |  |
| 1551 - 1650 | 1603 | 1631 | 1642 | 1551 | 1603 | 1605 | 1602 | 1604 |
| 1651 - 1750 |  |  |  | 1715 |  |  |  |  |
| 1751 - 1850 |  |  |  |  |  |  |  |  |
| 1851 - 1950 |  |  |  | 1883 |  |  |  |  |
| 1951 - 2050 |  |  |  |  |  |  |  |  |
| 2051 - 2150 |  |  |  |  |  |  |  |  |
| 2151 - 2250 |  |  |  |  |  |  |  |  |
| 2251 - 2350 |  |  |  |  |  |  |  |  |
| 2351 - 2450 |  |  |  |  |  |  |  |  |
| 2451 - 2550 |  | 2549 |  |  |  |  |  |  |
| 2551 - 2650 |  | 2575 |  |  |  |  |  |  |
| 2651 - 2750 |  | 2722 |  |  |  |  |  |  |

Figure S1. Schematic of FDTD Simulation for one, two, and three Janus particles using Ansys Lumerical software.