## Slide 1
Supplementary figures
Alan Boyde, QMUL
HAC, ACC, SCB, OsteoArthritis &
responses to overload exercise

## Slide 2
S 1Aa
Notes: Suppl. 01Aa. Another example of 20kV BSE SEM image of carbon coated, micromilled PMMA embedded block surface of distal condyle of 2 year old Thoroughbred (TB) racehorse third metacarpal bone (Mc3). HAC (top left) hyaline articular cartilage region which here shows black as it contains no mineral. ACC shows incremental mineralization-front-progress layers with more and less mineral content. It appears that there is zero or a very low mineral content after each growth arrest line (tidemark). SCB (lower right segment) is attached via a hypermineralized reversal cement line to the deep layer of the ACC. after local ‘cutting cone’ resorption events. FW = 1166µm.

## Slide 3
S 1Ab
Notes: Suppl. 1Ab. 20kV BSE SEM, ‘BioOss’ bone augmentation material used for improving dental implant survival, from an implant site trephine core sample. This material is made by calcining bovine bone. The presence of ACC and SCB proves that not only trabecular bone is used in the manufacture. The presence of the dark inter-layer lines shows the near absence of mineral.

## Slide 4
S 1Ac
Notes: Suppl. 1Ac. 20kV BSE SEM of TB Mc3 macerated in NaOCl bleach to remove non-mineralized components. The ACC is splitting where there was no mineral in the inter-layers between successive ‘tidemarks’. FW = 4450µm.

## Slide 5
S 1Ad
Notes: Suppl. 1Ad. 20kV BSE SEM of TB Mc3 macerated, another animal. The ACC has split to reveal the current ACC MF at right and the next deeper ‘tidemark’ at left. Details of the shape of the successive ‘tidemarks’ is identical. FW = 4450µm.

## Slide 6
S 1B
Notes: Suppl. 1B. Co-registration of BSE-SEM and CSLM images seen in GIF movie format, courtesy of Michael Doube [9, 10].

## Slide 7
S 1C
Notes: Suppl. 1C. 2 year old TB MC3 from the Bristol Treadmill training experiment, treadmill group, embedded in PMMA+IEMA (iodinated methacrylate). Iodine here gives negative staining contrast. Another example matching Figure 01C. Region shows less loaded dorsal part of condyle.

## Slide 8
S 1D
Notes: Suppl. 1D. GIF movie version of Figure 01D made by recording the same field of view at multiple tilt angles. 14 frames. 20kV BSE SEM image of gold coated PMMA cast of mid-shaft transverse section of 2 yr old TB Mc3. Near the centre can be seen a ‘cutting cone’ coming towards you. FW = 1937µm.

## Slide 9
S 1Ea
Notes: Suppl. 1Ea. Same image as Figure 01E, untrimmed, higher resolution. 20kV BSE SEM image of gold coated PMMA cast of marrow space at the osteo-chondral junction in a 2 year old TB Mc3 condyle, made by dissolving embedded bone with sequential acid and bleach treatments and ultrasonic dispersal of osteocyte lacunar and canalicular casts. Many ‘cutting cone’ replicas are seen, large ones with detail of the individual resorption pits by osteoclasts contrast with narrow projections which show the space in shut-down ‘osteones’. FW = 1900µm

## Slide 10
S 1Eb
Notes: Suppl. 1Eb. Same subject. Adjacent, overlapping field. In this colour version, colour shows the direction of collection of the BSE signal [39,40], i.e. colour codes for the direction of illumination by analogy with ordinary light. FW = 1900µm

## Slide 11
NZ14PE51.gif
S 2A
Notes: Suppl. 2A. GIF movie version of Fig. 2A showing the BSE-SEM and CSLM autofluorescence components separately.

## Slide 12
S 2B
Notes: Suppl. 2B. Macerated sample. HAC invasion by cutting cones. ACC MF in 6 week old foal Mc3, showing the radically different nature of the MF during rapid growth, which is much more affine to conditions in the growth plate cartilage. Two ‘canals’ penetrate the ACC and it is possible that they were occupied by one capillary blood vessel loop. A thin shell of bone has formed lining the right hand canal. FW = 900µm.

## Slide 13
S 2CD
50% ev 4°
Notes: Suppl. 2CD. Same field as Figure 2C,D. 20kV BSE SEM images of vertical section through superior surface ACC MF of femoral head of 33 year old male, GIF movie version to show 3D.The same field was imaged at multiple tilt angle differences. FW 2700µm.

## Slide 14
S 2EF
50% ev 4°
Notes: Suppl. 2EF. Same field as Figure 2EF. Superior surface of femoral head of 75 year old male, MF ACC. GIF movie version to show 3D.The same field was imaged at multiple 2°tilt angle differences.
To view this using ImageJ, go to Stacks: Animation: Animation Options and choose ‘to and fro’ and frame speed 10fps. FW 2700µm.

## Slide 15
3D
Notes: Suppl. 3D. 20kV BSE SEM, femoral head of a PM reference case. FW = 1782 µm.

## Slide 16
S 3D
Notes: Suppl. 3D. Densification by forming new bone in prior marrow space in SCB in human OA femoral head. Quantitative BSE SEM image. Quantitative BSE SEM image, same field as Figure 3D. Pseudocoloured version of Figure 3D using ImageJ 16cols LUT. FW = 1350µm.

## Slide 17
3E
Notes: Suppl. 3E. 20kV BSE SEM, femoral head of a PM reference case. FW = 1782 µm.

## Slide 18
S 3E
Notes: Suppl. 3E. 20kV BSE SEM, femoral head of a PM reference case. Pseudocoloured version of Figure 3E. ImageJ 16cols LUT. FW = 1782 µm.

## Slide 19
3F
Notes: Suppl. 3F. 20kV BSE SEM showing deep subchondral trabecular bone in an OA (elective arthroplasty) femoral head. FW = 1114µm.

## Slide 20
S 3F
Notes: Suppl. 3F. 20kV BSE SEM showing deep subchondral trabecular bone in an OA (elective arthroplasty) femoral head. Differences in the fabric density of the old and the repair bone are better seen in this pseudocoloured version of Figure 3F. ImageJ 16cols LUT. FW = 1114µm.

## Slide 21
S 7A
Notes: Suppl. 7A. HDMP in human patella OA. Macerated sample showing ACC MF with HDMP at centre. 20kV BSE SEM.

## Slide 22
9A
Notes: Fig. 9A. Human OA. Articular surface at top is eburnated and SCB is dense with much prior marrow space filled. FW =2700µm.

## Slide 23
S 9A
Notes: Suppl. 9A. Human OA. Articular surface at top is eburnated and SCB is dense with much prior marrow space filled. Pseudocolour version of Figure 09A, ImageJ 16cols LUT . FW =2700µm.

## Slide 24
S 9Da
Notes: Suppl. 9Da. 20kV 3D BSE-SEM, macerated Mc3 condyle of Tb, large POD lesion. Anaglyph stereo-pair version for viewing with Red (for left eye) and Cyan filter spectacles. Tilt angle difference = 6°. Same field as Figure 09D rotated 90° for stereo viewing. Surface left is eburnated over elevations: at right is the cut surface of the slice: Extensive cavity with numerous osteoclastic resorption profiles. FW =1782µm.

## Slide 25
S 09Db
Notes: Suppl. 9Db. Same field as GIF movie file with 3 views at 6° tilt angle differences. FW = 1782µm.
To view this using ImageJ, go to Stacks: Animation: Animation Options and choose ‘to and fro’ and frame speed 4fps.

## Slide 26
S 9Ea
Notes: Suppl. 9Ea. Same field as Figure 9E but field rotated 90°, as an anaglyph stereo-pair, tilt angle difference = 6°. POD lesion in TB MC3 condyle. Surface right is eburnated and flat. Left is the cut surface of the slice with an extensive cavity with numerous osteoclastic resorption profiles. FW = 2700µm.

## Slide 27
S 9Eb
Notes: Suppl. 9Eb. Same field as Figure 9E and Suppl 09Ea as a GIF movie. Eburnated surface below, cut surface top. FW = 2700µm.
To view this using ImageJ, go to Stacks: Animation: Animation Options and choose ‘to and fro’ and frame speed 4fps.

## Slide 28
S 9Fa
Notes: Suppl. 9Fa. Macerated Mc3 condyle of Tb horse. Part of an extensive POD lesion (ulcer) cavity with numerous osteoclastic resorption profiles. One spot only (towards top left side) of the surface is eburnated. Anaglyph stereo pair. Same field as Figure 09F. FW = 1782µm.

## Slide 29
S 9Fb
Notes: Suppl. 9Fb. Same field as GIF movie file with 3 views at 6° tilt angle differences. FW = 1782µm.

## Slide 30
S 10A
Notes: Suppl.10A. Higher magnification view of part of Fig 10A. Cavitation and repair in equine OA (POD). Base of extensive cavity in a POD lesion being repaired with new woven bone formation towards top and right showing the numerous and large, closely spaced osteocyte lacunae. FW 900µm.

## Slide 31
S 10C
Notes: Suppl. 10C. Higher magnification version of 20kV BSE SEM montage in Figure 10C. FW = 22mm. This is a large image and can be seen as such if you modify the PPTX

## Slide 32
S 10E
Notes: Suppl. 10E. Colour version of Figure 10E. Extensive POD lesion cavity filled with dense fibrous connective tissue firmly attached to bone. Six images were recorded with 15° rotations of crossed linearly polarising filters used as Red, Yellow, Green, Cyan. Magenta in colour circle sequence. Colour codes for orientation of collagen in plane [49]. Brightness is greatest when collagen is lying in the plane of the section. FW = 2800µm.

## Slide 33
S 10F
Notes: Suppl. 10F. TB MC3 POD lesion. Decalcified section. ACC is missing entirely in the centre of the field. Six images were recorded at 15° rotations of crossed linearly polarizing filters here shown as GIF movie [49]. FW = 3050µm.

## Slide 34
S 11B
Notes: Suppl. 11B. Macerated femoral head removed at operation for arthroplasty. Cut through sub-articular resorption cavity 20Pa chamber pressure, no coating. 20kV 3D BSE-SEM image. Same field as Figure 11B. Through tilt series of 28 frames. FW = 2800µm.

## Slide 35
S 11C
Notes: Suppl. 11C. Same case, same field as Figure 11C. Through tilt series as a 3D movie GIF file. Two surfaces at right angles: below the centreline is the naturally eburnated surface: above is a cut made and polished in the laboratory. Both show the extreme volumetric densification of the SCB by in-filling with both woven and lamellar bone.. FW = 1527µm.

## Slide 36
S 11Da
Notes: Suppl. 11Da. Same case. Same field as Figure 11D. Through focus series here showing images at 100µm mechanical focus level differences [39]. Many trabecular surfaces are covered with non-mineralized osteoid seams. FW = 2917µm.

## Slide 37
S 11Db
Notes: Suppl. 11Db. Co-morbidity of OA with osteomalacia in the reparative tissues in equine OA. TB racehorse MC3 POD lesion (for comparison with Figure 10D which showed extensive osteoid seams which appears darker than mineralized bone). 20kV BSE SEM. FW = 3570µm. Fragments of tissue in marrow spaces result from cutting this 600µm section before embedding.

## Slide 38
S 12A
Notes: Suppl. 12 A. Cartilage in bone trabecula in human distal femur OA. 10µm section prepared by Laser Ablation Microtomy [47]. Same field as figure 12A. Sequence showing LM after MacNeal’s tetrachrome staining and BSE-SEM and mixtures of the two imaging modalities. A ‘trabecula’ has hyaline cartilage at its centre which is mineralizing peripherally. FW 7367µm.

## Slide 39
S 12Da
Notes: Suppl. 12Da. (Same case as 12A and Suppl. 2Ab). Human distal femur, osteochondral junction, unstained, undecalcified 10µm Laser Ablation Machined section from osteoarthritis case (knee arthroplasty), complex polarised light image [49]. A trabecular excrescence is seen in top left of field, ACC in bottom right. FW = 1220µm. This is a higher resolution copy of Figure 12D.

## Slide 40
S 12Db
Notes: Suppl. 12 Db. Trabecular excrescences in the same case (see also Figure 12D). Another Laser Ablation Microtomy section. Level of the field is one field height above the SCB-HAC junction. Sequence shows 20kV 3D BSE SEM, pseudocoloured BSE-SEM using our in-house topo9c LUT, polarised light microscopy and LM after MacNeal’s tetrachrome staining. FW = 1620µm.