SUPPORTING INFORMATION

Exploring Wood as a Sustainable Solution for Water Filtration: Nanoparticle Removal, Size Exclusion and Molecular Adsorption

Antoni Sánchez-Ferrer*, Jenifer Guerrero Parra

Technical University of Munich, School of Life Sciences, Chair of Wood Science, D-80797 Munich, Germany

Antoni Sánchez-Ferrer*:	orcid.org/0000-0002-1041-0324; email: sanchez@hfm.tum.de

Jenifer Guerrero-Parra:						email: jenifer.guerrero@tum.de

Figure SI-1	Wood filtration disk and filtration setup		2

Figure SI-2	DLS data and fitting autocorrelation function		2

Figure SI-3	Hydrodynamic diameter as a function of particle concentration		3

Figure SI-4	Count rate as a function of particle concentration 		3

Figure SI-5	Gymnosperms and angiosperms anatomical structure		4

Figure SI-6 and SI-7	SEM image of the four wood species	5-6

Figure SI-8	Autocorrelation function and PSD for the reference dispersions	8-9

Figure SI-9 to SI-13	DLS data for the tracers before and after filtration	10-14

Figure SI-14 to SI-18	PSD for the tracers before and after filtration	15-19

Figure SI-19	Size reduction percentage of the tracers before and after filtration	20

Figure SI-20	PdI of the tracers before and after filtration	21

Figure SI-21	Manual water filtration system with a beech wood cylindrical filter	23

Figure SI-22	Structure and characteristics of the dye Molecules	24

Figure SI-23	UV-vis spectra of the dye molecules	25

Table SI-1	Density and dimensions of the anatomical features for the wood species		7

Table SI-2	Flow rate values through the three wood directions		7

Table SI-3	Nanopaerticle’s removal per mass of wood		22

(6)

(5)

(4)

(2)

(1)

(3)

Figure SI-1. Left: Wood filtration disks (50 mm diameter and 1 mm thickness at 20 °C and 65% RH). Right: Setup for the filtration experiments: graduated funnel (1), filter flask (2), aluminum clamp (3), water trap (4), pressure gauge (5), and vacuum membrane pump (6).

Figure SI-2. DLS data from a 300 ppm NCC dispersion in water (filled symbols), DLS autocorrelation function g1(t) (red curve), and the parameters obtained after the analysis following the cumulant method for polydisperse samples.

Figure SI-3. Hydrodynamic diameter dh as a function of particle concentration C for the different tracers: NCC (black), GG (red), Fe2O3 (blue), SiO2 (green) and -SiO2 (violet).

Figure SI-4. Mean count rate I0 as a function of particle concentration C for the different tracers: NCC (black), GG (red), Fe2O3 (blue), SiO2 (green) and -SiO2 (violet).

Angiosperms

Gymnosperms

Figure SI-5. Gymnosperms and angiosperms anatomical structure (Chen et al., 2020).

| A) | B) |
| --- | --- |

Figure SI-6. Scanning electron microscope image of the two gymnosperm species – A) silver fir and B) Douglas fir in the longitudinal (upper), radial (middle), and tangential (bottom) directions.

| A) | B) |
| --- | --- |

Figure SI-7. Scanning electron microscope image of the two angiosperm species – A) poplar and B) beech in the longitudinal (upper), radial (middle), and tangential (bottom) directions.

Table SI-1. Density  for the four wood species, mean diameter values d of tracheids (silver fir and Douglas fir) and vessels (poplar and beech) in the L-directions, and minor/major diameter values for rays and pits in the R- and T-direction.

| wood |  (kg/m3) | dL (m) | dR (m) | dT (m) |
| --- | --- | --- | --- | --- |
| silver fir | 415 | 30-60 | 10-16 | 4-5 |
| Douglas fir | 530 | 30-60 | 8-18 | 7-8 |
| poplar | 400 | 80-150 | 9-19 | 7-8 |
| beech | 750 | 70-90 | 9-12 | 2-5 |

Table SI-2. Average flow rates during the filtration process for the four wood species in the three directions – water and 100 ppm nanoparticles.

| Q (mL/(hcm2)) | silver fir | Douglas fir | poplar | beech |
| --- | --- | --- | --- | --- |
| L | 547 | 619 | 594 | 590 |
| R | 0.02 | 0.07 | 0.39 | 0.17 |
| T | 0.01 | 0.01 | 0.06 | 0.05 |

| A) |  |
| --- | --- |
| B) |  |
| C) |  |
| D) |  |
| E) |  |

Figure SI-8. Left: DLS data (open symbols) and autocorrelation function g1(t) (red curve) of a ca. 100 ppm dispersion of A) NCC, B) GG, C) Fe2O3, D) SiO2, and E) -SiO2 tracers. Right: Intensity particle size distribution (PSD) obtained from the deconvolution of the DLS fitting function. Note: the blue and green curves are the deconvolution curves when more than one particle distribution was present in the sample.

Figure SI-9. DLS data for the 130 ppm NCC dispersion (black), and after filtration for the four different wood species in the three orthotropic directions.

Figure SI-10. DLS data for the 104 ppm GG dispersion (black), and after filtration for the four different wood species in the three orthotropic directions.

Figure SI-11. DLS data for the 105 ppm Fe2O3 dispersion (black), and after filtration for the four different wood species in the three orthotropic directions.

Figure SI-12. DLS data for the 100 ppm SiO2 dispersion (black), and after filtration for the four different wood species in the three orthotropic directions.

Figure SI-13. DLS data for the 115 ppm -SiO2 dispersion (black), and after filtration for the four different wood species in the three orthotropic directions.

| A) | B) |
| --- | --- |
| C) | D) |

Figure SI-14. Intensity particle size distribution (PSD) of the NCC filtrates in the three directions (L, red; R, blue; T, green) for the four different wood species: A) silver fir, B) Douglas fir, C) poplar, and D) beech. The black curves correspond to the ca. 100 ppm dispersion before filtering.

| A) | B) |
| --- | --- |
| C) | D) |

Figure SI-15. Intensity particle size distribution (PSD) of the GG filtrates in the three directions (L, red; R, blue; T, green) for the four different wood species: A) silver fir, B) Douglas fir, C) poplar, and D) beech. The black curves correspond to the ca. 100 ppm dispersion before filtering.

| A) | B) |
| --- | --- |
| C) | D) |

Figure SI-16. Intensity particle size distribution (PSD) of the Fe2O3 filtrates in the three directions (L, red; R, blue; T, green) for the four different wood species: A) silver fir, B) Douglas fir, C) poplar, and D) beech. The black curves correspond to the ca. 100 ppm dispersion before filtering.

| A) | B) |
| --- | --- |
| C) | D) |

Figure SI-17. Intensity particle size distribution (PSD) of the SiO2 filtrates in the three directions ((L, red; R, blue; T, green) for the four different wood species: A) silver fir, B) Douglas fir, C) poplar, and D) beech. The black curves correspond to the ca. 100 ppm dispersion before filtering.

| A) | B) |
| --- | --- |
| C) | D) |

Figure SI-18. Intensity particle size distribution (PSD) of the -SiO2 filtrates in the three directions (L, red; R, blue; T, green) for the four different wood species: A) silver fir, B) Douglas fir, C) poplar, and D) beech. The black curves correspond to the ca. 100 ppm dispersion before filtering.

Figure SI-19. Size reduction percentage for the four wood species (S = silver fir, D = Douglas fir, P = poplar, B = beech) in the three directions (L, R and T) for the five tracers (NCC, GG, Fe2O3, SiO2 and -SiO2) after filtration. The orange dotted line corresponds to 100% efficiency.

Figure SI-20. Polydispersity index of the filtrates for the four wood species (S = silver fir, D = Douglas fir, P = poplar, B = beech) in the three directions (L, R and T) with the five tracers (NCC, GG, Fe2O3, SiO2 and -SiO2) after filtration. The orange dotted line corresponds to 100% efficiency.

Table SI-3. Nanoparticles removal per mass of wood for each tracer and for the four wood species and the three directions (L, R and T). The concentration before filtration for NNC, GG, Fe2O3, SiO2 and
-SiO2 was 130, 104, 105, 100 and 115 ppm, respectively.

| wood m (g) | direction | NPs removal (mg/g) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | NCC | GG | Fe2O3 | SiO2 | -SiO2 |
| silver fir 0.471 g | L | 0 | 0.8 | 1.6 | 0.1 | 2.1 |
|  | R | 0 | 0.9 | 2.2 | 0.7 | 2.0 |
|  | T | 0 | 0.8 | 2.2 | 1.2 | 2.0 |
| Douglas fir 0.601 g | L | 0 | 0.3 | 0.8 | 0.2 | 1.5 |
|  | R | nd | 0 | 1.7 | 0.4 | 1.6 |
|  | T | nd | 0 | 1.5 | nd | 1.7 |
| poplar 0.454 g | L | 0 | 0.8 | 1.7 | 0.1 | 2.3 |
|  | R | 0 | 0.2 | 1.7 | 0 | 2.3 |
|  | T | 0.7 | 0.8 | 2.3 | 0.1 | 2.3 |
| beech 0.851 g | L | 0 | 0.5 | 0.9 | 0.1 | 1.2 |
|  | R | 0.1 | 0.7 | 1.2 | 0.6 | 1.1 |
|  | T | 0 | 0.2 | 1.2 | 0.4 | 1.2 |

Figure SI-21. Details of a manual water filtration system using a cylinder of 4.5 mm in length and 2.5 mm in diameter beech wood sample in the L-direction. A) Filtration system and beech wood filter. B) Filtration of 100 ppm Fe2O3 NPs. C) Filtration of 1000 ppm -SiO2 particles.

A) mw = 319 Da, V = 0.269 nm3, Vexc = 0.856 nm3,  = 4.3 D, Rg = 0.40 nm, dmax = 1.4 nm

B) AZ4 AZ12 (AZ4) mw = 228 Da, V = 0.213 nm3, Vexc = 0.725 nm3,  = 1.6 D, Rg = 0.39 nm, dmax = 1.4 nm (AZ12) mw = 227 Da, V = 0.210 nm3, Vexc = 0.715 nm3,  = 14.1 D, Rg = 0.39 nm, dmax = 1.4 nm

C) PH4 PH12 (PH4) mw = 318 Da, V = 0.282 nm3, Vexc = 0.880 nm3,  = 2.6 D, Rg = 0.35 nm, dmax = 1.0 nm (PH12) mw = 317 Da, V = 0.283 nm3, Vexc = 0.886 nm3,  = 25.5 D, Rg = 0.35 nm, dmax = 1.0 nm

Figure SI-22. Molecular structure, charge density (blue: negative; red: positive), molar mass, molecular volume, excluded volume, dipole moment, radius of gyration and the largest molecular distance for the three dye molecules: A) methylene blue (MB), B) azobenzene (AZ), and C) phenolphthalein (PH).

Figure 23. UV-vis spectra of methylene blue (pH 7) – blue -, phenolphthalein (pH 4) – black -, phenolphthalein (pH 12) – violet -, and azobenzene (pH 12) – orange – with the corresponding peak maxima.