Supporting Information:

Towards the Clinical Translation of a Silver Sulfide Nanoparticle Contrast Agent: Large Scale Production with a Highly Parallelized Microfluidic Chip

Katherine J. Mossburg1,2*, Sarah J. Shepherd1*, Diego Barragan2,3, Nathaniel H. O2,4,5, Emily K. Berkow2,6, Portia S. N. Maidment2, Derick N. Rosario Berrios2,7, Jessica C. Hsu1,2┼, Michael J. Siedlik8, Sagar Yadavali8, Michael J. Mitchell1,9, David Issadore1,10,11**, David P. Cormode1,2,9**

1Department of Bioengineering, University of Pennsylvania, Philadelphia, PA, USA

2Department of Radiology, University of Pennsylvania, Philadelphia, PA, USA

3Department of Biology, University of Pennsylvania, Philadelphia, PA, USA

4Department of Pharmaceutical Sciences, St. Joseph’s University, Philadelphia, PA, USA

5Department of Physics, St. Joseph’s University, Philadelphia, PA, USA

6Department of Chemistry, University of Pennsylvania, Philadelphia, PA, USA

7Biochemistry and Molecular Biophysics Graduate Group, University of Pennsylvania, Philadelphia, PA, USA

8InfiniFluidics, Inc, Philadelphia, PA, USA

9 Cardiovascular Institute, Perelman School of Medicine, University of Pennsylvania, PA, USA

10 Department of Electrical and Systems Engineering, University of Pennsylvania, PA, USA

11 Department of Chemical and Biomolecular Engineering, University of Pennsylvania, PA, USA

┼This author’s current affiliation is the Departments of Radiology and Medical Physics, University of Wisconsin-Madison, Madison, WI, USA.

*These authors contributed equally to this work.

**Corresponding authors.

Emails: issadore@seas.upenn.edu; david.cormode@pennmedicine.upenn.edu

Figure S1. Ag2S-NP A) product size as evaluated by TEM and B) concentration as evaluated by ICP measured over time during synthesis by a 1X SSMS chip.

Figure S2. UV-visible absorption spectra of Ag2S-NP immediately after synthesis (pre-concentration) and after concentration and washing using molecular weight cut off tubes (post-concentration).

Figure S3. Table of zeta potential values for each Ag2S-NP synthetic condition.

Figure S4. X-ray diffraction patterns of Ag2S-NP from each synthesis method.

Figure S5. Survey XPS spectra of each type of Ag2S-NP.

Figure S6. FT-IR spectra of each synthesis method of Ag2S-NP.

Figure S7. HR-TEM micrograph of representative CS-Ag2S-NP, showing 0.3 nm lattice fringe distance.

Figure S8. Representative µCT images showing Ag2S-NP being renally cleared through A) the kidneys (yellow circle) and B) the bladder (green circle).

Figure S9. Quantification of CT attenuation in the A) heart and B) liver at each time point. n=5 per group. Data is presented as mean ± SEM.

Figure S10. Silver content retained by the carcass and the tail of mice injected with Ag2SNP.