Supplementary information

Rapid adsorptive and optimization of batch process for removal of methylene blue using hybrid GA@SnO2-AC composite materials

John Busayo Adeoye1,2*, Sie Yon Lau1,11*, Yie Hua Tan3*, Yee Yong Tan4, Tung Chiong1, Nabisab Mujawar Mubarak5,6,7, Mohammad Khalid8,9, Jeffrey Tze Wei Ng10

1Department of Chemical and Energy Engineering, Faculty of Engineering and Science, Curtin University Malaysia, CDT 250, 98009 Miri, Sarawak, Malaysia

2Department of ChemicalEngineering,Covenant University, Ota, Ogun State, Nigeria

3Chemical and Energy Engineering, Faculty of Engineering, UniversitiTeknologi Brunei, Gadong, BE1410, Brunei Darussalam

4Department of Civil and Construction Engineering, Faculty of Engineering and Science, Curtin University Malaysia, CDT 250, Miri, Sarawak, 98009, Malaysia

5Department of Chemical Engineering, College of Engineering, Imam Mohammad Ibn Saud Islamic University(IMSIU), Riyadh, 11432, Saudi Arabia

6Department of Biosciences, Saveetha School of Engineering, Saveetha Institute of Medical and Technical Sciences, Chennai, India

7Centre for Research Impact and Outcome, Chitkara University, Rajpura, Punjab, 140401, India

8James Watt School of Engineering, University ofGlasgow, G12 8QQ Glasgow, UK

9Manipal Institute of Technology, Manipal Academy of Higher Education, Manipal, Karnataka, 576104, India

10Enforture Sdn Bhd, 3, Jalan Hi-Tech 3/1, Semenyih Hi-Tech 3 Industrial Park, Semenyih, Selangor, 43500, Malaysia

11Center of Excellence in New and Sustainable Energy Research and Ventures (CONSERV), Curtin University Malaysia, CFT 250, Miri, Sarawak, 98009, Malaysia

*Corresponding Author: johnadeoye@postgrad.curtin.edu.my, johnlsy@curtin.edu.my   yiehua.tan@utb.edu.bn

Text S1. Isotherm, kinetics, and thermodynamic equations

Isotherms adsorption study

The Langmuir model was used to describe the adsorption equilibrium between the adsorbent and adsorbate systems, in which adsorbate adsorption is limited to a molecular layer before a relative pressure of unity is attained. The linearized form is evaluated using the Langmuir equation in Table S1, where qmax is the maximum adsorption capacity of metal ions (mg/g).

The Freundlich model is based on the interaction of adsorbed molecules in an adsorption multilayer. The linearized form of the Freundlich model equation is given as in Table S1, where KF and n are the Freundlich constant; n gives speculations about the favourability of the adsorption process, and KF is the metal ions adsorption capacity.

The adsorption effect on adsorbate interactions was described by the Temkin model.

The linearized form of the equation is given as in Table S1, where KT (L/mg) is the Temkin model constant, and B is the heat adsorption (kJ/mol). Where indicates the adsorbent adsorption potential, R is the universal gas constant (8.314 J/mol K), and T (K) is the temperature.

The Dubinin-Radushkevich helps to determine the type of adsorption process present, whether chemisorption or physisorption. The Linearized form is given in Table S1, where qs is the saturation adsorption capacity, mg/g; K is the activity constant-coefficient- constant related to adsorption capacity; Ԑ2 is the Polanyi potential (kJ/mol), and E is the mean free energy of adsorption (J/mol).

The Polanyi potential is estimated using the Eq. (8)(8)

The mean adsorption energy E in KJ/mol is estimated using Eq. (9)(9)

Table S1. Detailed information of Isotherm, kinetic, and thermodynamic equations.

| Type | Models | Linear Equations | Parameters |
| --- | --- | --- | --- |
| Isotherm models | Langmuir | Ceqe=1qmCe+1KLqm | qm: is the maximum adsorption capacity (mg/g); Ce: is the TC and MB concentrations at equilibrium (mg/L); KL: is the Langmuir constant (L/mg). |
|  | Freundlich | lnln qe =lnln Kf+1n lnln Ce | KF and n: are the Freundlich constants. |
|  | Temkin | qe=BTlnln KT + BTlnln ce | KT: is the Temkin equilibrium binding constant, corresponding to binding energy (L/mg), BT: is Temkin constant in relative to heat of adsorption (J/mol). |
|  | Dubinin-Radushkevich (D-R) | lnln qe= lnln qs - βε2 | qs is the maximum sorption capacity, qe is the quantity of pollutant adsorbed per unit weight of the adsorbent (mg/g) |
| Kinetics models | Pseudo-first order (PFO) | lnln qe-qt =lnln qe-K1t | qe: is the adsorption capacity at equilibrium (mg/g); qt: is the adsorption capacity at time (mg/g), t; k1: is the PFO adsorption rate constant (min-1). |
|  | Pseudo-second order (PSO) | tqt=1K2qe2+1qet | k2: is the adsorption rate constant ((g/(mg·min)). |
|  | Elovich model | qt=1βe lnln αe βe+1βelnln t | α: is the Elovich initial adsorption rate constant (mg/(g·min); β is the Elovich desorption coefficient (mg/g). |
|  | Intra-particle diffusion | qt=Kipt1/2+C | Ki (mg/(g·min0.5)): is the intraparticle rate constant; Ci (mg/g): is the film thickness of intra-particle diffusion adsorption. |
| Thermodynamic equations |  | ∆G=-RTlnln Kd ∆G=∆H-T∆S=-RTlnln Kc lnln Kd=∆SR-∆HRT Kd=qeCe | Keo: is the thermodynamic equilibrium constant (dimensionless); Mw is the MB or TC molecular weight (g/mol); γ is the coefficient activity, and [C]° is the pollutants standard concentration; T is the absolute temperature (K) and R is the ideal gas constant (8.314 J/mol. K). |

References

Adeoye JB, Balogun DO, Etemire OJ, Ezeh PN, Tan YH, Mubarak NM (2023) Rapid adsorptive removal of eosin

yellow and methyl orange using zeolite Y. Scientific Reports. 4;13(1):21373. https://doi.org/10.1038/s41598-023-48675-4