Table 2. Commercial name, manufacturer, material, length and diameter of the stents used in the study. SS=stainless steel; PTFE=polytetrafluorethylene; SC=Silicon Carbide; *this stent will be named Lekton2 throughout the article
Name
Manufacturer
Material
Length [mm]
Diameter [mm]

Micro II
AVE
SS 316L
15.5 ± 0.3
3.6 ± 0.1

Jostent Stent Graft
Jomed
SS 316L + PTFE graft
14.8 ± 0.3
2.8 ± 0.1

Lekton
Biotronik
SS 316L + PTFE graft
13.5 ± 0.3
3.4 ± 0.1

Lekton*
Biotronik
SS 316L SC coating + markers
12.7 ± 0.3
3.0 ± 0.1

Lekton Motion
Biotronik
SS 316L + SC coating + markers
19.7 ± 0.3
3.0 ± 0.1

Cypher
Cordis
SS 316L
17.7 ± 0.3
2.7 ± 0.1

Bx Sonic
Cordis
SS 316L
10.6 ± 0.3
3.0 ± 0.1

Taxus
Boston Scientific
SS 316L
12.5 ± 0.3
3.2 ± 0.1

Multi-link Zeta
Guidant
SS 316L
15.7 ± 0.3
3.1 ± 0.1

