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	Figure S1. Optical microscope images of single-layer fibrous tissue scaffolds containing bioactive glass (crosslinked with 2% CaCl₂); (a) 5BG-SA; (b)15BG-SA; (c) 30BG-SA; (d) 60BG-SA. Scale bars: 2000 µm (left), 700 µm (right).


[bookmark: _GoBack]Figure S2. UV-Vis spectrum of the AMOX solution (1 mg/ml) prepared in DI water.
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Figure S3. Graphs showing the compatibility of AMOX release from microfibers prepared within the scope of the study in the first 48 hours with the Korsmeyer-Peppas model; (a) 0BG-SA, (b) 5BG-SA, (c) 10BG-SA, (d) 15BG-SA, (e) 30BG-SA and (f) 60BG-SA.
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Figure S4. Graphs showing the compatibility of AMOX release from microfibers prepared in the study between 48-400 hours with the Korsmeyer-Peppas model; (a) 0BG-SA, (b) 5BG-SA, (c) 10BG-SA, (d) 15BG-SA, (e) 30BG-SA and (f) 60BG-SA.

oleObject3.bin

image5.emf
10BG-SA


Log Time (h)


-0,5


0,0


0,5


1,0


1,5


2,0


Log Cumulative Drug Release (%)


0,4


0,5


0,6


0,7


0,8


0,9


1,0


1,1


1,2


y= 0,296x + 0,6152


        R


2


 = 0,9332




10BG-SA

Log Time (h)

-0,5 0,0 0,5 1,0 1,5 2,0

Log Cumulative Drug Release (%)

0,4

0,5

0,6

0,7

0,8

0,9

1,0

1,1

1,2

y= 0,296x + 0,6152

        R

2

 = 0,9332


oleObject4.bin

image6.emf
15BG-SA


Log Time (h)





-0,5


0,0


0,5


1,0


1,5


2,0


Log Cumulative Drug Release (%)


0,2


0,4


0,6


0,8


1,0


1,2


y= 0,3098x + 0,5448


        R


2


 = 0,9263




15BG-SA

Log Time (h)



-0,5 0,0 0,5 1,0 1,5 2,0

Log Cumulative Drug Release (%) 0,2

0,4

0,6

0,8

1,0

1,2

y= 0,3098x + 0,5448

        R

2

 = 0,9263


oleObject5.bin

image7.emf
30BG-SA


Log Time (h)





-0,5


0,0


0,5


1,0


1,5


2,0


Log Cumulative Drug Release (%)


0,2


0,4


0,6


0,8


1,0


1,2


y= 0,2859x + 0,5749


        R


2


 = 0,9342




30BG-SA

Log Time (h)



-0,5 0,0 0,5 1,0 1,5 2,0

Log Cumulative Drug Release (%)

0,2

0,4

0,6

0,8

1,0

1,2

y= 0,2859x + 0,5749

        R

2

 = 0,9342


oleObject6.bin

image8.emf
60BG-SA


Log Time (h)





-0,5


0,0


0,5


1,0


1,5


2,0


Log Cumulative Drug Release (%)


0,3


0,4


0,5


0,6


0,7


0,8


0,9


1,0


1,1


y= 0,2841x + 0,5794


        R


2


 = 0,9291




60BG-SA

Log Time (h)



-0,5 0,0 0,5 1,0 1,5 2,0

Log Cumulative Drug Release (%)

0,3

0,4

0,5

0,6

0,7

0,8

0,9

1,0

1,1

y= 0,2841x + 0,5794

        R

2

 = 0,9291


oleObject7.bin

image9.emf
0BG-SA


Log Time (h)


1,8


2,0


2,2


2,4


2,6


2,8


Log Cumulative Drug Release (%)


1,10


1,15


1,20


1,25


1,30


1,35


1,40


y= 0,29x + 0,6234


R


2  


= 0,9882




0BG-SA

Log Time (h)

1,8 2,0 2,2 2,4 2,6 2,8

Log Cumulative Drug Release (%) 1,10

1,15

1,20

1,25

1,30

1,35

1,40

y= 0,29x + 0,6234

R

2  

= 0,9882


oleObject8.bin

image10.emf
5BG-SA


Log Time (h)


1,8


2,0


2,2


2,4


2,6


2,8


Log Cumulative Drug Release (%)


1,15


1,20


1,25


1,30


1,35


1,40


1,45


y= 0,3411x + 0,5321


R


2  


= 0,9907




5BG-SA

Log Time (h)

1,8 2,0 2,2 2,4 2,6 2,8

Log Cumulative Drug Release (%)

1,15

1,20

1,25

1,30

1,35

1,40

1,45

y= 0,3411x + 0,5321

R

2  

= 0,9907


oleObject9.bin

image11.emf
10BG-SA


Log Time (h)


1,8


2,0


2,2


2,4


2,6


2,8


Log Cumulative Drug Release (%)


1,15


1,20


1,25


1,30


1,35


1,40


1,45


y= 0,3093x + 0,5924


R


2  


= 0,9887




10BG-SA

Log Time (h)

1,8 2,0 2,2 2,4 2,6 2,8

Log Cumulative Drug Release (%)

1,15

1,20

1,25

1,30

1,35

1,40

1,45

y= 0,3093x + 0,5924

R

2  

= 0,9887


oleObject10.bin

image12.emf
15BG-SA


Log Time (h)


1,8


2,0


2,2


2,4


2,6


2,8


Log Cumulative Drug Release (%)


1,10


1,15


1,20


1,25


1,30


1,35


1,40


y= 0,3397x + 0,4878


R


2  


= 0,9856




15BG-SA

Log Time (h)

1,8 2,0 2,2 2,4 2,6 2,8

Log Cumulative Drug Release (%)

1,10

1,15

1,20

1,25

1,30

1,35

1,40

y= 0,3397x + 0,4878

R

2  

= 0,9856


oleObject11.bin

image13.emf
30BG-SA


Log Time (h)


1,8


2,0


2,2


2,4


2,6


2,8


Log Cumulative Drug Release (%)


1,10


1,15


1,20


1,25


1,30


1,35


1,40


y= 0,2974x + 0,5829


R


2  


= 0,9886




30BG-SA

Log Time (h)

1,8 2,0 2,2 2,4 2,6 2,8

Log Cumulative Drug Release (%)1,10

1,15

1,20

1,25

1,30

1,35

1,40

y= 0,2974x + 0,5829

R

2  

= 0,9886


oleObject12.bin

image14.emf
60BG-SA


Log Time (h)


1,8


2,0


2,2


2,4


2,6


2,8


Log Cumulative Drug Release (%)


1,10


1,15


1,20


1,25


1,30


1,35


y= 0,2563x + 0,6476


R


2  


= 0,9686




60BG-SA

Log Time (h)

1,8 2,0 2,2 2,4 2,6 2,8

Log Cumulative Drug Release (%)1,10

1,15

1,20

1,25

1,30

1,35

y= 0,2563x + 0,6476

R

2  

= 0,9686


oleObject13.bin

image1.emf
     


image2.emf
272 nm


Wavelength (nm)


200


220


240


260


280


300


320


340


Absorbance


0


1


2


3


4


AMOX solution in DI water 


(1 mg/ml)




272 nm

Wavelength (nm)

200 220 240 260 280 300 320 340

Absorbance

0

1

2

3

4

AMOX solution in DI water 

(1 mg/ml)


oleObject1.bin

image3.emf
0BG-SA


Log Time (h)





-0,5


0,0


0,5


1,0


1,5


2,0


Log Cumulative Drug Release (%)


0,4


0,5


0,6


0,7


0,8


0,9


1,0


1,1


1,2


y= 0,2858x + 0,6204


R


2


 = 0,9345




0BG-SA

Log Time (h)



-0,5 0,0 0,5 1,0 1,5 2,0

Log Cumulative Drug Release (%)

0,4

0,5

0,6

0,7

0,8

0,9

1,0

1,1

1,2

y= 0,2858x + 0,6204

R

2

 = 0,9345


oleObject2.bin

image4.emf
5BG-SA


Log Time (h)





-0,5


0,0


0,5


1,0


1,5


2,0


Log Cumulative Drug Release (%)


0,4


0,5


0,6


0,7


0,8


0,9


1,0


1,1


1,2


y= 0,2978x + 0,6113 


        R


2


 = 0,9266




5BG-SA

Log Time (h)



-0,5 0,0 0,5 1,0 1,5 2,0

Log Cumulative Drug Release (%)

0,4

0,5

0,6

0,7

0,8

0,9

1,0

1,1

1,2

y= 0,2978x + 0,6113 

        R

2

 = 0,9266


