Supplementary Materials

Fabrication of a Low-Adhesion Metallic Cell Culture Surface by Nanosecond Laser Processing

Kaisei Ito1, Atsushi Ezura2, Hideharu Shimozawa3, Yoshikatsu Akiyama4, Chikahiro Imashiro5, Jun Komotori6

Correspondence should be addressed to Chikahiro Imashiro, Jun Komotori

E-mail:imashiro@pe.t.u-tokyo.ac.jp, komotori@mech.keio.ac.jp

- School of Science for Open and Environmental Systems, Graduate School of Science and Technology, Keio University, Kanagawa 223-0061, Japan.

- Sanjo City University, 5002-5 Kamisugoro, Sanjo-shi, Niigata 955-0091, Japan.

- Medical Systems and Components Operations, Canon Inc., 3-30-2 Shimomaruko, Ota-ku, Tokyo 146-8501, Japan.

- Institute of Advanced Biomedical Engineering and Science, Tokyo Women's Medical University (TWIns), 8-1 Kawada-cho, Shinjuku-ku, Tokyo 162-8886, Japan.

- Graduate School of Engineering, The University of Tokyo, Hongo 7-3-1, Bunkyo-ku, Tokyo 113-8654, Japan.

- Department of Mechanical Engineering, Keio University, Yokohama, Kanagawa 223-0061, Japan.

Supplementary Table.1. Laser processing parameters for surface microstructure fabrication

| Series name | A (L-series) | B | C | D | E |
| --- | --- | --- | --- | --- | --- |
| Output [W] | 13.7 | 13.7 | 13.7 | 13.7 | 13.7 |
| Repetition rate [kHz] | 100 | 100 | 100 | 100 | 100 |
| Pulse width [ns] | 200 | 200 | 200 | 200 | 200 |
| Scanning speed [m/s] | 2 | 2 | 2 | 1.5 | 1 |
| Shot pitch [µm] | 20 | 20 | 20 | 15 | 10 |
| Hatching pitch [µm] | 15 | 20 | 10 | 15 | 10 |

Supplementary Fig.1. 3D surface profiles of laser-processed surfaces under various irradiation conditions. (a) Shot pitch: 20 µm, hatching pitch: 15 µm (L-series), (b) Shot pitch: 20 µm, hatching pitch: 20 µm, (c) Shot pitch: 20 µm, hatching pitch: 10 µm, (d) Shot pitch: 15 µm, hatching pitch: 15 µm, (e) Shot pitch: 10 µm, hatching pitch: 10 µm.

Supplementary Fig. 2. PDMS ring: configuration and dimensions (dimensions in mm)

Supplementary Fig. 3. Binarized fluorescence images of jet-induced cell detachment with best-fit circle overlays. (a) P-series; (b) L-series.

Supplementary Note.1.

The wall shear stress τr was computed following Phares et al. (2000) for an axisymmetric normally impinging jet using the dimensionless profile g2r/H:

τr=ρu02Re0-1/2HD-2g2rH .

where ρ, ν, Q, D, H, u0 and Re0, and are the fluid density ρ=993 kg/m3 PBS and viscosity ν=0.90×10-6 m2/s, volumetric flow rate Q=1.72 mL/s, nozzle diameter D=7.0 mm, nozzle–plate distance H=17 mm, nozzle-exit velocity u0=4Q/πD2≈4.47 m/s, Reynolds number Re0=u0D/ν≈3.48×103 (Phares et al. 2000. https://doi.org/10.1017/S002211200000121X). The function g2r/H as obtained from the universal curve reported by Phares et al. via numerical reading with spline interpolation.

Because ρ, ν, Q, D, and H were held constant, τ is effectively set by the detachment radius r through g2(r/H); in the inner impingement region, τ increases approximately linearly with r. Accordingly, the shear stresses required for detachment on two surfaces can be compared from their detachment radii:

τLτP=rPrL=1.26 mm2.03 mm≈0.621

which indicates that the minimum shear required to detach cells on the L-series was about 62% of that on the P-series, as determined from the detachment radii in Fig. 5c. In other words, the cell adhesion strength on the L-series was probably suppressed to approximately 62% of the P-series value.