Comparing the efficiency of living and non-living macroalgae biomass in removing classical and emergent contaminants from complex multi-element mixtures

Supplementary Material Section

In this section, Figure S1 and Tables S1, S2, S3 and S4 are presented, which support and complement the information presented in the article.

Figure S1 – Fittings of pseudo-first order (in blue), pseudo-second order (in green) and Elovich (in red) models to experimental data on Y, Dy, Pb and Hg uptake by living and non-living macroalgal biomass.

Table S1, 2,3 and 4 – Parameters of the fittings of pseudo-first order, pseudo-second-order and Elovich models to experimental data on Y, Dy, Pb and Hg uptake by living and non-living macroalgal biomass.

Figure S1 – Fittings of pseudo-first order (in blue), pseudo-second order (in green) and Elovich (in red) models to experimental data on Y, Dy, Pb and Hg uptake by living and non-living macroalgal biomass.

Table S1– Parameters of the fittings of pseudo-first order, pseudo-second order and Elovich models to experimental data on Y, Dy, Pb and Hg, respectively, uptake by living biomass of Ulva lactuca.

|  | Living biomass – Ulva lactuca |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Y | La | Nd | Eu | Gd | Dy | Pb | Hg |
| Pseudo-first order | qe ±SD (µg g-1) | 51.43 | 107.7 | 116.2 | 126.5 | 126.5 | 134.7 | 141.8 | 211.3 |
|  | k1±SD (h-1) | 0.1590 | 0.1116 | 0.1018 | 0.09534 | 0.1094 | 0.1193 | 0.1677 | 0.1040 |
|  | R2 | 0.9475 | 0.9626 | 0.9699 | 0.9697 | 0.9742 | 0.9709 | 0.8905 | 0.9919 |
|  | Sy.x | 4.533 | 8.233 | 7.900 | 8.644 | 7.993 | 9.045 | 18.38 | 9.185 |
| Pseudo-second order | qe ±SD (µg g-1) | 57.37 | 124.4 | 135.1 | 148.2 | 146.0 | 145.2 | 158.7 | 245.0 |
|  | k2±SD (h-1) | 0.0036 | 0.001039 | 0.0008622 | 0.0007202 | 0.0008697 | 0.0009205 | 0.001351 | 0.0004359 |
|  | R2 | 0.9723 | 0.9737 | 0.9734 | 0.9719 | 0.9784 | 0.9807 | 0.9295 | 0.9950 |
|  | Sy.x | 3.291 | 6.911 | 7.426 | 8.335 | 7.325 | 7.371 | 14.75 | 7.249 |
| Elovich | β ±SD (g µg-1) | 0.09141 | 0.03677 | 0.03338 | 0.02968 | 0.03133 | 0.03042 | 0.03329 | 0.01723 |
|  | α ±SD (µg g-1 h-1) | 27.38 | 28.09 | 27.01 | 26.09 | 32.40 | 39.81 | 80.61 | 36.64 |
|  | R2 | 0.9759 | 0.9700 | 0.9666 | 0.9650 | 0.9695 | 0.9742 | 0.9493 | 0.9924 |
|  | Sy.x | 3.072 | 7.377 | 8.315 | 9.297 | 8.700 | 8.524 | 12.50 | 8.872 |

Table S2– Parameters of the fittings of pseudo-first order, pseudo-second order and Elovich models to experimental data on Y, Dy, Pb and Hg, respectively, uptake by living biomass of Gracilaria gracilis.

|  | Living biomass – Gracilaria gracilis |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Y | La | Nd | Eu | Gd | Dy | Pb | Hg |
| Pseudo-first order | qe ±SD (µg g-1) | 79.14 | 184.9 | 193.4 | 216.2 | 204.3 | 216.7 | 249.6 | 332.5 |
|  | k1±SD (h-1) | 0.1146 | 0.06372 | 0.04382 | 0.04501 | 0.05328 | 0.06118 | 0.1919 | 0.2138 |
|  | R2 | 0.9353 | 0.8734 | 0.8771 | 0.8355 | 0.8825 | 0.9061 | 0.9636 | 0.7959 |
|  | Sy.x | 7.839 | 26.89 | 27.32 | 35.70 | 28.10 | 26.42 | 18.04 | 82.23 |
| Pseudo-second order | qe ±SD (µg g-1) | 90.54 | 231.4 | 263.7 | 291.1 | 264.6 | 272.6 | 272.4 | 381.7 |
|  | k2±SD (h-1) | 0.001520 | 0.0002651 | 0.0001350 | 0.0001291 | 0.0001811 | 0.0002148 | 0.001002 | 0.0005684 |
|  | R2 | 0.9468 | 0.8714 | 0.8718 | 0.8320 | 0.8795 | 0.9054 | 0.9800 | 0.8018 |
|  | Sy.x | 7.113 | 27.11 | 27.90 | 36.08 | 28.46 | 26.52 | 13.37 | 81.04 |
| Elovich | β ±SD (g µg-1) | 0.05290 | 0.01629 | 0.01201 | 0.01117 | 0.01327 | 0.01368 | 0.02099 | 0.01244 |
|  | α ±SD (µg g-1 h-1) | 24.15 | 19.10 | 10.66 | 12.75 | 15.86 | 21.26 | 213.9 | 133.6 |
|  | R2 | 0.9472 | 0.8661 | 0.8653 | 0.8270 | 0.8744 | 0.9013 | 0.9670 | 0.7881 |
|  | Sy.x | 7.083 | 27.66 | 28.61 | 36.61 | 29.05 | 27.09 | 17.18 | 83.79 |

Table S3 – Parameters of the fittings of pseudo-first order, pseudo-second order and Elovich models to experimental data on Y, Dy, Pb and Hg, respectively, uptake by non-living and non-living biomass of Ulva lactuca.

|  | Non-living biomass – Ulva lactuca |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Y | La | Nd | Eu | Gd | Dy | Pb | Hg |
| Pseudo-first order | qe ±SD (µg g-1) | 40.57 | 36.16 | 27.53 | 29.37 | 41.00 | 40.98 | 85.32 | 229.6 |
|  | k1±SD (h-1) | 0.5502 | 0.2779 | 0.1726 | 0.1311 | 0.1698 | 0.2004 | 2.255 | 1.384 |
|  | R2 | 0.9667 | 0.8387 | 0.6457 | 0.6175 | 0.7328 | 0.7588 | 0.8936 | 0.8902 |
|  | Sy.x | 2.806 | 6.551 | 10.46 | 12.11 | 12.20 | 10.88 | 10.31 | 30.15 |
| Pseudo-second order | qe ±SD (µg g-1) | 42.51 | 39.07 | 31.68 | 34.94 | 47.02 | 46.09 | 85.99 | 236.8 |
|  | k2±SD (h-1) | 0.02258 | 0.009865 | 0.005498 | 0.003478 | 0.003747 | 0.004875 | 0.1155 | 0.01037 |
|  | R2 | 0.9228 | 0.7766 | 0.6065 | 0.5860 | 0.6895 | 0.7097 | 0.8908 | 0.8999 |
|  | Sy.x | 4.269 | 7.710 | 11.04 | 12.60 | 13.15 | 11.93 | 10.44 | 28.80 |
| Elovich | β ±SD (g µg-1) | 0.2415 | 0.1597 | 0.1336 | 0.1094 | 0.09217 | 0.09958 | 1.850 | 0.06100 |
|  | α ±SD (µg g-1 h-1) | 2206 | 52.26 | 6.932 | 4.791 | 11.06 | 15.68 | 1,664e+066 | - |
|  | R2 | 0.8218 | 0.6781 | 0.5478 | 0.5446 | 0.6260 | 0.6466 | - | 0.9015 |
|  | Sy.x | 6.488 | 9.256 | 11.82 | 13.21 | 14.43 | 13.30 | - | 28.55 |

Table S3 – Parameters of the fittings of pseudo-first order, pseudo-second order and Elovich models to experimental data on Y, Dy, Pb and Hg, respectively, uptake by non-living and non-living biomass of Gracilaria gracilis.

|  | Non-living biomass – Gracilaria gracilis |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Y | La | Nd | Eu | Gd | Dy | Pb | Hg |
| Pseudo-first order | qe ±SD (µg g-1) | 37.72 | 35.24 | 23.33 | 25.79 | 42.96 | 41.96 | 218.2 | 329.1 |
|  | k1±SD (h-1) | 0.6416 | 0.5662 | 0.4721 | 0.4263 | 0.3488 | 0.4022 | 0.5659 | 0.2867 |
|  | R2 | 0.6870 | 0.4455 | 0.2657 | 0.2188 | 0.3962 | 0.7764 | 0.9486 | 0.8601 |
|  | Sy.x | 12.74 | 15.45 | 17.90 | 20.36 | 22.28 | 9.441 | 18.60 | 53.61 |
| Pseudo-second order | qe ±SD (µg g-1) | 39.69 | 37.14 | 24.19 | 27.90 | 46.66 | 44.83 | 232.0 | - |
|  | k2±SD (h-1) | 0.02719 | 0.02457 | 0.03078 | 0.02052 | 0.009987 | 0.01230 | 0.003912 | - |
|  | R2 | 0.6536 | 0.4067 | 0.2049 | 0.2035 | 0.3720 | 0.7483 | 0.9446 | 0.8018 |
|  | Sy.x | 10.04 | 15.98 | 18.58 | 20.56 | 22.72 | 10.02 | 19.32 | 63.81 |
| Elovich | β ±SD (g µg-1) | 0.2754 | 0.2684 | 0.3937 | 0.2490 | 0.1362 | 0.1535 | 0.04000 | 0.01921 |
|  | α ±SD (µg g-1 h-1) | 3849 | 1410 | 441.8 | 80.12 | 77.52 | 114.5 | 5603 | 804.1 |
|  | R2 | 0.5833 | 0.3421 | 0.1347 | 0.1726 | 0.3218 | 0.6788 | 0.8858 | 0.8018 |
|  | Sy.x | 11.01 | 16.83 | 19.43 | 20.96 | 23.62 | 11.32 | 27.74 | 63.81 |