Supplementary Tables for

Estimating the permeability-depth relation of slate formation for 
geothermal project

Tables

Table S1 Determination of average JRC values for vertical and horizontal profiles oriented parallel (i.e., profile AA) and perpendicular (i.e., profile BB) to the flow direction, respectively

Table S2 Parameters of the stress-dependent permeability of intact slates oriented parallel to the incipient foliation in the loading and unloading paths calculated based on a power law

Table S3 Parameters of stress-dependent hydraulic aperture for fractured samples in the loading and unloading paths calculated by an exponential function

Table S1 Determination of average JRC values for vertical and horizontal profiles oriented parallel (i.e., profile AA) and perpendicular (i.e., profile BB) to the flow direction, respectively

| Sample type |  | Sample number | Fracture surface |  | JRC |
| --- | --- | --- | --- | --- | --- |
| Fractured sample | Natural fracture along the foliation | NFF-01 | Surface #1 | Vertical | 0.8 |
|  |  |  |  | Horizontal | 0.6 |
|  |  |  | Surface #2 | Vertical | 0.7 |
|  |  |  |  | Horizontal | 0.6 |
|  |  | NFF-02 | Surface #1 | Vertical | 0.6 |
|  |  |  |  | Horizontal | 0.8 |
|  |  |  | Surface #2 | Vertical | 0.9 |
|  |  |  |  | Horizontal | 0.9 |
|  |  | NFF-03 | Surface #1 | Vertical | 1.0 |
|  |  |  |  | Horizontal | 1.0 |
|  |  |  | Surface #2 | Vertical | 0.9 |
|  |  |  |  | Horizontal | 0.8 |
|  | Artificial tensile fracture along the foliation | ATF-01 | Surface #1 | Vertical | 1.4 |
|  |  |  |  | Horizontal | 1.5 |
|  |  |  | Surface #2 | Vertical | 1.4 |
|  |  |  |  | Horizontal | 1.0 |
|  |  | ATF-02 | Surface #1 | Vertical | 3.1 |
|  |  |  |  | Horizontal | 2.1 |
|  |  |  | Surface #2 | Vertical | 3.1 |
|  |  |  |  | Horizontal | 2.1 |
|  |  | ATF-03 | Surface #1 | Vertical | 8.0 |
|  |  |  |  | Horizontal | 4.0 |
|  |  |  | Surface #2 | Vertical | 8.4 |
|  |  |  |  | Horizontal | 3.7 |

Table S2 Parameters of the stress-dependent permeability of intact slates oriented parallel to the incipient foliation in the loading and unloading paths calculated based on a power law

| Sample number | Loading/ Unloading | k0 (mD) | p | R2 |
| --- | --- | --- | --- | --- |
| SL1// | Loading | 0.019 | 1.162 | 0.89 |
| SL2// | Loading | 1.195 | 2.022 | 0.96 |
| SL3// | Loading | 0.027 | 0.688 | 0.80 |
|  | Unloading | 0.189 | 1.083 | 0.99 |
| SL4// | Loading | 2.066 | 1.912 | 0.90 |
|  | Unloading | 0.005 | 0.891 | 0.87 |

Table S3 Parameters of stress-dependent hydraulic aperture of fractured samples in the loading and unloading paths calculated by an exponential function

| Sample type |  | Sample number | Loading/ Unloading | ei (µm) | er (µm) | αe | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Fractured sample | Natural fracture along the foliation | NFF-01 | Loading | 7.4 | 1.3 | 0.050 | 0.99 |
|  |  |  | Unloading | 5.2 | 1.7 | 0.120 | 0.99 |
|  |  | NFF-02 | Loading | 5.8 | 1.2 | 0.084 | 0.98 |
|  |  |  | Unloading | 3.3 | 1.1 | 0.125 | 0.97 |
|  |  | NFF-03 | Loading | 6.4 | 5.1 | 0.049 | 0.95 |
|  |  |  | Unloading | 6.4 | 5.0 | 0.073 | 0.94 |
|  | Artificial tensile fracture along the foliation | ATF-01 | Loading | 5.5 | 1.8 | 0.064 | 0.99 |
|  |  |  | Unloading | 4.2 | 1.8 | 0.136 | 0.99 |
|  |  | ATF-02 | Loading | 7.6 | 0.8 | 0.032 | 0.99 |
|  |  |  | Unloading | 6.4 | 2.0 | 0.103 | 0.99 |
|  |  | ATF-03 | Loading | 8.5 | 1.1 | 0.049 | 0.99 |
|  |  |  | Unloading | 5.9 | 1.5 | 0.156 | 0.99 |