Electronic Supplementary Material

# Microneedles-based nanoporous gold electrochemical sensor for real time catecholamine detection

# Cristina Tortolinia, Anthony E.G. Cassb, Riccardo Pofic, Andrea Lenzic, Riccarda Antiochiaa,*

aDepartment of Chemistry and Drug Technologies, Sapienza University of Rome, P.le Aldo Moro 5, 00185, Rome, Italy

bDepartment of Chemistry & Institute of Biomedical Engineering, Imperial College, London, UK

aDepartment of Experimental Medicine, Sapienza University of Rome, Rome, Italy

* Corresponding author.

E-mail address: riccarda.antiochia@uniroma1.it

(A)

(B)

Spectrum: Microneedles_ 1

Element   Series  unn. C norm. C Atom. C Error (1 Sigma)

[wt.%]  [wt.%]  [at.%]          [wt.%]

--------------------------------------------------------

Gold     M-series  86.98   91.24   40.08            3.45

Carbon   K-series   6.23    6.53   47.05            1.16

Oxygen   K-series   1.12    1.17    6.34            0.33

Nitrogen K-series   1.01    1.06    6.53            0.38

--------------------------------------------------------

Total:  95.33  100.00  100.00

Fig. S1 EDX spectra of h-nPG microneedles electrode (panel A) and chemical composition (%) of h-nPG microneedles electrode (panel B) obtained from EDX analysis.

(A)

(B)

Fig. S2 CV of 0.1 mM DA with h-nPG Au classical electrode at 25 mV s-1 (panel A); Possible EP and NEP oxidative pathways (panel B).

(A)

(B)

Fig. S3 CVs of 0.1 mM EP (A) and NEP (B) with microneedles h-nPG electrode at different scan rates (5-50 mV s-1), in 0.1 M PBS, 0.1 M KCl (pH 7.4).  In the insets, the plot of the peak current density vs. scan rate and/or square root of scan rate (5÷300 mV s-1).

Fig. S4 Plots of peak potential Ep vs log of h-nPG microneedles electrode in PBS buffer, containing 1.0 mM of DA (○), EP (▼) and NEP (●).

Fig. S5 Log Ip vs. log v plots of the three catecholamines: DA (□), EP (●) and NEP (○), respectively.

(A)

(B)

(C)

Fig. S6 Stability measurements over a period of 30 days in presence of 10 μM of DA (A), EP (B) and NEP (C) in 0.1 M PBS, 0.1 M KCl (pH 7.4), (n=10).

Table S1. Linear regression equations of Jpa versus  and 1/2 for DA, EP and NEP.

| Catecholamine | Linear regression equation |  |
| --- | --- | --- |
|  | 5-100 mV s-1 | 150-300 mV s-1 |
| DA | Jpa/mA cm-2 = 0.04 /mVs-1 + 1.9, R = 0.999 |  |
| EP | Jpa/ mA cm-2 = 0.04 mVs-1 + 0.7, R = 0.992 | Jpa/mA cm-2 = 1.2 1/2/(mVs-1)1/2 – 7.8, R = 0.999 |
| NEP | Jpa/mA cm-2 = 0.02 /mVs-1 + 0.8, R = 0.994 | Jpa/mA cm-2 = 0.6 1/2/(mVs-1)1/2 – 3.8, R = 0.998 |