Supporting Information for:

Multi-walled carbon nanotubes/carbon black/rPLA for high-performance conductive additive manufacturing filament and the simultaneous detection of acetaminophen and phenylephrine

Robert D. Crapnell,1 Iana V.S. Arantes,1,2 Jéssica R. Camargo,1,3 Elena Bernalte,1 Matthew J. Whittingham,1 Bruno C. Janegitz,3 Thiago R.L.C. Paixão,2 and Craig E. Banks1*

1Faculty of Science and Engineering, Manchester Metropolitan University, Chester Street,

M1 5GD, United Kingdom.

2Departmento de Química Fundamental, Instituto de Química, Universidade de São Paulo, São Paulo, SP, 05508-000, Brazil.

3Laboratory of Sensors, Nanomedicine and Nanostructured Materials, Federal University of São Carlos, Araras, 13600-970, Brazil.

*To whom correspondence should be addressed.

E-mail: c.banks@mmu.ac.uk; Tel: +44(0)1612471196

Figure S1. (A) Castor oil and (B) PLA structures. Reproduced with permission from ref [27]. Copyright Royal Society of Chemistry 2023.

Figure S2. XPS wide angle spectra for (A) carbon black powder and (B) MWCNT powder, and XPS C 1s spectra for (A) carbon black powder and (B) MWCNT powder.

Figure S3. EIS Bode plots of [Fe(CN)6]4-/3- (1 mM in 0.1 M KCl) comparing the (A) MWCNT/CB electrode with the (B) commercial CB/PLA.

Figure S1. A) Differential pulse voltammograms of a fixed concentration of phenylephrine (5 mM) and different concentrations of acetaminophen (5 to 200 mM) in 0.01 M PBS pH 7.4 recorded at MWCNT additively manufactured electrode using commercial additively manufactured electrode as reference and counter electrodes and B) the respective calibration plot. C) Differential pulse voltammograms of a fixed concentration of acetaminophen (5 mM) and different concentrations of phenylephrine (5 to 80 mM) in 0.01 M PBS pH 7.4 recorded at MWCNT additively manufactured electrode using commercial additively manufactured electrode as reference and counter electrodes and D) the respective calibration plot. Step potential: 8 mV. Amplitude: 50 mV.

Table S1. Resistance measurements and printability evaluation of the filaments made from different ratios of MWCNT:CB.

| MWCNT:CB ratio | Resistance across 10 cm (Ω) | Printability |
| --- | --- | --- |
| 0:100 | 864 ± 54 | Very good |
| 20:80 | 315 ± 33 | Very good |
| 40:60 | 243 ± 24 | Good |
| 60:40 | 174 ± 93 | Poor |
| 80:20 | 200 ± 55 | Poor |
| 100:0 | 131 ± 87 | Very poor |

Table S2. XPS atomic concentration data from the activated and non-activated CB/MWCNT electrodes.

| Group Assignment | Non-activated Electrode %At Concentation | Activated Electrode %At Concentation |
| --- | --- | --- |
| Graphitic | 23.48 | 29.93 |
| C-C/C-H | 34.43 | 35.67 |
| C=O | 21.33 | 15.51 |
| O-C=O | 18.70 | 16.84 |
| π-π* | 2.06 | 2.05 |

Table S3. Summary of the fitted values from EIS obtained for electrodes printed from each filament tested (n=3).

| Element | Protopasta | CB only | MWCNT/CB |
| --- | --- | --- | --- |
| R1 (Ω) | 650 ± 14 | 222 ± 10 | 115 ± 18 |
| C (x10-6 F) | 5.8 ± 0.7 | 26 ± 5 | 23 ± 3 |
| R2 (kΩ) | 2.94 ± 0.62 | 0.47 ± 0.09 | 0.31 ± 0.06 |
| W (x10-3 Ω s-1/2) | 2.8 ± 1.0 | 2.6 ± 0.3 | 2.7 ± 0.2 |

Table S4. Summary of all calibration plots, equations, and R² for acetaminophen and phenylephrine individual and simultaneous analyses.

| Analyte | Range (mM) | Equation | R2 |
| --- | --- | --- | --- |
| ACE | 5 - 200 | I = 0.1412[Ace] – 0.3795 | 0.9990 |
| PHE | 5 - 60 | I = 0.1829 [Phe] + 1.1209 | 0.9946 |
| PHE and ACE | 5 - 60 | I = 0.1432 [Phe] + 1.121 and I = 0.0510 [Ace] + 0.9266 | 0.9946 and 0.9897 |