SM Table 1a. EPMA data for magnetite (wt%) given as means for individual samples and summary statistics for the total population (FF slag)

|  | FF21-A | FF21-B | FF21-2 | FF21-3A | FF21-3B | ALL ANALYSES |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mean | Mean | Mean | Mean | Mean | Mean | S.D. | Max. | Min. |
|  | n=23 | n=141 | n=55 | n=22 | n=27 | n=222 |  |  |  |
| SiO2 | 0.06 | 0.03 | 0.04 | 0.05 | 0.04 | 0.05 | 0.013 | 0.06 | 0.03 |
| TiO2 | 0.06 | 0.10 | 0.05 | 0.04 | 0.04 | 0.06 | 0.025 | 0.10 | 0.04 |
| Al2O3 | 1.80 | 1.32 | 1.09 | 0.93 | 0.91 | 1.21 | 0.368 | 1.80 | 0.91 |
| Cr2O3 | 0.01 | 0.01 | 0.07 | 0.06 | 0.13 | 0.06 | 0.048 | 0.13 | 0.01 |
| V2O3 | 0.00 | 0.46 | 0.00 | 0.00 | 0.00 | 0.09 | 0.207 | 0.46 | 0.00 |
| Fe2O3 | 65.18 | 65.98 | 67.11 | 65.57 | 66.23 | 66.01 | 0.733 | 67.11 | 65.18 |
| FeO | 30.05 | 29.99 | 29.86 | 29.55 | 29.70 | 29.83 | 0.207 | 30.05 | 29.55 |
| MgO | 0.29 | 0.35 | 0.35 | 0.33 | 0.43 | 0.35 | 0.049 | 0.43 | 0.29 |
| CoO | 0.54 | 0.54 | 0.56 | 0.52 | 0.55 | 0.54 | 0.015 | 0.56 | 0.52 |
| Total | 98.01 | 98.78 | 99.37 | 97.06 | 98.03 | 98.25 | 0.876 | 99.37 | 97.06 |
| Calculated formula (O=24 apfu) |  |  |  |  |  |  |  |  |  |
| Si | 0.020 | 0.011 | 0.01 | 0.017 | 0.01 | 0.014 | 0.004 | 0.02 | 0.01 |
| Ti | 0.014 | 0.030 | 0.01 | 0.009 | 0.01 | 0.015 | 0.009 | 0.03 | 0.01 |
| Sum (4+) |  |  |  |  |  |  |  |  |  |
| Al | 0.660 | 0.479 | 0.39 | 0.347 | 0.34 | 0.443 | 0.134 | 0.66 | 0.34 |
| Cr | 0.003 | 0.003 | 0.02 | 0.014 | 0.03 | 0.014 | 0.012 | 0.03 | 0.00 |
| V | 0.001 | 0.47 | 0.00 | 0.001 | 0.00 | 0.094 | 0.210 | 0.47 | 0.00 |
| Fe3+ | 15.27 | 15.35 | 15.54 | 15.58 | 15.59 | 15.47 | 0.149 | 15.59 | 15.27 |
| Sum (3+) | 15.93 | 15.83 | 15.95 | 15.95 | 15.96 | 15.92 | 0.053 | 15.96 | 15.83 |
| Fe2+ | 7.82 | 7.75 | 7.68 | 7.80 | 7.77 | 7.77 | 0.054 | 7.82 | 7.68 |
| Mg | 0.135 | 0.163 | 0.16 | 0.158 | 0.20 | 0.163 | 0.023 | 0.20 | 0.14 |
| Co | 0.136 | 0.136 | 0.14 | 0.133 | 0.14 | 0.136 | 0.003 | 0.14 | 0.13 |
| Sum (2+) | 8.09 | 8.05 | 7.98 | 8.10 | 8.11 | 8.07 | 0.051 | 8.11 | 7.98 |
| Total | 24.000 | 24.000 | 24.000 | 24.000 | 24.000 | 24.000 | 0.000 | 24.000 | 24.000 |

Note: The data in this table are mean concentrations. In some cases, these means are of datasets in which concentration values are both above and below the respective minimum detection limit values. Taking the <mdl values as zero, the resultant mean is thus less than the mdl given in the text.

SM Table 1b. EPMA data for magnetite (wt%) given as means for individual samples and summary statistics for the total population (EF slag)

|  | EF21-B | EF21-C | EF21-3A | EF21-3B | EF21-4B | EF21-5 | ALL ANALYSES |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mean | Mean | Mean | Mean | Mean | Mean | Mean | S.D. | Max. | Min. |
|  | n=20 | n=91 | n=11 | n=6 | n=73 | n=45 | n=246 |  |  |  |
| SiO2 | 0.451 | 0.431 | 0.565 | 0.589 | 0.905 | 0.341 | 0.547 | 0.197 | 0.905 | 0.341 |
| TiO2 | 0.460 | 0.443 | 0.337 | 0.340 | 0.309 | 0.234 | 0.354 | 0.085 | 0.460 | 0.234 |
| Al2O3 | 3.577 | 3.316 | 2.393 | 2.407 | 2.188 | 2.165 | 2.674 | 0.612 | 3.577 | 2.165 |
| V2O3 | 0.002 | 0.004 | 0.006 | 0.006 | 0.006 | 0.004 | 0.005 | 0.002 | 0.006 | 0.002 |
| Fe2O3 | 61.795 | 62.236 | 63.902 | 64.318 | 63.391 | 63.215 | 63.143 | 0.966 | 64.318 | 61.795 |
| FeO | 31.790 | 31.611 | 31.976 | 32.202 | 32.332 | 32.503 | 32.069 | 0.338 | 32.503 | 31.611 |
| MgO | 0.036 | 0.043 | 0.037 | 0.038 | 0.043 | 0.991 | 0.198 | 0.388 | 0.991 | 0.036 |
| CoO | 0.288 | 0.308 | 0.392 | 0.405 | 0.406 | 0.448 | 0.375 | 0.063 | 0.448 | 0.288 |
| Total | 98.399 | 98.392 | 99.609 | 100.305 | 99.580 | 96.997 | 98.880 | 1.189 | 100.305 | 96.997 |
| Calculated formula (O=24 apfu) |  |  |  |  |  |  |  |  |  |  |
| Si | 0.138 | 0.132 | 0.172 | 0.178 | 0.273 | 0.104 | 0.166 | 0.059 | 0.273 | 0.104 |
| Ti | 0.106 | 0.102 | 0.077 | 0.077 | 0.071 | 0.053 | 0.081 | 0.020 | 0.106 | 0.053 |
| Sum (4+) | 0.244 | 0.226 | 0.249 | 0.255 | 0.339 | 0.157 | 0.245 | 0.059 | 0.339 | 0.157 |
| Al | 1.289 | 1.200 | 0.858 | 0.858 | 0.786 | 0.775 | 0.961 | 0.224 | 1.289 | 0.775 |
| V | 0.000 | 0.001 | 0.001 | 0.002 | 0.001 | 0.001 | 0.001 | 0.000 | 0.002 | 0.000 |
| Fe3+ | 14.215 | 14.349 | 14.637 | 14.630 | 14.517 | 14.894 | 14.540 | 0.239 | 14.894 | 14.215 |
| Sum (3+) | 15.504 | 15.038 | 15.497 | 15.489 | 15.095 | 15.670 | 15.382 | 0.254 | 15.670 | 15.038 |
| Fe2+ | 8.127 | 8.100 | 8.140 | 8.140 | 8.225 | 8.012 | 8.124 | 0.069 | 8.225 | 8.012 |
| Mg | 0.017 | 0.020 | 0.017 | 0.017 | 0.020 | 0.032 | 0.020 | 0.006 | 0.032 | 0.017 |
| Co | 0.071 | 0.076 | 0.096 | 0.098 | 0.099 | 0.113 | 0.092 | 0.016 | 0.113 | 0.071 |
| Sum (2+) | 8.214 | 7.925 | 8.252 | 8.255 | 8.229 | 8.156 | 8.172 | 0.126 | 8.255 | 7.925 |
| Total | 24.000 | 24.000 | 24.000 | 24.000 | 24.000 | 24.000 | 24.000 | 0.000 | 24.000 | 24.000 |

Note: The data in this table are mean concentrations. In some cases, these means are of datasets in which concentration values are both above and below the respective minimum detection limit values. Taking the <mdl values as zero, the resultant mean is thus less than the mdl given in the text.

SM Table 1c. EPMA data for fayalite (wt%) given as means for individual samples and summary statistics for the total population (EF slag)

|  | EF21-3B | EF21-3A | EF21-B | FF21-4B | EF21-5 | EF21-C |  | ALL ANALYSES |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Mean | Mean | Mean | Mean | Mean | Mean |  | Mean | S.D. | Max. | Min. |
|  | n=6 | n=11 | n=116 | n=67 | n=2 | n=33 |  | n=235 |  |  |  |
| SiO2 | 28.481 | 28.456 | 28.891 | 28.932 | 28.621 | 28.719 | SiO2 | 28.684 | 0.201 | 28.932 | 28.456 |
| TiO2 | 0.000 | 0.003 | 0.002 | 0.001 | 0.000 | 0.003 | TiO2 | 0.001 | 0.001 | 0.003 | 0.000 |
| Al2O3 | 0.044 | 0.070 | 0.230 | 0.064 | 0.045 | 0.069 | Al2O3 | 0.087 | 0.071 | 0.230 | 0.044 |
| FeO | 68.230 | 67.568 | 67.672 | 69.478 | 68.549 | 68.619 | FeO | 68.353 | 0.703 | 69.478 | 67.568 |
| MnO | 0.007 | 0.008 | 0.003 | 0.004 | 0.000 | 0.008 | MnO | 0.005 | 0.003 | 0.008 | 0.000 |
| MgO | 0.419 | 0.465 | 0.347 | 0.409 | 0.378 | 0.456 | MgO | 0.412 | 0.045 | 0.465 | 0.347 |
| NiO | 0.000 | 0.000 | 0.001 | 0.003 | 0.000 | 0.000 | NiO | 0.001 | 0.001 | 0.003 | 0.000 |
| CaO | 0.116 | 0.126 | 0.174 | 0.096 | 0.144 | 0.133 | CaO | 0.132 | 0.027 | 0.174 | 0.096 |
| P2O5 | 0.161 | 0.198 | 0.215 | 0.154 | 0.054 | 0.198 | P2O5 | 0.163 | 0.058 | 0.215 | 0.054 |
| CoO | 0.483 | 0.475 | 0.440 | 0.578 | 0.491 | 0.491 | CoO | 0.493 | 0.046 | 0.578 | 0.440 |
| V2O3 | 0.000 | 0.003 | 0.005 | 0.004 | 0.000 | 0.005 | V2O3 | 0.003 | 0.002 | 0.005 | 0.000 |
| Cu2O | 0.038 | 0.053 | 0.045 | 0.107 | 0.051 | 0.074 | Cu2O | 0.061 | 0.025 | 0.107 | 0.038 |
| ZnO | 0.000 | 0.005 | 0.016 | 0.023 | 0.000 | 0.017 | ZnO | 0.010 | 0.010 | 0.023 | 0.000 |
| Na2O | 0.138 | 0.031 | 0.062 | 0.039 | 0.106 | 0.069 | Na2O | 0.074 | 0.041 | 0.138 | 0.031 |
| Total | 98.117 | 97.461 | 98.103 | 99.892 | 98.439 | 98.862 | Total | 98.479 | 0.831 | 99.892 | 97.461 |
| apfu (Fe,Mg)2SiO4 |  |  |  |  |  |  | apfu (Fe,Mg)2SiO4 |  |  | apfu (Fe,Mg) 2SiO4 |  |
| Si | 0.993 | 0.998 | 1.002 | 0.991 | 0.987 | 0.994 | Si | 0.994 | 0.005 | Si | 0.993 |
| Ti | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | Ti | 0.000 | 0.000 | Ti | 0.000 |
| P | 0.005 | 0.005 | 0.006 | 0.004 | 0.006 | 0.006 | P | 0.005 | 0.001 | P | 0.005 |
| Σ (4+, 5+) | 0.998 | 1.003 | 1.000 | 0.966 | 0.992 | 1.000 | Σ (4+, 5+) | 0.993 | 0.014 | Σ (4+, 5+) | 0.998 |
| Al | 0.002 | 0.003 | 0.009 | 0.003 | 0.002 | 0.003 | Al | 0.004 | 0.003 | Al | 0.002 |
| V | 0.000 | 0.000 | 0.000 | 0.000 | 0.001 | 0.000 | V | 0.000 | 0.000 | V | 0.000 |
| Σ (3+) | 0.002 | 0.003 | 0.010 | 0.003 | 0.003 | 0.004 | Σ (3+) | 0.004 | 0.003 | Σ (3+) | 0.002 |
| Fe | 1.989 | 1.976 | 1.963 | 1.992 | 1.994 | 1.983 | Fe | 1.983 | 0.012 | Fe | 1.989 |
| Mn | 0.000 | 0.000 | 0.000 | 0.000 | 0.001 | 0.000 | Mn | 0.000 | 0.000 | Mn | 0.000 |
| Mg | 0.022 | 0.025 | 0.018 | 0.021 | 0.028 | 0.024 | Mg | 0.023 | 0.003 | Mg | 0.022 |
| Ca | 0.004 | 0.005 | 0.006 | 0.003 | 0.005 | 0.005 | Ca | 0.005 | 0.001 | Ca | 0.004 |
| Co | 0.014 | 0.013 | 0.012 | 0.016 | 0.015 | 0.014 | Co | 0.014 | 0.001 | Co | 0.014 |
| Zn | 0.000 | 0.000 | 0.000 | 0.001 | 0.000 | 0.000 | Zn | 0.000 | 0.000 | Zn | 0.000 |
| Σ (2+) | 2.029 | 2.019 | 1.983 | 1.972 | 2.042 | 2.027 | Σ (2+) | 2.012 | 0.028 | Σ (2+) | 2.029 |
| Cu | 0.001 | 0.002 | 0.001 | 0.003 | 0.002 | 0.002 | Cu | 0.002 | 0.001 | Cu | 0.001 |
| Na | 0.009 | 0.002 | 0.004 | 0.003 | 0.005 | 0.004 | Na | 0.005 | 0.003 | Na | 0.009 |
| Σ (1+) | 0.010 | 0.004 | 0.006 | 0.006 | 0.007 | 0.006 | Σ (1+) | 0.006 | 0.002 | Σ (1+) | 0.010 |
| Total | 3.039 | 3.028 | 2.998 | 2.947 | 3.045 | 3.037 | Total | 3.016 | 0.038 | Total | 3.039 |

Note: The data in this table are mean concentrations. In some cases, these means are of datasets in which concentration values are both above and below the respective minimum detection limit values. Taking the <mdl values as zero, the resultant mean is thus less than the mdl given in the text.

SM Table 1d. Summary statistics for EPMA data (wt%) for Glass 1 (FF slag)

|  | Mean | Min. | Max. | S.D. |
| --- | --- | --- | --- | --- |
|  | (n=6) |  |  |  |
| SiO2 | 41.52 | 39.61 | 43.42 | 2.70 |
| Fe2O3 | 14.25 | 11.60 | 16.89 | 3.74 |
| Al2O3 | 5.02 | 4.61 | 5.43 | 0.58 |
| CaO | 8.02 | 5.03 | 11.01 | 4.23 |
| BaO | 1.83 | 1.60 | 2.06 | 0.33 |
| K2O | 0.44 | 0.42 | 0.46 | 0.03 |
| P2O5 | 4.17 | 0.80 | 7.53 | 4.76 |
| La2O3 | 2.26 | 1.71 | 2.82 | 0.78 |
| Ce2O3 | 3.14 | 2.32 | 3.96 | 1.16 |
| UO2 | 0.53 | 0.51 | 0.54 | 0.02 |
| PbO | 0.55 | 0.48 | 0.61 | 0.09 |
| ThO2 | 0.01 | 0.01 | 0.01 | 0.00 |
| TiO2 | 0.02 | 0.02 | 0.03 | 0.00 |
| Na2O | 0.18 | 0.15 | 0.22 | 0.05 |
| CoO | 0.09 | 0.08 | 0.11 | 0.02 |
| Cu2O | 12.67 | 9.88 | 15.46 | 3.95 |
| ZrO2 | 0.08 | 0.07 | 0.09 | 0.01 |
| Nb2O5 | 0.16 | 0.16 | 0.17 | 0.01 |
| V2O3 | 0.02 | 0.01 | 0.02 | 0.01 |
| MnO | 0.01 | 0.01 | 0.01 | 0.00 |
| MgO | 0.89 | 0.66 | 1.13 | 0.33 |
| ZnO | 0.08 | 0.07 | 0.08 | 0.00 |
| Cl | 0.10 | 0.09 | 0.11 | 0.01 |
| F | 0.13 | 0.10 | 0.16 | 0.05 |
| TOTAL | 96.09 | 96.07 | 96.12 | 0.04 |

Note: The data in this table are mean concentrations. In some cases, these means are of datasets in which concentration values are both above and below the respective minimum detection limit values. Taking the <mdl values as zero, the resultant mean is thus less than the mdl given in the text.

SM Table 1e. Summary statistics for EPMA data (wt%) for Glass 2 (FF slag)

|  | Mean | Min. | Max. | S.D. |
| --- | --- | --- | --- | --- |
|  | (n=43) |  |  |  |
| SiO2 | 70.43 | 65.33 | 75.80 | 4.41 |
| Fe2O3 | 7.48 | 5.56 | 9.93 | 1.63 |
| Al2O3 | 5.87 | 4.49 | 7.00 | 1.23 |
| CaO | 2.56 | 1.87 | 3.47 | 0.66 |
| BaO | 1.32 | 1.20 | 1.40 | 0.08 |
| K2O | 1.33 | 0.98 | 1.81 | 0.30 |
| P2O5 | 0.18 | 0.06 | 0.39 | 0.13 |
| La2O3 | 0.25 | 0.07 | 0.56 | 0.17 |
| Ce2O3 | 0.36 | 0.12 | 0.80 | 0.25 |
| UO2 | 0.07 | 0.00 | 0.19 | 0.08 |
| PbO | 0.32 | 0.24 | 0.43 | 0.08 |
| ThO2 | 0.00 | 0.00 | 0.00 | 0.00 |
| TiO2 | 0.03 | 0.02 | 0.06 | 0.02 |
| Na2O | 0.37 | 0.24 | 0.53 | 0.11 |
| CoO | 0.04 | 0.02 | 0.06 | 0.02 |
| Cu2O | 7.50 | 4.61 | 11.20 | 2.48 |
| ZrO2 | 0.01 | 0.00 | 0.04 | 0.01 |
| Nb2O5 | 0.01 | 0.00 | 0.03 | 0.01 |
| V2O3 | 0.01 | 0.00 | 0.03 | 0.01 |
| MnO | 0.00 | 0.00 | 0.01 | 0.00 |
| MgO | 0.18 | 0.10 | 0.26 | 0.07 |
| ZnO | 0.01 | 0.00 | 0.03 | 0.01 |
| Cl | 0.04 | 0.01 | 0.09 | 0.03 |
| F | 0.03 | 0.01 | 0.05 | 0.01 |
| TOTAL | 98.45 | 96.87 | 99.52 | 0.97 |

Note: The data in this table are mean concentrations. In some cases, these means are of datasets in which concentration values are both above and below the respective minimum detection limit values. Taking the <mdl values as zero, the resultant mean is thus less than the mdl given in the text.

SM Table 1f. Summary statistics for EPMA data (wt%) for Glass 1 (EF slag)

|  | Mean | Min. | Max. | S.D. |
| --- | --- | --- | --- | --- |
|  | (n=58) |  |  |  |
| SiO2 | 45.97 | 41.99 | 48.40 | 2.17 |
| Fe2O3 | 19.82 | 17.82 | 21.49 | 1.37 |
| Al2O3 | 10.98 | 10.11 | 11.93 | 0.65 |
| CaO | 6.30 | 4.74 | 8.74 | 1.72 |
| BaO | 3.54 | 2.61 | 4.12 | 0.43 |
| K2O | 1.81 | 0.84 | 3.01 | 0.88 |
| P2O5 | 2.20 | 1.77 | 3.01 | 0.49 |
| La2O3 | 1.79 | 1.30 | 2.45 | 0.37 |
| Ce2O3 | 2.73 | 1.75 | 3.77 | 0.69 |
| UO2 | 0.60 | 0.32 | 1.29 | 0.33 |
| PbO | 0.50 | 0.35 | 0.76 | 0.16 |
| ThO2 | 0.03 | 0.00 | 0.10 | 0.03 |
| TiO2 | 0.14 | 0.02 | 0.29 | 0.08 |
| Na2O | 0.32 | 0.17 | 0.49 | 0.13 |
| CoO | 0.07 | 0.05 | 0.11 | 0.02 |
| Cu2O | 0.15 | 0.06 | 0.36 | 0.09 |
| ZrO2 | 0.12 | 0.09 | 0.21 | 0.04 |
| Nb2O5 | 0.15 | 0.08 | 0.27 | 0.07 |
| V2O3 | 0.01 | 0.00 | 0.03 | 0.01 |
| MnO | 0.01 | 0.00 | 0.02 | 0.01 |
| MgO | 0.04 | 0.00 | 0.15 | 0.05 |
| ZnO | 0.07 | 0.01 | 0.16 | 0.05 |
| Cl | 0.03 | 0.02 | 0.09 | 0.02 |
| F | 0.06 | 0.01 | 0.13 | 0.05 |
| TOTAL | 97.45 | 96.46 | 100.27 | 1.18 |

Note: The data in this table are mean concentrations. In some cases, these means are of datasets in which concentration values are both above and below the respective minimum detection limit values. Taking the <mdl values as zero, the resultant mean is thus less than the mdl given in the text.

SM Table 1g. Summary statistics for EPMA data (wt%) for Glass 2 (EF slag)

|  | Mean | Min. | Max. | S.D. |
| --- | --- | --- | --- | --- |
|  | (n=62) |  |  |  |
| SiO2 | 69.04 | 60.61 | 73.18 | 4.60 |
| Fe2O3 | 12.61 | 10.19 | 14.93 | 1.69 |
| Al2O3 | 8.35 | 7.10 | 10.25 | 1.21 |
| CaO | 1.73 | 0.98 | 3.33 | 0.71 |
| BaO | 2.08 | 1.44 | 3.12 | 0.52 |
| K2O | 3.85 | 3.26 | 4.69 | 0.50 |
| P2O5 | 0.20 | 0.05 | 0.59 | 0.20 |
| La2O3 | 0.17 | 0.03 | 0.48 | 0.15 |
| Ce2O3 | 0.28 | 0.09 | 0.74 | 0.23 |
| UO2 | 0.03 | 0.00 | 0.13 | 0.04 |
| PbO | 0.21 | 0.10 | 0.28 | 0.05 |
| ThO2 | 0.00 | 0.00 | 0.01 | 0.00 |
| TiO2 | 0.01 | 0.01 | 0.02 | 0.01 |
| Na2O | 0.51 | 0.36 | 0.75 | 0.11 |
| CoO | 0.04 | 0.03 | 0.06 | 0.01 |
| Cu2O | 0.19 | 0.00 | 1.08 | 0.32 |
| ZrO2 | 0.01 | 0.00 | 0.02 | 0.01 |
| Nb2O5 | 0.00 | 0.00 | 0.01 | 0.01 |
| V2O3 | 0.01 | 0.00 | 0.01 | 0.00 |
| MnO | 0.00 | 0.00 | 0.01 | 0.01 |
| MgO | 0.04 | 0.00 | 0.09 | 0.03 |
| ZnO | 0.01 | 0.00 | 0.03 | 0.01 |
| Cl | 0.01 | 0.00 | 0.11 | 0.04 |
| F | 0.03 | 0.00 | 0.06 | 0.02 |
| TOTAL | 99.47 | 98.01 | 100.72 | 1.02 |

Note: The data in this table are mean concentrations. In some cases, these means are of datasets in which concentration values are both above and below the respective minimum detection limit values. Taking the <mdl values as zero, the resultant mean is thus less than the mdl given in the text.

SM Table 2. STEM-EDS analysis of monazite (n=24, wt%, normalised) and apatite

|  | Monazite |  |  |  | Apatite |
| --- | --- | --- | --- | --- | --- |
|  | Mean | S.D. | Min. | Max. |  |
| P2O5 | 28.77 | 4.20 | 22.99 | 36.30 | 42.25 |
| CaO | 1.59 | 0.60 | 0.67 | 3.82 | 57.22 |
| La2O3 | 20.9 | 1.4 | 18.2 | 22.6 | <mdl |
| Ce2O3 | 36.12 | 1.5 | 32.35 | 37.60 | 0.18 |
| Nd2O3 | 7.20 | 0.9 | 5.39 | 9.34 |  |
| Y2O3 |  |  |  |  | 0.02 |
| PbO | 1.03 | 0.41 | 0.49 | 2.09 |  |
| ThO2 | 0.99 | 0.46 | 0.45 | 2.14 |  |
| UO2 | 3.4 | 2.7 | 0.31 | 7.6 |  |
| F |  |  |  |  | 4.83 |
| Cl |  |  |  |  | 0.17 |
| Total | 100.00 | 0.01 | 99.98 | 100.02 |  |
| Formula calculation (cations only) |  |  |  |  |  |
| Ca | 0.04 | 0.13 | 0.07 | 0.03 | 5.157 |
| La | 0.33 | 0.27 | 0.31 | 0.04 | - |
| Ce | 0.59 | 0.44 | 0.53 | 0.05 | 0.006 |
| Nd | 0.10 | 0.11 | 0.10 | 0.01 |  |
| Y |  |  |  |  | 0.001 |
| Pb | 0.01 | 0.02 | 0.01 | 0.01 |  |
| Th | 0.01 | 0.02 | 0.01 | 0.00 |  |
| U | 0.00 | 0.05 | 0.03 | 0.03 |  |
| ΣREY | 1.02 | 0.82 | 0.94 | 0.08 |  |
| P | 0.97 | 0.99 | 0.97 | 0.08 |  |
| mol % end-members |  |  |  |  |  |
| % Monazite-La | 32.73 | 32.77 | 32.78 | 2.11 |  |
| % Monazite-Ce | 57.87 | 54.12 | 56.28 | 1.17 |  |
| % Monazite-Nd | 9.40 | 13.11 | 10.94 | 1.17 |  |