Supplementary Table S1 — Relative changes in the evaluated roughness parameters after acid immersion.
ZR-LS, zirconia and lithium disilicate reinforced glass-ceramic (Vita Suprinity, Vita Zahnfabrik GmbH), LDSLDS-P, polished lithium disilicate reinforced glass-ceramic (e.max CAD, Ivoclar Vivadent), LDSCAD-G glazed lithium disilicate reinforced glass-ceramic (e.max CAD, e.max Crystall/Glaze Spray, Ivoclar Vivadent), LDSCAD-PG polished and glazed lithium disilicate reinforced glass-ceramic (e.max CAD, e.max Crystall/Glaze Spray, Ivoclar Vivadent), AFM, atomic force microscope, Sa, arithmetic average roughness, Sq root mean squared roughness, Sal, autocorrelation length, Sq/Sal, normalized roughness, Sdr developed surface area ratio, Sds density of summits.

	 Param.:
	LDS-G
	LDS -P
	LDS-PG
	ZR-LS

	Sa
	0.11
	0.94
	0.88
	1.37

	Sq
	0.18
	0.95
	0.72
	1.36

	Sdr
	0.14
	2.27
	0.79
	1.38

	Sal
	0.43
	1.02
	1.07
	0.97

	Sq/Sal
	0.43
	0.93
	0.68
	1.41

	Sds
	0.33
	1.35
	0.71
	1.03




