Supplementary Table S1 — Relative changes in the evaluated roughness parameters after acid immersion.

ZR-LS, zirconia and lithium disilicate reinforced glass-ceramic (Vita Suprinity, Vita Zahnfabrik GmbH), LDS-P, polished lithium disilicate reinforced glass-ceramic (e.max CAD, Ivoclar Vivadent), LDS-G glazed lithium disilicate reinforced glass-ceramic (e.max CAD, e.max Crystall/Glaze Spray, Ivoclar Vivadent), LDS-PG polished and glazed lithium disilicate reinforced glass-ceramic (e.max CAD, e.max Crystall/Glaze Spray, Ivoclar Vivadent), AFM, atomic force microscope, Sa, arithmetic average roughness, Sq root mean squared roughness, Sal, autocorrelation length, Sq/Sal, normalized roughness, Sdr developed surface area ratio, Sds density of summits.

| Param.: | LDS-G | LDS -P | LDS-PG | ZR-LS |
| --- | --- | --- | --- | --- |
| Sa | 0.11 | 0.94 | 0.88 | 1.37 |
| Sq | 0.18 | 0.95 | 0.72 | 1.36 |
| Sdr | 0.14 | 2.27 | 0.79 | 1.38 |
| Sal | 0.43 | 1.02 | 1.07 | 0.97 |
| Sq/Sal | 0.43 | 0.93 | 0.68 | 1.41 |
| Sds | 0.33 | 1.35 | 0.71 | 1.03 |