Supporting Information

Evaluation of Durability of A201 Anion Exchange Membranes Towards Organic Solvents

Juri Harada1, Akizumi Yonezawa1, Yusuke Muto1, Ayaka Wakasugi1, Reno Fukui1, Naoki Shida1,2, Mahito Atobe1,2

1Department of Chemistry and Life Science, Yokohama National University, 79-5 Tokiwadai, Hodogaya-ku, Yokohama 240-8501, Japan

2Institute of Advanced Sciences, Yokohama National University, 79-5 Tokiwadai, Hodogaya-ku, Yokohama 240-8501, Japan

Table of contents

1.	General considerations	3

2.	Preparation of cathode electrode	3

3.	Assembly of an AEM reactor	4

4.	Water electrolysis with soaked membranes	5

5.	EIS using soaked membranes	8

6.	Electrolysis with organic solvents as catholytes	9

7.	EIS with organic solvents as catholytes	11

- General considerations

Reagents and solvents were purchased from commercial sources and used without further purification unless otherwise noted. Anion-exchange membranes (AEMs, A201) and anion ionomers (AS-4) were supplied by Tokuyama Corporation. Fuel cell catalysts TEC10E50E, Pt/Ketjenblack (Pt/C; 46.8 wt.%) were purchased from TANAKA precious metals corporation. Carbon paper used as a gas-diffusion layer (GDL, Sigracet® GDL39BB) was purchased from SGL CARBON. The DSE® anode for the oxygen evolution was supplied by De Nora Permelec. Electrolysis was performed using a diaphragm pump (Q-100-TT-P-S, Tacmina). Constant current electrolysis was performed using a multichannel potentiostat (VSP-3e; Biologic). EISere measurements were performed using an electrochemical analyzer (ALS/CH Instruments 660E, BAS). An Ag/AgCl electrode (RE-1BP, EC Frontier; RE-1B, BAS) was used as the reference electrode.

- Preparation of cathode electrode

The carbon-supported Pt catalyst, deionized water, the ionomer, and 1-propanol were mixed to obtain a catalyst dispersion. The ionomer-to-carbon ratio was 4:5. The dispersion was sprayed onto carbon paper with GDL, and it was dried for 10 min at 40 ℃. The total loading amount of Pt was 0.5 mg cm−2, and the area of the cathode electrode was 4 cm2 (1 cm × 4 cm).

- Assembly of an AEM reactor

The MEA was configured by sandwiching the A201 anion exchange membrane between the Pt/C cathode and the DSE® anode. To assemble an AEM reactor, gold-plated stainless steel end plates, carbon separators, Teflon® gaskets, and an MEA were tightened to 3.0 N·m using a torque wrench with the screws (Fig. S1).

Fig. S1 Assembly of an AEM reactor.

- Water electrolysis with soaked membranes

Fig. S2 Cell voltage and cathode potential during water electrolysis with AEM soaked in solvents: (a) nonsoaked, (b) hexane, (c) cyclohexane, (d)toluene, (e) THF, (f) 1, 2-doxane, (g) CPME, (h) MTBE.

Fig. S3 Cell voltage and cathode potential during water electrolysis with AEM soaked in solvents: (i) DME, (j) dichloromethane, (k) chloroform, (l) acetone, (m) ethyl acetate, (n) methanol, (o) ethanol, (p) isopropanol.

Fig. S4 Cell voltage and cathode potential during water electrolysis with AEM soaked in solvents: (q) tert-butanol, (r) acetonitrile, (s) DMF, (t) DMSO, (u) water.

- EIS using soaked membranes

Fig. S5 Results of EIS measurements with AEM soaked in solvents: (a) nonsoaked, (b) hexane, (c) cyclohexane, (d) toluene, (e) THF, (f) 1, 2-doxane, (g) CPME, (h) MTBE, (i) DME, (j) dichloromethane, (k) chloroform, (l) acetone, (m) ethyl acetate, (n) methanol, (o) ethanol, (p) isopropanol, (q) tert-butanol, (r) acetonitrile, (s) DMF, (t) DMSO, (u) water.

- Electrolysis with organic solvents as catholytes

Fig. S6 Cell voltage and cathode potential during electrolysis with organic solvents as catholytes: (a) hexane, (b) cyclohexane, (c) toluene, (d) THF, (e) 1, 2-doxane, (f) CPME, (g) MTBE (h) DME.

Fig. S7 Cell voltage and cathode potential during electrolysis with organic solvents as catholytes: (i) ethyl acetate, (j) acetonitrile, (k) DMSO.

- EIS with organic solvents as catholytes

Fig. S8 Results of EIS measurements with organic solvents as catholyte: (a) hexane, (b) cyclohexane, (c) toluene, (d) THF, (e) 1, 2-dioxane, (f) CPME, (g) MTBE (h) DME, (i) ethyl acetate, (j) acetonitrile, (k) DMSO.