Supporting Information

Enhancing Ammonia Electrosynthesis from Nitrate on Ru-RuO2 Electrodeposited Film

Felipe H. S. Santosa, Maykon L. Souzaa,b, Samuel C. Silvaa, Gabriel F. Costaa, João Batista Souza Juniora,c, Raphael Nagaoa,b,*

a Institute of Chemistry, University of Campinas, Campinas, SP 13083-862, Brazil

b Center for Innovation on New Energies, University of Campinas, Campinas, SP 13083-084, Brazil

c Brazilian Nanotechnology National Laboratory (LNNano), Brazilian Center for Research in Energy and Materials (CNPEM), Campinas, SP 13083-100, Brazil

*Corresponding author: nagao@unicamp.br

Figure S1. Cyclic voltammetry of gold rod at a scan rate of 20 mV s-1 in NaOH 1.0 mol L-1.

Figure S2. XPS survey spectrum of Ru-RuO2 pristine.

Figure S3. XPS survey spectrum of Ru-RuO2 after 1 h of NO3RR in 20 mmol L-1 NaNO3 + 1.0 mol L-1 NaOH at 0.0 V vs. RHE.

Figure S4. XPS survey spectrum of Ru-RuO2 after 2 h of NO3RR in 20 mmol L-1 NaNO3 + 1.0 mol L-1 NaOH at 0.0 V vs. RHE.

Figure S5. XPS survey spectrum of Ru-RuO2 after 12 h of NO3RR in 20 mmol L-1 NaNO3 + 1.0 mol L-1 NaOH at 0.0 V vs. RHE.

Figure S6. ECSA estimation. Cyclic voltammograms (CV) scan-rate/current relationship and the corresponding electrochemical active surface area (ECSA) analysis of the Ru-RuO2. Each CV curve (a-c) corresponds to its respective linear fitting plot shown directly below in panels (d-f). All measurements were carried out in 1.0 mol L-1 NaOH.

Figure S7. Calibration curve for ammonia (a) and calibration curve for nitrite (b).

Figure S8. UV-Vis spectra obtained after electrolysis at 0.0 V vs. RHE in electrolytes with and without nitrate. Only the electrolyte containing NO3- exhibits a pronounced absorbance peak within the wavelength range characteristic of the indophenol blue method used to quantify NH3, whereas the nitrate-free electrolyte shows no measurable absorbance. The blank solution and the NaOH electrolyte prior to electrolysis exhibited identical spectra, and their subtraction confirmed the absence of any spectral changes induced by electrolysis in nitrate-free conditions, confirming that the ammonia detected originates exclusively from NO3RR.

Figure S9. (a) AFM images and (b) Height profile of the pristine Ru-RuO2.

Figure S10. EDS spectra of the Au/Ru-RuO2 catalyst in the pristine and after 1, 2, and 12 h of NO3RR, with the inset highlighting the variation in the O signal around 0.52 keV.

Table S1. Comparison of the electrocatalytic NO3RR performance of Ru-RuO2 with those of some representative NO3RR electrocatalysts using inorganic aqueous electrolyte under room temperature and atmospheric pressure.

| Catalyst | Electrolyte | Max. FE for NH3 (potential) | Max. NH3 yield rate (potential) | Ref. |
| --- | --- | --- | --- | --- |
| Ru-RuO2 | 20 mmol L-1 NaNO3 + 1.0 mol L-1 NaOH | 71.20 ± 11.81% (0.0V vs. RHE) | 39.25 ± 0.92 µmol h-1 cm-2 (0.0 vs. RHE) | This work |
| RuO2 nanotubes | 1.0 mol L-1 KNO3 + 1.0 mol L-1 KOH | 18.2% FE (-1.10 V vs. SCE) | 30.5 µmol h-1 mgcat-1 (-1.10 V vs. SCE) | [1] |
| Strained Ru nanoclusters | 1.0 mol L-1 KOH + 1.0 mol L-1 KNO3 | ~100% (-0,2V vs. RHE) | 1.17 mmol h-1 cm-2 | [2] |
| Ru dispersed on Cu nanowires | 32.3 mmol L-1 KNO3 + 1.0 mol L-1 KOH | 96% (0.04 V vs. RHE) | 4.49 mmol h-1 cm-2 | [3] |
| Highly crystalline RuO2 nanosheets | 14 mmol L-1 NaNO3 + 0.5 mol L-1 Na2SO4 | 7.03% (-0.35 V vs. RHE) | 0.0013 mmol h-1 cm-2 (-0.35 V vs. RHE) | [4] |
| Ru single atoms (Ru SACs) | 3.57 mmol L-1 NaNO3 + 0.2 mol L-1 Na2SO4 | 85.6% (-0.55 V vs. RHE) | 45.82 µmol h-1 cm-2 (-0.55 V vs. RHE) | [5] |
| Ru Nanoclusters/TiO2 Nanotubes | 7.14 mmol L-1 KNO3 + 0.05 mol L-1 Na2SO4 | 96.91% (-0.4 V vs. RHE) | 35.35 µmol h-1 cm-2 | [6] |
| black Pearl 2000 carbon black (CB) | 0.1 mol L-1 KOH + 0.1 mol L-1 KNO3 | 50% (-0.45 V vs. RHE) | 104.55 µmol h-1 cm-2 (-0.45 V vs. RHE) | [7] |

References

- Jiang X, Chen PY, Wu WW, Guo JY, Li WW, Mao YJ, Sheng T, Zhao X, Wei L (2024) Enhanced electrocatalytic activity for nitrate reduction to ammonia by tuning a ruthenium oxidation state of ruthenium-based nanotubes. ACS Appl Nano Mater 7:22044-22051. https://doi.org/10.1021/acsanm.4c04066

- Li J, Zhan G, Yang J, Quan F, Mao C, Liu Y, Wang B, Lei F, Li L, Chan AWM, Xu L, Shi Y, Du Y, Hao W, Wong PK, Wang J, Dou SX, Zhang L, Yu JC (2020) Efficient ammonia electrosynthesis from nitrate on strained ruthenium nanoclusters. J Am Chem Soc 142:7036-7046. https://doi.org/10.1021/jacs.0c00418

- Chen FY, Wu ZY, Gupta S, Rivera DJ, Lambeets SV, Pecaut S, Kim JYT, Zhu P, Finfrock YZ, Meira DM, King G, Gao G, Xu W, Cullen DA, Zhou H, Han Y, Perea DE, Muhich CL, Wang H (2022) Efficient conversion of low-concentration nitrate sources into ammonia on a Ru-dispersed Cu nanowire electrocatalyst. Nat Nanotechnol 17:759-767. https://doi.org/10.1038/s41565-022-01121-4

- Wang Y, Li H, Zhou W, Zhang X, Zhang B, Yu Y (2022) Structurally disordered RuO2 nanosheets with rich oxygen vacancies for enhanced nitrate electroreduction to ammonia. Angew Chem Int Ed 61:e202202604. https://doi.org/10.1002/anie.202202604

- Xiang T, Liu X, Wang Z, Zeng Y, Deng J, Xiong W, Cheng M, Liu J, Zhou C, Yang Y (2025) Boosting active hydrogen generation via ruthenium single atoms for efficient electrocatalytic nitrate reduction to ammonia. Appl Catal B Environ Energy 365:124943. https://doi.org/10.1016/j.apcatb.2024.124943

- Qiu W, Xie M, Wang P, Gao T, Li R, Xiao D, Jin Z, Li P (2023) Size-defined Ru nanoclusters supported by TiO2 nanotubes enable low-concentration nitrate electroreduction to ammonia with suppressed hydrogen evolution. Small 19:2300437. https://doi.org/10.1002/smll.202300437

- Yhobu Z, Velmurugan R, Ebenezer J et al (2026) On the role of carbon additives in the electrochemical reduction of nitrate to ammonia in energy storage. J Solid State Electrochem. https://doi.org/10.1007/s10008-026-06525-z