Table S1 Properties and chemical composition of adsorbents (PAC, CNZ and XSZ)

| Properties | PAC | CNZ | XSZ | Composition (wt %) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Surface area(m2/g) Pore volume(mL3/g) Pore diameter(nm) Real density(g/mL3) | 853.80.799 3.74 0.423 | 76.35 0.251 7.50 2.430 | 316.80 0.543 3.61 1.242 | Na2O MgO Al2O3 SiO2 K2O CaO TiO2 MnO Fe2O3 P2O5 loss of ignition | CNZ | XSZ |
|  |  |  |  |  | 1.86 0.71 12.84 52.32 2.46 0.25 0.06 0.03 1.49 0.07 6.84 | 5.38 2.64 26.75 32.24 0.54 8.78 1.65 0.14 7.01 0.37 14.95 |

Table S2 Characteristics of the synthetic produced water

| Parameter | Range |
| --- | --- |
| Oil & grease (ppm) | 50-10000 |
| COD (ppm) | 1357-28609 |
| Turbidity (NTU) | 435 |
| TDS (ppm) | 100000 |
| pH | 2-10 |

Table S3 Isotherm parameters for oil and COD  adsorbed over  PAC and CNZ with the correlation coefficient.

| Isotherms | Langmuir |  |  | Freundlich |  |  | Temkin |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qmax (mg/g) | KL (L/mg) | R2 | KF (mg1−n g−1Ln) | 1/n | R2 | At(L/g) | bt(J/mol) | R2 |
| PAC (Oil) | 416 | 0.03709 | 0.9503 | 0.26859 | 0.4199 | 0.9901 | 0.52123 | 45.43919 | 0.9672 |
| CNZ (Oil) | 526 | 0.00366 | 0.8834 | 0.76952 | 0.7701 | 0.9983 | 0.10106 | 34.94065 | 0.8882 |
| PAC (COD) | 10000 | 0.00053 | 0.9142 | 0.22407 | 0.5134 | 0.9967 | 0.01400 | 1.56858 | 0.8843 |
| CNZ (COD) | 5000 | 0.00013 | 0.9805 | 0.46283 | 0.6128 | 0.9825 | 0.00231 | 3.136802 | 0.9645 |

Table S4 Thermodynamic parameters for the adsorption of oil  and COD over  PAC and CNZ adsorbents

| Oil adsorbed by PAC |  |  |  | Oil adsorbed by CNZ |  |  |  |  | COD adsorbed by PAC |  |  |  |  | COD adsorbed by CNZ |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Temp. (oC) | ΔHo (KJ/mol) | ΔSo (KJ/mol.ₒC) | ΔGo (KJ/mol) | ΔHo (KJ/mol) |  | ΔSo (KJ/mol.ₒC) |  | ΔGo (KJ/mol) | ΔHo (KJ/mol) |  | ΔSo (KJ/mol.ₒC) |  | ΔGo (KJ/mol) | ΔHo (KJ/mol) |  | ΔSo (KJ/mol.ₒC) | ΔGo (KJ/mol) |
| 10 |  |  | -1473 | 6278 |  | 20 |  | 389 | 6440 |  | 22 |  | -107 | 5762 |  | 4 | 4573 |
| 20 |  |  | -1587 |  |  |  |  | 267 |  |  |  |  | -140 |  |  |  | 4613 |
| 30 | 6758 | 28 | -1888 |  |  |  |  | 111 |  |  |  |  | -213 |  |  |  | 4633 |
| 40 |  |  | -2175 |  |  |  |  | 93 |  |  |  |  | -415 |  |  |  | 4528 |
| 50 |  |  | -2589 |  |  |  |  | 65 |  |  |  |  | -709 |  |  |  | 4433 |
| 55 |  |  | -2711 |  |  |  |  | 49 |  |  |  |  | -881 |  |  |  | 4423 |

Table S5 Kinetic adsorption parameters obtained using pseudo-first-order and pseudo-second-order models

| Adsorbent | pseudo-first-order |  |  | pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qe (mg g-1) | k1 (min−1) | R2 | qe (mg g-1) | k2 (g min-1 mg-1) | R2 |
| PAC (Oil) | 7.8146 | 0.0534 | 0.8913 | 50.34 | 0.004819 | 0.9995 |
| CNZ (Oil) | 3.7946 | 0.0544 | 08779 | 32.15 | 0.013359 | 0.9995 |
| PAC (COD) | 24.230 | 0.0446 | 0.8735 | 1111.11 | 0.000218 | 0.9991 |
| CNZ (COD) | 11.738 | 0.0415 | 0.8533 | 555.55 | 0.000456 | 0.9982 |

Table S6 The Optimum condition on the turbidity removal efficiency (initial turbidity =435 NTU)

| ReT% | Res.T(NTU) | Time (min) | pH | Dose (g/100mL) | Type of adsorbent |
| --- | --- | --- | --- | --- | --- |
| 99.65 | 1.5 | 60 | 2 | 0.3 | PAC |
| 99.91 | 0.38 | 60 | 2 | 0.3 | CNZ |
| 99.97 | 0.13 | 60 | 2 | 0.3 | XSZ |

Res.T: Residual turbidity, ReT   : Removal of turbidity

Table S7 The Optimum condition on the oil and COD removal efficiency (optimum Coil = 50 ppm and CCOD = 1357 ppm)

| ReTPH % | ReCOD % | Reoil % | Time (min) | pH | Dose (g/100mL) (g/100ml) | Type of adsorbent |
| --- | --- | --- | --- | --- | --- | --- |
| 99.84 | 95.87 | 99.58 | 60 | 2 | 0.3 | PAC |
| 85.06 | 63.74 | 84.8 | 50 | 2 | 0.3 | CNZ |
| 93.59 | 80.32 | 91.08 | 50 | 2 | 0.3 | XSZ |

Reoil : Removal of oil, ReCOD : Removal of COD,  ReTPH :Removal of  total petroleum hydrocarbon

Table S8  Results obtained  after adsorbent regeneration

| ReTPH % | ReCOD % | Reoil % | ReT % | Type of adsorbent |
| --- | --- | --- | --- | --- |
| 90.54 | 87.1 | 89.8 | 99.71 | PAC |
| 81.70 | 61.82 | 81 | 99.59 | CNZ |
| 84.45 | 71.48 | 83.2 | 99.75 | XSZ |