Immobilized Ionic Liquids/Deep Eutectic Solvents in Carbon Capture: Current Progress and Future Potential

Sahar Foorginezhad a*, Xiaoyan Ji a*

aEnergy Science/Energy Engineering, Department of Engineering Sciences and Mathematics, Luleå University of Technology, Luleå, Sweden

Xiaoyan Ji: xiaoyan.ji@ltu.se

Sahar Foorginezhad: sahar.foorginezhad@ltu.se

Table S1. Reported research studies on CO2 uptake using immobilized ILs/DESs.

| Porous solid | IL loading (wt.%) | Pore size (°A) | Pore volume (cm3/g) | Surface area (m2/g) |  | Recyclability |  | Uptake (mmol/g) |  |  | T (K) |  | Gas composition |  | Sorption type |  | P (bar) |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Bulk |  | Confined |  |  |  |  |  |  |  |  |  |
| SiO2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| DESs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [ChCl][U]@nanoporous silica | 10 | 31 | 0.018 | 275 |  | - |  | - |  | 0.52 | 298 |  | Pure CO2 |  | Chemical/ physical |  | 1 |  | (Ghazali et al., 2020) |
| [ChCl][EG]@nanoporous silica | 10 | 26 | 0.23 | 294 |  | - |  | - |  | 0.43 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Ghazali, Yarmo, et al., 2019) |
| [ChCl][Gly]@nanoporous silica | 10 | 28 | 0.15 | 194 |  | - |  | - |  | 0.46 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Ghazali, Yarmo, et al., 2019) |
| [ChCl][U]@mesoporous silica | 10 | 65.4 | 0.65 | 317.5 |  | - |  | - |  | 0.51 | 303 |  | Pure CO2 |  | Physical |  | 1 |  | (Ghazali, Hassan, et al., 2019) |
| [L-Arg][EG]@silica gel | 30 | 89.6 | 0.51 | 222 |  | - |  | - |  | 0.36 0.18 | 298 |  | Pure CO2, 15% CO2, 85% N2 |  | Chemical/ physical |  | 1 |  | (Suhaili et al., 2023) |
| [ChCl][EG]@silica gel | 30 | 81 | 0.39 | 147 |  | - |  | - |  | 0.33, 0.05 | 298 |  | Pure CO2, 15% CO2, 85% N2 |  | Chemical/ physical |  | 1 |  | (Suhaili et al., 2023) |
| [ChCl][EG][L-Arg]@silica gel | 30 | 89.8 | 0.33 | 138 |  | - |  | - |  | 0.34, 0.06 | 298 |  | Pure CO2, 15% CO2, 85% N2 |  | Chemical/ physical |  | 1 |  | (Suhaili et al., 2023) |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [BMIM][TF2N]@silica xerogel | - | 14.1 | 0.24 | 343 |  | 5 |  | 1.09 |  | 5 | 298 |  | Pure CO2 |  | Physical |  | 20 |  | (Dos Santos et al., 2020) |
| [BMIM][PF6]@SiO2 | 50-70 (20 was optimum) | 15-45 | 0.034 | 41 |  | 8 |  | 0.27 |  | 0.66 | 298 |  | - |  | Chemical |  | 1 |  | (Wang et al., 2022) |
| [BMIM][CF3SO3]@SiO2 | 1 | - | 0.033 | 47 |  | - |  | - |  | 1.68 | 298 |  | Pure CO2 |  | Physical/chemical |  | 1 |  | (Marliza et al., 2022) |
| [apaeP444][Lys]@silica | 50 | 589 | 1.22 | 42 |  | 138 |  | - |  | 1.44 | 298 |  | 14% CO2, 86% N2 |  | Chemical |  | 1 |  | (Ren et al., 2012) |
| [apaeP444][Gly]@silica | 50 | 420 | 1.21 | 58 |  | 1.38 × 103 |  | - |  | 1.54 | 298 |  | 14% CO2, 86% N2 |  | Chemical |  | 1 |  | (Ren et al., 2012) |
| [EMIM][Gly]@mesoporous silica gel | 50 | 224 | 0.19 | 34 |  | 10 |  | - |  | 1.31 | 303 |  | 15% CO2, 85% He |  | Chemical |  | - |  | (Sheshkovas et al., 2022) |
| [BMIM][acetate]@silica | 40 | - | - | 28 |  | - |  | ~1.8 |  | ~1.8 | 299 |  | Pure CO2 |  | Chemical |  | 1 |  | (Santiago et al., 2019) |
| [(3-aminopropyl)tributylphosphonium bromide hydrobromide][Gly]@Mesocellular silica foam | - | - | 0.27 | 33 |  | 10 |  | - |  | 0.58 | 348 |  | 15% CO2, 85% N2 |  | Chemical |  | 1 |  | (Liu & Sie, 2016) |
| [(3-aminopropyl)tributylphosphonium bromide hydrobromide][Lys]@Mesocellular silica foam | - | - | 0.26 | 40 |  | 10 |  | - |  | 1.38 | 348 |  | 15% CO2, 85% N2 |  | Chemical |  | 1 |  | (Liu & Sie, 2016) |
| [(3-aminopropyl)tributylphosphonium bromide hydrobromide][Arg]@Mesocellular silica foam | - | - | 0.38 | 47 |  | 10 |  | - |  | 0.63 | 348 |  | 15% CO2, 85% N2 |  | Chemical |  | 1 |  | (Liu & Sie, 2016) |
| [C6MIM][NO3]@SiO2 | 20 | 73.3 | 0.381 | 206.38 |  | 8 |  | 0.54 |  | 0.48 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Mirzaei et al., 2024) |
| [P4444][AcO]@SiO2 | 100 | - | 0.12 | 11 |  | 6 |  | - |  | 0.38 | 298 |  | 15% CO2, 80% N2, 5% O2 |  | Chemical |  | 1 |  | (Yousefe et al., 2023) |
| 1-ethyl-3-methylimidazolium tri[bis(trifluoromethylsulfo-nyl)amide]zincate@ alumino-silicate | 25 | - | 0.06 | 11 |  | - |  | ~0.7 |  | 2.93 | 313 |  | Pure CO2 |  | Chemical/ physical |  | 1 |  | (Arellano et al., 2015a) |
| 1-ethyl-3-methylimidazolium tri[bis(trifluoromethylsulfo-nyl)amide]zincate@nano SiO2 | 25.1 | Interparticle porosity | Interparticle porosity | 82 |  | - |  | ~0.7 |  | 3.4 | 313 |  | Pure CO2 |  | Chemical/ physical |  | 1 |  | (Arellano et al., 2015a) |
| 1-ethyl-3-methylimidazolium tri[bis(trifluoromethylsulfo-nyl)amide]zincate@fumed SiO2 | 26.2 | 152 & 254 | 0.39 | 99 |  | - |  | ~0.7 |  | 2.7 | 313 |  | Pure CO2 |  | Chemical/ physical |  | 1 |  | (Arellano et al., 2015a) |
| [P4444][2-Op]@mesoporous SiO2 | 10 | 112 | 1.41 | 620.5 |  | 10 |  | ~0.58 |  | ~1.7 | 323 |  | 14.9% CO2, 85.1% N2 |  | Chemical |  | - |  | (Xue, Feng, Zhu, et al., 2019) |
| [N4444][2-Op]@mesoporous silica | 15 | 112 | 1.44 | 664.0 |  | 10 |  | ~0.52 mol/mol |  | ~1.1 | 323 |  | 14.9% CO2, 85.1% N2 |  | Chemical |  | - |  | (Xue, Feng, Zhu, et al., 2019) |
| [C16MIM][Cl] @monodisperse silica microsphere | - | - | - | - |  | - |  | - |  | 0.170 | 343 |  | Pure CO2 |  | Physical |  | 1.02 |  | (Tanaka et al., 2011) |
| [C16MIM][BF-4]@monodisperse silica microsphere | - | - | - | - |  | - |  | - |  | 0.171 | 343 |  | Pure CO2 |  | Physical |  | 1.02 |  | (Tanaka et al., 2011) |
| [C16MIM][ (CF3SO2)2N–]@monodisperse silica microsphere | - | - | - | - |  | - |  | - |  | 0.169 | 343 |  | Pure CO2 |  | Physical |  | 1.02 |  | (Tanaka et al., 2011) |
| Mixture of molecular sieve 4 A°/Amine functionalized silica-gel confined by task-specific IL | 55 | 64 | 0.31 | 127 |  | 10 |  | 2.27 |  | 4.83 | 298 |  | Pure CO2 |  | Chemical/ physical |  | 1 |  | (Aboudi & Vafaeezadeh, 2015) |
| [BMIM][NO3]@silica | 50 | <10 | 0.0004 | <1 |  | - |  | 0.32 |  | 0.36 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Mirzaei et al., 2017) |
| [BMIM][SCN]@silica | 50 | <10 | 0.0031 | <2 |  | - |  | 0.25 |  | 0.28 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Mirzaei et al., 2017) |
| [BMIM][N(CN)2]@silica | 50 | - | - | - |  | - |  | 0.42 |  | 0.30 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Mirzaei et al., 2017) |
| [BMIIM][HSO4]@silica | 50 | - | - | - |  | - |  | 0.30 |  | 0.56 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Mirzaei et al., 2017) |
| P[VBTMA][BF4]@meso-SiO2 | - | - | - | - |  | 2 |  | 0.39 |  | 0.40 | 303 |  | 10% CO2, 90% N2 |  | Physical |  | 1 |  | (Cheng et al., 2015) |
| P[VBTMA][PF6]@meso-SiO2 | - | - | - | - |  | 2 |  | 0.33 |  | 0.38 | 303 |  | 10% CO2, 90% N2 |  | Physical |  | 1 |  | (Cheng et al., 2015) |
| [i-C5TPIm][Cl]@mesoporous SiO2 | 5 | 27.1 | 0.68 | 461 |  | 3 |  | - |  | 1.53 | 318 |  | Pure CO2 |  | - |  | 4 |  | (Duczinski et al., 2020) |
| [i-C5TPIm][Tf2N]@mesoporous SiO2 | 5 | 21.5 | 0.62 | 426 |  | 5 |  | - |  | 1.81 | 318 |  | Pure CO2 |  | - |  | 4 |  | (Duczinski et al., 2020) |
| 1,3-bis(3-trimethoxysilyl propyl)imidazolium chloride @mesoporous SiO2 from rice husk | 20 | - | - | 109.9 |  | - |  | - |  | 1.25 | 298 |  | Pure CO2 |  | - |  | 4 |  | (Duczinski et al., 2018) |
| 1-methyl-3-(3-trimethoxysilyl propyl)imidazolium chloride @mesoporous SiO2 from rice husk | 10 | 12.8 | 0.36 | 562.4 |  | 6 |  | - |  | 1.78 | 298 |  | Pure CO2 |  | - |  | 4 |  | (Duczinski et al., 2018) |
| 1,3-dibutylimidazolium acetate@amino-propyl functionalized mesoporous SiO2 | - | 61 | 0.22 | 111 |  | - |  | - |  | 1.8 | 273 |  | Pure CO2 |  | - |  | 1 |  | (MacQueen et al., 2014) |
| 1-(silylpropyl)-3-methyl-imidazolium hexafluorophosphate@Vycor® | - | - | 0.2 | 147 |  | - |  | ~0.11 |  | ~0.6 | 273 |  | - |  | - |  | 1 |  | (Romanos et al., 2009) |
| [AEMP][Gly]@SiO2 | - | - | 0.29 | 223.43 |  | 6 |  | 1.4 molar fraction (20% [AEMP][Gly] in water) |  | 1.5 (mol CO2:mol IL) | 333 |  | Pure CO2 |  | Chemical |  | 1 |  | (Peng et al., 2013) |
| P[VYIM][Bu2PO4]@SiO2 | 8.16 | <10 | 0.0733 | 250.4 |  | - |  | - |  | 1.03 | 273 |  | Pure CO2 |  | Physical |  | 1 |  | (Sun et al., 2017) |
| P[AMIM][BF4]@SiO2 | 5 | <10 | 0.0636 | 213.2 |  | - |  | - |  | 0.88 | 273 |  | Pure CO2 |  | Physical |  | 1 |  | (Sun et al., 2017) |
| P(C8H17)PF6@SiO2 | 50 | 4-8 | - | 349.7 |  | - |  | - |  | 1.44 | 273 |  | Pure CO2 |  | Physical |  | 1 |  | (JM Zhu et al., 2014) |
| [N6666][Ile]@SiO2 | 40 | - | - | - |  | - |  | - |  | 1 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Kolding et al., 2012) |
| [N6666][Gly]@ SiO2 | 40 | - | - | - |  | - |  | - |  | 0.8 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Kolding et al., 2012) |
| [N6666][Asn]@ SiO2 | 40 | - | - | - |  | - |  | - |  | 0.77 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Kolding et al., 2012) |
| [N6666][Tyr]@ SiO2 | 40 | - | - | - |  | - |  | - |  | 0.84 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Kolding et al., 2012) |
| [N6666][Pro]@ SiO2 | 40 | - | - | - |  | - |  | - |  | 1.05 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Kolding et al., 2012) |
| 1-methyl-3-(3-trimethoxysilylpropyl) imidazolium chloride@silica xerogel | 20 | 75 | 0.008 | 4 |  | - |  | - |  | 2.16 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (S Aquino et al., 2019) |
| [BMIM][Cl]@rice husk SiO2, [BMIM][OAc]@rice husk SiO2 | 10 | 38.8, 31.1 | 0.23, 0.25 | 164, 165 |  | 10 |  | - |  | 0.86, 0.98 | 298 |  | - |  | Chemical/ physical |  | 1 |  | (Bárbara B Polesso et al., 2019) |
| [BMIM][BF4]@SiO2 | 50 | Negligible | 0.0005 | <1 |  | - |  | - |  | 0.25, 0.14, 0.1 | 298 |  | - |  | Physical |  | 12, 25, 50 mL/min |  | (Mirzaei et al., 2018) |
| [P4444][2-Op]@mesoprous silica vesicle | 10 | 92 | 1.38 | 847 |  | 10 |  | - |  | 1.49 | 323 |  | 15% vol. CO2 and 85% N2 |  | Chemical/ physical |  | 0.15, 0.2 bar |  | (Xue, Feng, Zhang, et al., 2019) |
| 1-Ethyl-3-methylimidazolium bis(trifluoromethylsulfonyl)imide@amine-based silica aerogel | - | 110.40 | - | 6.37 |  | - |  | - |  | 5.53 | 298 |  | 50% CO2 50% N2 |  | Chemical/ physical |  | 1 |  | (Garip & Gizli, 2020) |
| Si-[P8883]TFSI@SiO2, [OMIM]TFSI@SiO2, [EMIM]TFSI@SiO2 | 20-50 (20 was the optimum) | <16 | 0.09, 0.0496, 0.0437 | 263.9, 144.3, 127.4 |  | 6 |  | - |  | ~1, ~0.65, ~0.21 | 313 |  | - |  | Physical |  | 1 |  | (Zhu et al., 2018) |
| Si–P4443BF4@ SiO2 Si–P8883BF4@ SiO2 | - | <8 | 0.0781 | 253.7 |  | 4 |  | - |  | 1.12 | 298 |  | Pure CO2 |  | Physical |  | 2 |  | (Jiamei Zhu et al., 2014) |
| 1-ethyl-3-methylimidazolium tri[bis(trifluoromethylsulfonyl)imide] zincate(II)@ Bio-templated mesoporous silica beads | 27.8 | 50-150 | 0.23 | 94 |  | - |  | 0.11 (ET), 0.66 (EZT) |  | ~2 | 313 |  | Pure CO2 |  | Chemical/ physical |  | - |  | (Arellano et al., 2016) |
| Commercial silica: [MBMIM][Br]@SiO2 [MBMIM][Tf2N]@SiO2 | 10-30 (10 was the highest) | 23.8, 23.8 | 0.56, 0.54 | 441, 381 |  | 5 |  | - |  | ~1.86, ~1.27 | 318 |  | Pure CO2 |  | Chemical |  | 4 |  | (Bárbara Burlini Polesso et al., 2019) |
| [BMIM][CF3SO3]@SiO2 | 1-10 (1 was the highest) | 28 | 0.033 | 46.51 |  | - |  | - |  | 1.52 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Marliza et al., 2017) |
| 1-methyl-3-(3-triethoxysilylpropyl) imidazolium Chloride (lysine)@ordered mesoporous silica | - | 96 | 0.78 | 325 |  | 10 |  | - |  | 0.61 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Hiremath et al., 2016) |
| 1-methyl-3-(3-triethoxysilylpropyl) imidazolium Chloride (glycine)@ordered mesoporous silica | - | 109 | 0.77 | 281 |  | 10 |  | - |  | 0.5 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Hiremath et al., 2016) |
| 1-methyl-3-(3-triethoxysilylpropyl) imidazolium Chloride (alanine)@ordered mesoporous silica | - | 108 | 0.79 | 294 |  | 10 |  | - |  | 0.5 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Hiremath et al., 2016) |
| 1-methyl-3-(3-triethoxysilylpropyl) imidazolium Chloride (proline)@ordered mesoporous silica | - | 105 | 0.8 | 304 |  | 10 |  | - |  | 0.53 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Hiremath et al., 2016) |
| SBA-15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| DESs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [MEACl][EDA]@SBA-15 | 5 | 99.3 | 1.18 | 385.15 |  | 5 |  | - |  | 1.98 | 298 |  | Pure CO2 |  |  |  | 1 |  | (Foorginezhad & Ji, 2024) |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [P4444][3-aminopyrazole]@SBA-15 | 50 | - | - | - |  | - |  | - |  | 1.41 | 393 |  | Pure CO2 |  | Chemical |  | 1 |  | (Mi et al., 2014) |
| DIL_2FeCl4@SBA-15 | 10 | 42.16–53.66 | 0.899 | 347 |  | 10 |  | - |  | 1.30 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Duarte et al., 2024) |
| DIL_NTf2/FeCl4@SBA-15 | 10 | 42.16–53.66 | 0.870 | 263 |  | - |  | - |  | 1.24 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Duarte et al., 2024) |
| [EMIM][Lys]@PE-SBA-15 | 50 | <40 | 1.07 | 191 |  | 6 |  | - |  | 1.4 | 303 |  | 15% CO2, 85% N2 |  | - |  | 1 |  | (Uehara et al., 2019b) |
| [EMIM][Lys]@SBA-15 | 60 | <10 | 0.05 | 33 |  | 6 |  | - |  | 1 | 303 |  | 15% CO2, 85% N2 |  | - |  | 1 |  | (Uehara et al., 2019b) |
| [AEMIM][Lys]@ SBA-15 | 50 | 71 | 0.09 | 44 |  | - |  | - |  | ~0.5 | 303 |  | 15% CO2, 85% N2 |  | Physical |  | 1 |  | (Huang et al., 2021) |
| [AEMIM][Lys]@ SBA-15-SA | 50 | 61 | 0.12 | 105 |  | - |  | - |  | ~0.83 | 303 |  | 15% CO2, 85% N2 |  | Physical |  | 1 |  | (Huang et al., 2021) |
| [AEMIM][Lys]@ PE-SBA-15 | 50 | 139 | 0.26 | 66 |  | 10 |  | - |  | ~0.85 | 303 |  | 15% CO2, 85% N2 |  | Physical |  | 1 |  | (Huang et al., 2021) |
| [BMIM][BF4]@SBA-15 | 6.85 | 52.3 | 0.75 | 575 |  | 5 |  | 0.375 |  | 0.758 | - |  | 3% CO2, 97% N2 (molar fraction) |  | - |  | - |  | (Yin et al., 2018) |
| [BMIM][Ac]@SBA-15 | 41.90 | ~53.9 | ~0.66 | ~490 |  | 5 |  | 0.465 |  | 0.849 | - |  | 3% CO2, 97% N2 (molar fraction) |  | - |  | - |  | (Yin et al., 2018) |
| [BMIM][BF4]@SBA-15 | 36.9 | 5.3 | 0.56 | 347 |  | - |  | 0.16 |  | 1.17 | 298 |  | 10% CO2, 90% N2 (molar ratio) |  | Chemical |  | 2 |  | (Xu et al., 2016) |
| [BMIM][Ac]@ SBA-15 | 60 | Negligible | 0.04 | 7.3 |  | 10 |  | - |  | ~0.88 | 303 |  | - |  | Chemical |  | 1 |  | (Mohamedali et al., 2020) |
| 1-n-butyl-3-methylimidazolium chloride @NH2-SBA-15 | 10 | 57 | 0.38 | 239.7 |  | 5 |  |  |  | 1.75 | 298 |  | 15% CO2 and 85% N2 |  | Chemical/ physical |  | 1 |  | (Wang & Yang, 2020) |
| [P66614][Triz]@ SBA-15 | 50 (Almost filled the pores) | 21.9 | 0.003 | 1.15 |  | 9 |  | - |  | 0.7, 0.68 | 293, 303 |  | CH4/H2 /CO2= 12:3:10 |  | Chemical |  | 1 |  | (Cheng et al., 2018) |
| [BMIM][Cl]@ SBA-15, [BMIM][OAc]@ SBA-15 | 8-10 | 50.7, 50.7 | 0.79, 0.76 | 491, 399 |  | 10 |  | - |  | 1.07 | 298 |  | - |  | Chemical/ physical |  | 4 |  | (Bárbara B Polesso et al., 2019) |
| EZT3 (1-ethyl-3-methylimidazolium tri [bis(trifluoromethyl sulfonyl) amide] zincate)@SBA-15 | 0-50 (50 was highest) Thickness 11 °A | 70 | 0.50 | 288 |  | - |  | ~0.5 |  | ~4.7 | 298 |  | Pure CO2 |  | Physical/ chemical |  | 1 |  | (Arellano et al., 2015b) |
| [TEPA][NO3]@SBA-15 | 0-85 (50 was the highest uptake) | 32.2 | 0.09 | 21.90 |  | 10 |  | - |  | 2.15 | 333 |  | 15% vol. CO2 85% N2 |  | Chemical/ physical |  | 0.15 |  | (Zhang, Gao, Li, Bernards, He, et al., 2019) |
| Triethylenetetrammonium nitrate protic ionic liquid@SBA-15 | 66 | 36.5 | 0.10 | 24.39 |  | 10 |  | - |  | 2.12 | 333 |  | 15% vol. CO2 85% N2 |  | Chemical/ physical |  | 1 |  | (Zhang, Gao, Li, Bernards, Li, et al., 2019) |
| [EMIM][Lys]@SBA-15 with surfactant | 50 | - | 0.15 | 24 |  | 10 |  | - |  | ~1.35 | 303 |  | 15% vol. CO2 85% N2 |  | - |  | 1 |  | (Uehara et al., 2019a) |
| [TMA][Tau]@SBA-15 (commercial) | 33 | 62 | 0.21 | 133 |  | - |  | - |  | 0.80 | 298 |  | Pure CO2 |  | - |  | 1 |  | (Ruckart et al., 2015) |
| [TBA][Tau]@SBA-15 | 58 | 78 | 0.02 | 10 |  | - |  | 4 |  | 1 | 298 |  | Pure CO2 |  | - |  | 1 |  | (Ruckart et al., 2015) |
| [EMIM][Ac]@PEI modified SBA-15 | ~32 | - | 0.01 | 7 |  | 11 |  | - |  | 2.20 | 303 |  | Pure CO2 |  | - |  | 1 |  | (Liu et al., 2018) |
| MCM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1-methyl-3-(trimethoxysilylpropyl)-imidazolium chloride@MCM-41 | 50 | - | 0.32 | 239.5 |  | - |  | - |  | 1.48 | 298 |  | Pure CO2 |  | - |  | 1 |  | (Aquino et al., 2015) |
| 1-methyl-3-(trimethoxysilylpropyl)-imidazolium tetrafluoroborate@MCM-41 | 50 | - | 0.048 | 9.39 |  | - |  | - |  | 0.34 | 298 |  | Pure CO2 |  | - |  | 1 |  | (Aquino et al., 2015) |
| 1-methyl-3-(trimethoxysilylpropyl)-imidazolium hexafluorophosphate@MCM-41 | 50 | - | 0.26 | 120.7 |  | - |  | - |  | 0.57 | 298 |  | Pure CO2 |  | - |  | 1 |  | (Aquino et al., 2015) |
| 1-methyl-3-(trimethoxysilylpropyl)-imidazolium bis(trifluoromethylsulfonyl)imide@MCM-41 | 50 | - | 0.25 | 233.7 |  | - |  | - |  | 0.23 | 298 |  | Pure CO2 |  | - |  | 1 |  | (Aquino et al., 2015) |
| [aP4443][2-Np]@MCM-41 | 30 | 28.84 | 0.733 | 891.59 |  | 6 |  | 1.9 |  | 3.19 | 303 |  | Pure CO2 |  | Chemical |  | 1 |  | (Ye et al., 2020) |
| [P4444][3-aminopyrazole]@MCM-41 | 50 | - | 0.01 | 7.5 |  | Drop from the 2nd cycle |  | - |  | 1.45 | 393 |  | Pure CO2 |  | Chemical |  | 1 |  | (Mi et al., 2014) |
| [P4444][3-aminopyrazole]@MCM-48 | 50 |  |  |  |  |  |  |  |  | 1.41 | 393 |  | Pure CO2 |  | Chemical |  | 1 |  | (Mi et al., 2014) |
| [C10MIN][NO3]@MCM-41 | 20 | - | - | - |  | 8 |  | - |  | 0.55 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Mirzaei et al., 2024) |
| [C6MIN][NO3]@MCM-41 | 20 | 31.7 | 0.173 | 217.74 |  | 8 |  | 0.54 |  | 0.52 | 298 |  | Pure CO2 |  | Physical |  | 1 |  | (Mirzaei et al., 2024) |
| [Tetrabutylphosphonium][3-aminopyrazole]@MCM-41 | 67 | - | 0.005 | 5.7 |  | 7 |  | - |  | 1.84 | 393 |  | Pure CO2 |  | Chemical |  | 1 |  | (Wan et al., 2014) |
| [Tetrabutylphosphonium][imidazole]@MCM-41 | 67 | - | 0.002 | 2 |  | 7 |  | - |  | 0.91 | 393 |  | Pure CO2 |  | Chemical |  | 1 |  | (Wan et al., 2014) |
| 1-methyl-3-(3-trimethoxysilylpropyl) imidazolium chloride@ MCM-41 | 20 | 17.1 | 0.39 | 455.7 |  | - |  | - |  | 1.31 | 298 |  | Pure CO2 |  | - |  | 4 |  | (Duczinski et al., 2018) |
| 1,3-bis(3-trimethoxysilyl propyl)imidazolium chloride @MCM-41 | 20 | 16.4 | 0.33 | 407.6 |  | - |  | - |  | 1.41 | 298 |  | Pure CO2 |  | - |  | 4 |  | (Duczinski et al., 2018) |
| [P66614][2-Op]@MCM-41 | 50 | 3.82 | 0.01 | 3.48 |  | - |  | 2.18 |  | 2.05 | 298 |  | Pure CO2 |  | Chemical |  | 1 |  | (Cheng et al., 2016) |
| [BMIM][Ac]@ MCM-41 | 60 | Negligible | 0.01 | 1.2 |  | 10 |  | - |  | ~1.75 | 303.15 |  | - |  | Chemical |  | 1 |  | (Mohamedali et al., 2020) |
| [EMIM][Lys]@MCM-41 | 50 | - | - | - |  | 10 |  | - |  | ~1.3 | 303 |  | 15% vol. CO2 85% N2 |  | - |  | 1 |  | (Uehara et al., 2019a) |
| Tetrabutyl phosphonium hydroxide solution and 2-hydroxypyridine@MCM-41 | 5 | 27.3 | 0.75 | 830.8 |  | 10 |  | ~0.13 |  | 1.21 | 323 |  | 14.5 vol% CO2 85.5% N2 |  | - |  | 1 |  | (Xue et al., 2017) |
| MCM-41 grafted with (3-mercaptopropyl) trimethoxysilane and oxidized with H2O2 and H2SO4 impregnated with: [thepAm][Br], [VBTMA][Cl] | - | 27.8, 27 | 0.31, 0.33 | 448, 484 |  | 10 |  | 1.16 at 50 bar and 313 K |  | 3.6, 3.9 | 303 |  | 0.20 CO2, 0.44 CO, 0.36 H2 (molar fraction) |  | Chemica/ physical |  | 50 |  | (Nkinahamira et al., 2017) |
| Al2O3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [P4444][3-aminopyrazole]@Alumina | 50 | - | 0.035 | 13 | Dropped after 2nd cycle |  | - |  | 1.2 |  |  | 393 |  | Pure CO2 |  | Chemical |  | 1 | (Mi et al., 2014) |
| [Tetrabutylphosphonium][3-aminopyrazole]@p-Al2O3 | 50 | - | 0.035 | 13 | 7 |  | - |  | 1.2 |  |  | 393 |  | Pure CO2 |  | Chemical |  | 1 | (Wan et al., 2014) |
| [Tetrabutylphosphonium][imidazole]@p-Al2O3 | 50 | - | 0.03 | 6.5 | 7 |  | - |  | 1.16 |  |  | 393 |  | Pure CO2 |  | Chemical |  | 1 | (Wan et al., 2014) |
| [MOEMIM][Gly]@mesoporous Al2O3 | - | - | ~0 | 0.03 | 8 |  | - |  | 3.27 |  |  | 313 |  | Pure CO2 |  | Chemica/ physical |  | 1 | (Sun & Tang, 2019) |
| [EMIM][Gly]@γ-alumina | 16 | 88 | 0.23 | 83 | 5 |  | - |  | 0.58 |  |  | 303 |  | 15% vol. CO2 and 85% N2 |  | Chemical/ physical |  | 1 | (Balsamo et al., 2018) |
| Commercial alumina: [MBMIM][Tf2N]@Al2O3 | 10 | 27.5 | 0.12 | 73 | 5 |  | - |  | 1.32 |  |  | 318 |  | Pure CO2 |  | - |  | 4 | (Bárbara Burlini Polesso et al., 2019) |
| P[VCIm]Cl@γ-Al2O3 | 60 | 180.3 | 0.79 | 159.20 | 5 |  | - |  | ~0.58 |  |  | 313 |  | Pure CO2 |  | Chemical/ physical |  | 1 | (Zhou et al., 2020) |
| [MBMIM][Br]@Al2O3 | 10 | - | - | 7 | 5 |  | - |  | 1.66 |  |  | 318 |  | 15.89% CO2 84.11% |  | - |  | 4 | (Bárbara Burlini Polesso et al., 2019) |
| Polymeric particles |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [EMIM][Gly]@PMMA | 50 | - | - | - | 5 |  | ~0.46 |  | 1.53 |  |  | 313 |  | Pure CO2 |  | Chemical |  | 1 | (Wang, Akhmedov, Duan, Luebke, & Li, 2013) |
| [EMIM][Ala]@PMMA | 50 | - | - | - | 5 |  | ~0.44 |  | 1.38 |  |  | 313 |  | Pure CO2 |  | Chemical |  | 1 | (Wang, Akhmedov, Duan, Luebke, & Li, 2013) |
| [EMIM][Arg]@PMMA | 50 | - | - | - | 5 |  | ~0.098 |  | 1.01 |  |  | 313 |  | Pure CO2 |  | Chemical |  | 1 | (Wang, Akhmedov, Duan, Luebke, & Li, 2013) |
| [EMIM][Lys]@PMMA | 50 | - | 0.35 | 38 | - |  | - |  | 1.06 |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical/ physical |  | 1 | (Uehara et al., 2018) |
| [P4444][Lys]@PMMA | 50 | - | 0.32 | 37 | - |  | - |  | 0.79 |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical |  | 1 | (Uehara et al., 2018) |
| [P4444][Gly]@PMMA | 50 | - | 0.25 | 26 | - |  | - |  | 0.83 |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical |  | 1 | (Uehara et al., 2018) |
| [EMIM][Gly]@PMMA | 50 | - | - | - | - |  | - |  | 0.88 |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical |  | 1 | (Uehara et al., 2018) |
| [EMIM][His]@PMMA | 50 | - | - | - | - |  | - |  | 0.63 |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical |  | 1 | (Uehara et al., 2018) |
| [EMIM][Ala]@PMMA | 50 | - | - | - | - |  | - |  | 0.80 mmol/g |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical |  | 1 | (Uehara et al., 2018) |
| [EMIM][BALA]@PMMA | 50 | - | - | - | - |  | - |  | 0.80 mmol/g |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical |  | 1 | (Uehara et al., 2018) |
| [EMIM][Arg]@PMMA | 50 | - | - | - | - |  | - |  | 0.28 mmol/g |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical |  | 1 | (Uehara et al., 2018) |
| [P4444][His]@PMMA | 50 | - | - | - | - |  | - |  | 0.56 mmol/g |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Chemical |  | 1 | (Uehara et al., 2018) |
| [AEMIM][Lys]@PMMA | 50 | - | - | - | 10 |  | - |  | 1.5 |  |  | 303 |  | 15% CO2, 85% N2 |  | Physical |  | 1 | (Huang et al., 2021) |
| [EMIM][Gly]@PMMA | - | - | - | - | 5 |  | - |  | 0.88 |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Physical/ chemical |  | 1 | (Uehara et al., 2017) |
| [EMIM][Lys]@PMMA | - | - | 0.35 | 38 | 5 |  | - |  | 1.06 |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Physical/ chemical |  | 1 | (Uehara et al., 2017) |
| [EMIM][Arg]@PMMA | - | - | - | - | 5 |  | - |  | 0.28 |  |  | 303 |  | 2.3% CO2, 97.7% N2 |  | Physical/ chemical |  | 1 | (Uehara et al., 2017) |
| [EMIM][Lys]@PMMA microsphere | 48.7 | <1200 | 0.31 | 27 | >14 |  | <0.19 (mol/mol) |  | 1.67 or 0.87 (mol/mol) |  |  | 298 |  | Pure CO2 |  | - |  | 1 | (Wang, Akhmedov, Duan, Luebke, Hopkinson, et al., 2013) |
| [EMIM][Lys]@PMMA | 50 | 100-1000 | 0.35 | 38 | 6 |  | - |  | 1.2 |  |  | 303 |  | 15% CO2, 85% N2 |  | - |  | 1 | (Uehara et al., 2017) |
| [N1111][Gly]@PMMA | 50 | 298 | 0.25 | 28.16 | 10 |  | - |  | 2.14 |  |  | 308 |  | 10% vol. CO2 and 90% N2 |  | Physical/ chemical |  | 0.1 | (Ren et al., 2018) |
| [C2OHMIM][Lys]@GDX | 60 | 70 | 0.05 | 31 | 6 |  | - |  | 1.29 |  |  | 313 |  | Pure CO2 |  | - |  | 1 | (Wu et al., 2023) |
| [N2222][Gly]@PDVB | 51 | <300 | 0.15 | 20.2 | 9 |  | ~2.7 at 348 K |  | ~1.75 |  |  | 303 |  | 1% vol CO2, 99% N2 |  | Physical/ chemical |  | 1 | (Xu, Zhang, Cheng, Li, Lan, Jiang, Huang, et al., 2021) |
| [BMIM Cl]@PUF [BMIM BF4]@PUF | 15, 40 | - | - | - | 6 |  | - |  | 9.66, 5.45 |  |  | 298 |  | 35% mol CO2 65% CH4 |  | Physical |  | 25 | (Rojas et al., 2017) |
| [N2222]2[IDA] @PDVB, [N2222]2[EDDA] @PDVB | 55, 60 | Negligible | 0.02, 0.04 | 6.8, 11.3 | 8 |  | - |  | 1.31, 1.65 |  |  | 303 |  | 10 vol% CO2 90 vol% N2 |  | Chemical |  | 1 | (Xu, Zhang, Cheng, Li, Lan, Jiang, Peng, et al., 2021) |
| [P2222][BnIm]@PDMS | - | - | - | - | 6 |  | - |  | 0.9 |  |  | 333 |  | - |  | Physical/ chemical |  | 1 | (T. Song et al., 2019) |
| Carbon |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| DESs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [ChCl][Gly]@carbon | 5 | 23.3 | 0.13 | 260 | 3 |  | - |  | 0.35 |  |  | 303 |  | Pure CO2 |  | - |  | 1 | (Ariyanto et al., 2021) |
| [ChCl][EG]@carbon | 5 | 22.9 | 0.10 | 218 | 3 |  | - |  | 0.31 |  |  | 303 |  | Pure CO2 |  | - |  | 1 | (Ariyanto et al., 2021) |
| [ChCl][1-butanol]@carbon | 5 | 23.6 | 0.09 | 244 | 3 |  | - |  | 0.30 |  |  | 303 |  | Pure CO2 |  | - |  | 1 | (Ariyanto et al., 2021) |
| [ChCl][Gly]@carbon | - | Micropore | 0.233 | 455.18 | - |  | - |  | 0.22 |  |  | - |  | 15% CO2 85% N2 |  | Chemical/physical |  | - | (Zulkurnai et al., 2017) |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [P66614][Triz]@carbon black | 25 | <500 |  | 35.6 | - |  | - |  | 0.62 |  |  | 298 |  | 3% CO2, 97% N2 |  | Chemical |  | 1 | (Gargiulo et al., 2016) |
| [P4444][3-aminopyrazole]@AC | 50 | - | - | - | - |  | - |  | 0.18 |  |  | 393 |  | Pure CO2 |  | Chemical |  | 1 | (Mi et al., 2014) |
| [BPIM][Br]@ activated carbon | - | 14.6 | 0.275 | 460 | 10 |  | - |  | ~1.7 |  |  | 293 |  | 76% CH4, 23% CO2, 1% H2S |  | Physical |  | 1 | (Wang et al., 2015) |
| [EPIM-NH2][Br]@ activated carbon | - | 13.8 | 0.289 | 495.3 | 10 |  | - |  | ~1.35 |  |  | 293 |  | 76% CH4, 23% CO2, 1% H2S |  | Physical/ chemical |  | 1 | (Wang et al., 2015) |
| [BPIM][BF4]@ activated carbon | - | - | - | - | - |  | - |  | ~1.9 |  |  | 293 |  | 76% CH4, 23% CO2, 1% H2S |  | Physical |  | 1 | (Wang et al., 2015) |
| [BPIM][PF6]@ activated carbon | - | - | - | - | - |  | - |  | ~2.15 |  |  | 293 |  | 76% CH4, 23% CO2, 1% H2S |  | Physical |  | 1 | (Wang et al., 2015) |
| [BPIM][TF2N]@ activated carbon | - | - | - | - | - |  | - |  | ~2.16 |  |  | 293 |  | 76% CH4, 23% CO2, 1% H2S |  | Physical |  | 1 | (Wang et al., 2015) |
| [EPIM-NH2][BF4]@ activated carbon | - | - | - | - | - |  | - |  | ~2.38 |  |  | 293 |  | 76% CH4, 23% CO2, 1% H2S |  | Physical/ chemical |  | 1 | (Wang et al., 2015) |
| [EPIM-NH2][PF6]@ activated carbon | - | - | - | - | - |  | - |  | ~2.4 |  |  | 293 |  | 76% CH4, 23% CO2, 1% H2S |  | Physical/ chemical |  | 1 | (Wang et al., 2015) |
| [EPIM-NH2][TF2N]@ activated carbon | - | - | - | - | - |  | - |  | ~2.41 |  |  | 293 |  | 76% CH4, 23% CO2, 1% H2S |  | Physical/ chemical |  | 1 | (Wang et al., 2015) |
| [DMEDAH][formate]@ activated carbon | 20 | 98.7 | 0.01 | 4.77 | 4 |  | - |  | 0.65 |  |  | 298 |  | Pure CO2 |  | Physical |  | 1 | (Shahrom et al., 2019) |
| [DMEDAH][acetate]@ activated carbon | 20 | 21.6 | 0.35 | 633.88 | 4 |  | - |  | 0.87 |  |  | 298 |  | Pure CO2 |  | Physical |  | 1 | (Shahrom et al., 2019) |
| [DMEDAH][propanoate]@ activated carbon | 20 | 20.5 | 0.36 | 681.95 | 4 |  | - |  | 1.06 |  |  | 298 |  | Pure CO2 |  | Physical |  | 1 | (Shahrom et al., 2019) |
| [VBTMA][Gly]@ activated carbon | 20 | 24.4 | 0.077 | 124.5 | 4 |  | - |  | 1.51 |  |  | 298 |  | Pure CO2 |  | Physical |  | 1 | (Shahrom et al., 2019) |
| [VBTMA][Arg]@ activated carbon | 20 | 23.8 | 0.10 | 172.53 | 4 |  | - |  | 0.96 |  |  | 298 |  | Pure CO2 |  | Physical |  | 1 | (Shahrom et al., 2019) |
| [VBTMA][Lys]@ activated carbon | 20 | 22.4 | 0.102 | 172.53 | 4 |  | - |  | 0.91 |  |  | 298 |  | Pure CO2 |  | Physical |  | 1 | (Shahrom et al., 2019) |
| [HMIM][BF4]@ F600-900 | - | <50 | 0.36 | 961 | 5 |  | - |  | 0.44 |  |  | 303 |  | 15% vol. CO2 85% N2 |  | - |  | 1 | (Erto et al., 2015) |
| [EMIM][Gly]@F600-900 | - | <50 | 0.36 | 971 | 5 |  | - |  | 0.50 |  |  | 303 |  | 15% vol. CO2 85% N2 |  | - |  | 1 | (Erto et al., 2015) |
| [HMIM][BF4]@RGC30 | - | <50 | 0.46 | 1318 | 5 |  | - |  | 0.39 |  |  | 303 |  | 15% vol. CO2 85% N2 |  | - |  | 1 | (Erto et al., 2015) |
| [EMIM][Gly]@RGC30 | - | <50 | 0.46 | 1307 | 5 |  | - |  | 0.43 |  |  | 303 |  | 15% vol. CO2 85% N2 |  | - |  | 1 | (Erto et al., 2015) |
| [ChCl2.mZnCl2]@activated carbon | 1 | 19.32 | 0.39 | 804 | 6 |  | - |  | 1.92 |  |  | 303 |  | 60% vol. CO2 40% H2 |  | - |  | 1 | (Yusuf et al., 2019) |
| 1,3-bis(cyanmethyl)imidazolium chlorine@carbon, | - | <50 | 0.28 | 390 | - |  | - |  | 2.02 |  |  | 298 |  | Pure CO2 |  | - |  | 1 | (Cui et al., 2017) |
| 1-ethyl-3-methylimidazolium tricyanomethanide@carbon | - | <50 | 0.35 | 506 | - |  | - |  | 2.29 |  |  | 298 |  | Pure CO2 |  | - |  | 1 | (Cui et al., 2017) |
| 1-ethyl-3-methylimidazolium dicyanamide@carbon | - | <50 | 0.50 | 600 | - |  | - |  | 2.21 |  |  | 298 |  | Pure CO2 |  | - |  | 1 | (Cui et al., 2017) |
| 1-ethyl-3-methylimidazolium thiocyanate@carbon | - | <50 | 0.59 | 646 | - |  | - |  | 2.11 |  |  | 298 |  | Pure CO2 |  | - |  | 1 | (Cui et al., 2017) |
| ZIF |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [TMGHIM]@ZIF-8 | 30 | <100 | 0.267 | 698.02 | 6 |  | - |  | 0.52 |  |  | 298 |  | - |  | Physical |  | 1 | (Hussain et al., 2024) |
| [TMGHPhO]@ZIF-8 | 30 | <100 | 0.580 | 1576.64 | - |  | - |  | 0.48 |  |  | 298 |  | - |  | Physical |  | 1 | (Hussain et al., 2024) |
| [C6MIM][B(CN)4]@ZIF-8 | 15 | - | - | - | - |  | - |  | 1.8 |  |  | 303 |  | Pure CO2 |  | Physical/ chemical |  | 0.5 | (Esteves et al., 2023) |
| [N2114][Ac]@ZIF-8 | 7.8 | - | 0.535 | 1457 | - |  | - |  | 0.56 |  |  | 304 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2023) |
| [BMIM][SCN]@ZIF-8 | ~25 | - | 0.027 | 60.56 | - |  | - |  | 0.33 |  |  | 298 |  | Pure CO2 |  | - |  | 1 | (Zeeshan, Keskin, et al., 2018) |
| [BMIM][Ac]@ZIF-8 | 30 | 43.5 | 0.15 | 266.2 | 10 |  | - |  | 0.98 |  |  | 303.15 |  | - |  | Chemical |  | 1 | (Mohamedali et al., 2018) |
| [HEMIM][DCA]@ZIF-8 | 40 | - | 0.0015 | 4.53 | 2 |  | - |  | 0.55 wt.% to ZIF-8 |  |  | 298 |  | - |  | - |  | 1 | (Zeeshan, Nozari, et al., 2018) |
| [BMIM][BF4]@ZIF-8 | 20 | - | 0.318 | 725 | - |  | - |  | 0.61 |  |  | 298 |  | - |  | Physical |  | 1 | (Koyuturk et al., 2017) |
| 1-(3-Aminopropyl)-3-(2-bromoethyl) imidazole (NAIm-Br)@ZIF-67 | - | 15.3 | 0.65 | 1707 | - |  | - |  | 1.02 |  |  | 298 |  | Pure CO2 |  | Physical |  | 1.07 | (X. Song et al., 2019) |
| 1-ethyl-3-methylimidazolium bis(-trifluoromethyl) sulfonylimide ([C2MIM][NTf2])@ZIF-8, | 9.3 mol% | <16 | 0.471 | 1184 | - |  | - |  | 0.43 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| 1-(2-hydroxyethyl)-3-methylimidazolium bis(trifluoromethyl)sulfonylimide ([C2OHMIM][NTf2])@ZIF-8 | 9.3 mol% | - | 0.489 | 1215 | - |  | - |  | 0.41 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| 1-hexyl-3-methylimidazolium bis(-trifluoromethyl) sulfonylimide ([C6MIM][NTf2])@ZIF-8 | 9.3 mol% | - | 0.501 | 1245 | - |  | - |  | 0.40 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| 1-benzyl-3-methylimidazolium bis(trifluoromethyl) sulfonylimide ([BzMIM][NTf2])@ZIF-8 | 9.3 mol% | - | 0.481 | 1226 | - |  | - |  | 0.39 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| 1-decyl-3-methylimidazolium bis(-trifluoromethyl) sulfonylimide ([C10MIM][NTf2])@ZIF-8 | 9.3 mol% | - | 0.515 | 1283 | - |  | - |  | 0.45 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| trihexyl(tetradecyl)phosphonium bis(trifluoromethyl) sulfonylimide ([P66614][NTf2])@ZIF-8 | 9.3 mol% | - | 0.637 | 1778 | - |  | - |  | 0.41 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| 1-hexyl-3-methylimidazolium dicyanamide ([C6MIM][N(CN)2])@ZIF-8 | 9.3 mol% |  | 0.485 | 1265 | - |  | - |  | 0.43 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| 1-hexyl-3-methylimidazolium tricyanomethanide ([C6MIM][C(CN)3])@ZIF-8 | 9.3 mol% |  | 0.473 | 1222 | - |  | - |  | 0.45 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| 1-hexyl-3-methylimidazolium Chloride ([C6MIM][Cl])@ZIF-8 | 9.3 mol% |  | 0.496 | 1319 | - |  | - |  | 0.43 |  |  | 303 |  | Pure CO2 |  | Physical |  | 1 | (Ferreira et al., 2019) |
| 1-ethyl-3-methylimidazolium acetate ([C2MIM][Ac])@ZIF-8 | 9.3 mol% |  | 0.606 | 1638 | - |  | - |  | 0.57 |  |  | 303 |  | Pure CO2 |  | Chemical |  | 1 | (Ferreira et al., 2019) |
| [C4MIM]2[NiCl4]@ZIF-8 | 9.3 mol% | <16 | 0.296 | 768 | - |  | - |  | ~0.47 |  |  | 303 |  | Pure CO2 |  | - |  | 1 | (Ferreira et al., 2020) |
| [C4MIM]2[MnCl4]@ZIF-8 | 9.3 mol% | <16 | 0.210 | 551 | - |  | - |  | ~0.38 |  |  | 303 |  | Pure CO2 |  | - |  | 1 | (Ferreira et al., 2020) |
| [C4MIM]2[CoCl4]@ZIF-8 | 9.3 mol% | <16 | 0.242 | 643 | - |  | - |  | ~0.5 |  |  | 303 |  | Pure CO2 |  | - |  | 1 | (Ferreira et al., 2020) |
| [C4MIM]2[Co(NCS)4]@ZIF-8 | 9.3 mol% | <16 | 0.278 | 731 | - |  | - |  | ~0.38 |  |  | 303 |  | Pure CO2 |  | - |  | 1 | (Ferreira et al., 2020) |
| [C4MIM][FeCl4]@ZIF-8 | 9.3 mol% | <16 | 0.237 | 639 | - |  | - |  | ~0.46 |  |  | 303 |  | Pure CO2 |  | - |  | 1 | (Ferreira et al., 2020) |
| [BMIM][PF6]@ZIF-8 | 24 | - | 0.22 | 415 | - |  | - |  | ~0.41 |  |  | 298 |  | Pure CO2 |  | Physical |  | 1 | (Kinik et al., 2016) |
| [EMIM][Gly]@ZIF-8 | 30 | <11 | 0.24 | 634 | 6 |  |  |  | ~1.2 |  |  | 313 |  | CO2/N2 |  | Physical/ chemical |  | 1 | (Philip & Henni, 2022) |
| [EMIM][Ala]@ZIF-8 | 30 | <11 | 0.26 | 718 | 6 |  |  |  | ~1.18 |  |  | 313 |  | CO2/N2 |  | Physical/ chemical |  | 1 | (Philip & Henni, 2022) |
| Zeolite |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [BMIM][ARG]@Na-Y | 10 | - | - | - | - |  | - |  | 1.08 |  |  | 298 |  | Pure CO2 |  | Physical/ chemical |  | 1 | (Sistla & Khanna, 2022) |
| [BMIM][VAL]@Na-Y | 15 | - | 0.19 | 349 | - |  | - |  | 1.76 |  |  | 298 |  | Pure CO2 |  | Physical/ chemical |  | 1.2 | (Sistla & Khanna, 2022) |
| [BMIM][MET]@Na-Y | 15 | - | - | - | - |  | - |  | 1.78 |  |  | 298 |  | Pure CO2 |  | Physical/ chemical |  | 1.09 | (Sistla & Khanna, 2022) |
| [BMIM][HIS]@Na-Y | 20 | - | 0.27 | 435 | - |  | - |  | 1.70 |  |  | 298 |  | Pure CO2 |  | Physical/ chemical |  | 1.3 | (Sistla & Khanna, 2022) |
| [BMIM][LEU]@Na-Y | 33 | - | 0.004 | 0.03 | - |  | - |  | 0.66 |  |  | 298 |  | Pure CO2 |  | Physical/ chemical |  | 1.66 | (Sistla & Khanna, 2022) |
| [BMIM][Ac]@SAPO-34 | 2.84 | <10 | 0.025 | 8.6 | 6 |  | 2.13 |  | 1.88 |  |  | 303 |  | 50% CO2 50% N2 |  | Physical/ chemical |  | 1 | (Ye et al., 2024) |
| [P4444][3-aminopyrazole]@NaY | 50 | - | - | - | - |  | - |  | 0.75 |  |  | 393 |  | Pure CO2 |  | Chemical |  | 1 | (Mi et al., 2014) |
| [APMIM]Br@NaY | 0.5 molar ratio | - | - | 456 | 10 |  | - |  | 4.94 |  |  | 273 |  | Pure CO2 |  | Physical/ chemical |  | 1 | (Yu, Mai, Wang, et al., 2014) |
| [C4MIM]Br@NaY | 18.5 | - | - | - | 6 |  | - |  | 0.83 |  |  | 308 |  | 14.9 vol% CO2 85.1% He |  | - |  | - | (Yu, Mai, Huang, et al., 2014) |
| [C6MIM]Br@NaY | 22.5 | - | - | - | 6 |  | - |  | 0.73 |  |  | 308 |  | 14.9 vol% CO2 85.1% He |  | - |  | - | (Yu, Mai, Huang, et al., 2014) |
| [C8MIM]Br@NaY | 17.6 | - | - | - | 6 |  | - |  | 0.68 |  |  | 308 |  | 14.9 vol% CO2 85.1% He |  | - |  | - | (Yu, Mai, Huang, et al., 2014) |
| [C10MIM]Br@NaY | 11.4 | - | - | - | 6 |  | - |  | 0.59 |  |  | 308 |  | 14.9 vol% CO2 85.1% He |  | - |  | - | (Yu, Mai, Huang, et al., 2014) |
| MOF |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Imidazolium-based poly(ionic liquid) synthesized from 1-Vinyl-3-ethylimidazolium Bromide@MIL-101 | - | <30 | 1.26 | 2462 | - |  | - |  | ~2.45 |  |  | 298 |  | - |  | - | ~1.1 |  | (Ding & Jiang, 2018) |
| [BMIM][AC]@ HKUST-1 | 5-20 (5 was the optimum) | 20.5, 20.4 | 0.52, 0.79 | 1017.8, 1557.8 | 10 |  | - |  | [BMIM][AC]@HKUST-1 ~1.7 (0.15 bar) ~4.4 (1 bar) |  |  | 303 |  | - |  | Chemical/ physical | 0.1 1 |  | (Mohamedali et al., 2019b) |
| [EMIM][Ac]@MOF-177 | - | <300 | 0.09 | 78.2 | 10 |  | - |  | ~1.14 |  |  | 303 |  | - |  | - | 1 |  | (Mohamedali et al., 2019a) |
| 1-carboxyethyl-3-methylimidazolium chloride@MIL-101-NO2, 1-carboxyethyl-3-methylimidazolium chloride@MIL-101-NH2 | - | <25 | 1.01, 0.96 | 1176, 1035 | 5 |  | - |  | ~1.9, ~7 |  |  | 298 |  | - |  | Chemical | 1 |  | (Wang et al., 2018) |
| [BMIM][MeSO4]@MIL-53(Al) | 26 | - | Immeasurable | 47.2 | 6 |  | - |  | 0.74 |  |  | 298 |  | - |  | - | 1 |  | (Kulak et al., 2019) |
| [BMIM][PF6]@CuBTC, [BMMIM][PF6]@CuBTC | 30 | <100 | 0.186, 0.143 | 364, 306 | - |  | - |  | ~2.13, ~1.96 |  |  | 298 |  | - |  | - | 1 |  | (Nozari et al., 2018) |
| [DETA][Cl]@MIL-101(Cr), [DETA][Ac]@MIL-101 (Cr), [DETA][Ac]Imp@MIL-101 (Cr) (Synthesized by direct impregnation of DETA-AC) | - | <30 | 0.81, 0.76, 0.67 | 1344, 1259, 1101 | 6 |  | - |  | 2.3460, 2.4595, ~2 |  |  | 298 |  | 15% CO2 85% N2 |  | Physical | 1 |  | (Chen et al., 2018) |
| 1- methylacetamido-3-methylimidazolium bromide@UiO-66-NH2, 1-methylacetamido-3-methylbenzimidazolium bromide@UiO-66-NH2 | - | - | 0.29, 0.17 | 304, 237 | - |  | - |  | 0.82, 0.69 |  |  | 298 |  | - |  | - | ~1.1 |  | (Kurisingal et al., 2019) |
| [BMIM][BF4]@MIL-53(Al) | 25.8 | - | 0.043 | 28.26 | - |  | - |  | ~0.82 |  |  | 298 |  | Pure CO2 |  | Physical | 1 |  | (Kavak et al., 2019) |
| [BMIM][PF6]@MIL-53(Al) | 25.4 | - | 0.059 | 39.59 | - |  | - |  | ~0.82 |  |  | 298 |  | Pure CO2 |  | Physical | 1 |  | (Kavak et al., 2019) |
| [BMIM][CF3SO3]@MIL-53(Al) | 25.8 | - | 0.070 | 44.64 | - |  | - |  | ~0.65 |  |  | 298 |  | Pure CO2 |  | Physical | 1 |  | (Kavak et al., 2019) |
| [BMIM][SbF6]@MIL-53(Al) | 26 | - | 0.067 | 43.42 | - |  | - |  | ~0.82 |  |  | 298 |  | Pure CO2 |  | Physical | 1 |  | (Kavak et al., 2019) |
| [BMIM][NTf2]@MIL-53(Al) | 24.1 | - | 0.078 | 51.45 | - |  | - |  | ~0.74 |  |  | 298 |  | Pure CO2 |  | Physical | 1 |  | (Kavak et al., 2019) |
| [BMIM][BF4]@ CuBTC | 5-30 (5 was the highest uptake) | - | - | 1229.1 ± 37.7 | - |  | - |  | ~11.45 |  |  | 298 |  | Pure CO2 |  | - | 30 |  | (Sezginel et al., 2016) |
| IL@UiO-67 | - | <15 | 0.43 | 846 | 5 |  | - |  | 2.12, 0.92 |  |  | 273, 298 |  | - |  | Physical | 1 |  | (Ding et al., 2017) |
| [BMIM][PF6]@Cu-BTC | 5 | - | 0.65 | 1205 | - |  | - |  | ~4.5 |  |  | 298 |  | Pure CO2 |  | - | 1 |  | (Silva et al., 2015) |
| [BMIM][TF2N]@Cu-BTC | 5 | - | 0.67 | 1311 | - |  | - |  | ~3.8 |  |  | 298 |  | Pure CO2 |  | - | 1 |  | (Silva et al., 2015) |
| Graphene |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| [BMPyr][DCA]@rGA300 | - | ~500 | 0.031 | 2.9 | - |  | 0.13 mol/mol |  | 0.082 |  |  | 298 |  | Pure CO2 |  | - | 1 |  | (Caglayan et al., 2023) |
| [BMPyr][PF6]@rGA300 | - | ~500 | 0.026 | 5.7 | - |  | 0.9 mol/mol |  | 0.12 |  |  | 298 |  | Pure CO2 |  | - | 1 |  | (Caglayan et al., 2023) |
| [BMPyr][DCA]@rGA500 | - | ~700 | 0.052 | 5.5 | - |  | 0.13 mol/mol |  | 0.2 |  |  | 298 |  | Pure CO2 |  | - | 1 |  | (Caglayan et al., 2023) |
| [BMPy[PF6]@rGA500 | - | ~500 | 0.034 | 5.5 | - |  | 0.9 mol/mol |  | 0.2 |  |  | 298 |  | Pure CO2 |  | - | 1 |  | (Caglayan et al., 2023) |
| [P4444][3-aminopyrazole]@GO | 50 | - | - | - | - |  | - |  | 0.39 |  |  | 393 |  | Pure CO2 |  | Chemical | 1 |  | (Mi et al., 2014) |
| P[MATMA][BF4]@GO | - | - | - | 18.84 | - |  | - |  | 0.71 |  |  | 298 |  | - |  | - | 1 |  | (Huang et al., 2017) |
| [BMIM][PF6]@reduced GO | 5 | 20-100 | - | 447 | 10 |  | - |  | 0.7 |  |  | 298 |  | - |  | - | 1 |  | (Zeeshan et al., 2021) |
| [P66614][Triz]@graphene nanoplatelet, [P66614][Triz]@reduced GO | 20 | - | - | 1.06, 5.45 | 10 |  | 1.32 |  | 1.45, ~1.39 |  |  | 293 |  | - |  | Chemical | 1 |  | (Li et al., 2018) |
| [DAMT][BF4]@graphene (HEG) | ~50 | - | - | - | - |  | 0.045 |  | 0.56 |  |  | 298 |  | Pure CO2 |  | Physical | 1 |  | (Tamilarasan & Ramaprabhu, 2016) |
| Other |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ILs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P[DADMA][OAc]@chitosan aerogel | 30 | 154 | 1.83 | 398 | - |  | - |  | 0.62 |  |  | 298 |  | Pure CO2 |  | Chemical | 1 |  | (Barrulas et al., 2021) |
| Glut:P[DADMA]Cl@chitosan aerogel | 0.3 & 15 | 142 | 1.47 | 344 | - |  | - |  | 0.76 |  |  | 298 |  | Pure CO2 |  | Chemical | 1 |  | (Barrulas et al., 2021) |
| [BMIM][Ac]@carbon fibers | 100 | - | 0.003 | 2 | 3 |  | 2.3 |  | 1.29 |  |  | 298 |  | Pure CO2 |  | Chemical | 1 |  | (Isaacs-Páez et al., 2022) |
| 1-aminoethyl-3-vinylimidazolium bromide hydrobromide@titanate nanotubes | - | 169 | 0.43 | 102.3 | 5 |  | - |  | 2.46 |  |  | 298 |  | - |  | Chemical/ physical | 0.2 |  | (Yuan et al., 2017) |
| Benzimidazole-based hyper-cross-linked poly(ionic liquid) | - | 5, 10, 15 | 0.77 | 780 | 5 |  | - |  | 3.25, 1.48 |  |  | 273, 298 |  | - |  | - | 1 |  | (Sang & Huang, 2020) |

References

Aboudi, J., & Vafaeezadeh, M. (2015). Efficient and reversible CO2 capture by amine functionalized-silica gel confined task-specific ionic liquid system. Journal of Advanced Research, 6(4), 571-577.

Aquino, A., Bernard, F., Borges, J., Mafra, L., Dalla Vecchia, F., Vieira, M., Ligabue, R., Seferin, M., Chaban, V. V., & Cabrita, E. (2015). Rationalizing the role of the anion in CO 2 capture and conversion using imidazolium-based ionic liquid modified mesoporous silica. RSC advances, 5(79), 64220-64227.

Arellano, I. H., Huang, J., & Pendleton, P. (2015a). High capacity CO 2 sorbents based on zinc-functionalized ionic liquid confined in morphologically diverse porous matrices. RSC Advances, 5(80), 65074-65083.

Arellano, I. H., Huang, J., & Pendleton, P. (2015b). Synergistic enhancement of CO2 uptake in highly ordered mesoporous silica-supported zinc-functionalized ionic liquid sorbents. Chemical Engineering Journal, 281, 119-125.

Arellano, I. H., Madani, S. H., Huang, J., & Pendleton, P. (2016). Carbon dioxide adsorption by zinc-functionalized ionic liquid impregnated into bio-templated mesoporous silica beads. Chemical Engineering Journal, 283, 692-702.

Ariyanto, T., Masruroh, K., Pambayun, G. Y. S., Mukti, N. I. F., Cahyono, R. B., Prasetya, A., & Prasetyo, I. (2021). Improving the separation of CO2/CH4 using impregnation of deep eutectic solvents on porous Carbon. ACS omega, 6(29), 19194-19201.

Balsamo, M., Erto, A., Lancia, A., Totarella, G., Montagnaro, F., & Turco, R. (2018). Post-combustion CO2 capture: On the potentiality of amino acid ionic liquid as modifying agent of mesoporous solids. Fuel, 218, 155-161.

Barrulas, R. V., López-Iglesias, C., Zanatta, M., Casimiro, T., Mármol, G., Carrott, M. R., García-González, C. A., & Corvo, M. C. (2021). The AEROPILs generation: novel poly (ionic liquid)-based aerogels for CO2 capture. International Journal of Molecular Sciences, 23(1), 200.

Caglayan, H. P., Unal, U., Keskin, S., & Uzun, A. (2023). Effect of Surface Characteristics of Graphene Aerogels and Hydrophilicity of Ionic Liquids on the CO2/CH4 Separation Performance of Ionic Liquid/Reduced Graphene Aerogel Composites. ACS Applied Nano Materials, 6(3), 2203-2217.

Chen, C., Feng, N., Guo, Q., Li, Z., Li, X., Ding, J., Wang, L., Wan, H., & Guan, G. (2018). Surface engineering of a chromium metal-organic framework with bifunctional ionic liquids for selective CO2 adsorption: Synergistic effect between multiple active sites. Journal of colloid and interface science, 521, 91-101.

Cheng, H., Wang, P., Luo, J., Fransaer, J., De Vos, D. E., & Luo, Z.-H. (2015). Poly (ionic liquid)-based nanocomposites and their performance in CO2 capture. Industrial & Engineering Chemistry Research, 54(12), 3107-3115.

Cheng, J., Li, Y., Hu, L., Liu, J., Zhou, J., & Cen, K. (2018). CO2 absorption and diffusion in ionic liquid [P66614][Triz] modified molecular sieves SBA-15 with various pore lengths. Fuel Processing Technology, 172, 216-224.

Cheng, J., Li, Y., Hu, L., Zhou, J., & Cen, K. (2016). CO2 adsorption performance of ionic liquid [P66614][2-Op] loaded onto molecular sieve MCM-41 compared to pure ionic liquid in biohythane/pure CO2 atmospheres. Energy & Fuels, 30(4), 3251-3256.

Cui, X., Yang, Q., Xiong, Y., Bao, Z., Xing, H., & Dai, S. (2017). Preparation of ordered N-doped mesoporous carbon materials via a polymer–ionic liquid assembly. Chemical Communications, 53(36), 4915-4918.

Ding, L.-G., Yao, B.-J., Jiang, W.-L., Li, J.-T., Fu, Q.-J., Li, Y.-A., Liu, Z.-H., Ma, J.-P., & Dong, Y.-B. (2017). Bifunctional imidazolium-based ionic liquid decorated UiO-67 type MOF for selective CO2 adsorption and catalytic property for CO2 cycloaddition with epoxides. Inorganic chemistry, 56(4), 2337-2344.

Ding, M., & Jiang, H.-L. (2018). Incorporation of imidazolium-based poly (ionic liquid) s into a metal–organic framework for CO2 capture and conversion. ACS Catalysis, 8(4), 3194-3201.

Dos Santos, L. M., Bernard, F. L., Polesso, B. B., Pinto, I. S., Frankenberg, C. C., Corvo, M. C., Almeida, P. L., Cabrita, E., & Einloft, S. (2020). Designing silica xerogels containing RTIL for CO2 capture and CO2/CH4 separation: Influence of ILs anion, cation and cation side alkyl chain length and ramification. Journal of Environmental Management, 268, 110340.

Duarte, E., Bernard, F., Dos Santos, L. M., Polesso, B. B., Duczinski, R., Forneck, V., Geshev, J., & Einloft, S. (2024). CO2 capture using silica-immobilized dicationic ionic liquids with magnetic and non-magnetic properties. Heliyon, 10(8).

Duczinski, R., Bernard, F., Rojas, M., Duarte, E., Chaban, V., Dalla Vecchia, F., Menezes, S., & Einloft, S. (2018). Waste derived MCMRH-supported IL for CO2/CH4 separation. Journal of Natural Gas Science and Engineering, 54, 54-64.

Duczinski, R., Polesso, B. B., Bernard, F. L., Ferrari, H. Z., Almeida, P. L., Corvo, M. C., Cabrita, E. J., Menezes, S., & Einloft, S. (2020). Enhancement of CO2/N2 selectivity and CO2 uptake by tuning concentration and chemical structure of imidazolium-based ILs immobilized in mesoporous silica. Journal of Environmental Chemical Engineering, 8(3), 103740.

Erto, A., Silvestre-Albero, A., Silvestre-Albero, J., Rodríguez-Reinoso, F., Balsamo, M., Lancia, A., & Montagnaro, F. (2015). Carbon-supported ionic liquids as innovative adsorbents for CO2 separation from synthetic flue-gas. Journal of colloid and interface science, 448, 41-50.

Esteves, L., Ferreira, T., Keba, A., Esperança, J., & Esteves, I. (2023). Carbon materials derived from cyano-based IL@ ZIF-8 composites for CO2 sorption separation systems. Materials Today Sustainability, 22, 100353.

Ferreira, T. J., de Moura, B. A., Esteves, L. M., Reis, P. M., Esperança, J. M., & Esteves, I. A. (2023). Biocompatible ammonium-based ionic liquids/ZIF-8 composites for CO2/CH4 and CO2/N2 separations. Sustainable Materials and Technologies, 35, e00558.

Ferreira, T. J., Ribeiro, R. P., Mota, J. P., Rebelo, L. P., Esperanca, J. M., & Esteves, I. A. (2019). Ionic liquid-impregnated metal–organic frameworks for CO2/CH4 separation. ACS Applied Nano Materials, 2(12), 7933-7950.

Ferreira, T. J., Vera, A. T., De Moura, B. A., Esteves, L. M., Tariq, M., Esperança, J. M., & Esteves, I. A. (2020). Paramagnetic Ionic Liquid/Metal Organic Framework Composites for CO2/CH4 and CO2/N2 Separations. Frontiers in chemistry, 8.

Foorginezhad, S., & Ji, X. (2024). Developing slurry based on immobilized and aqueous [MEACl][EDA] for CO2 capture. Chemical Engineering Journal, 156176.

Gargiulo, V., Alfè, M., Ammendola, P., Raganati, F., & Chirone, R. (2016). CO2 sorption on surface-modified carbonaceous support: Probing the influence of the carbon black microporosity and surface polarity. Applied Surface Science, 360, 329-337.

Garip, M., & Gizli, N. (2020). Ionic liquid containing amine-based silica aerogels for CO2 capture by fixed bed adsorption. Journal of Molecular Liquids, 310, 113227.

Ghazali, Z., Hassan, N. H., Yarmo, M. A., Peng, T. L., & Othaman, R. (2019). Immobilization of choline chloride: Urea onto mesoporous silica for carbon dioxide capture. Sains Malaysiana, 48(5), 1025-1033.

Ghazali, Z., Yarmo, M. A., Hassan, N. H., Teh, L. P., & Othaman, R. (2020). New green adsorbent for capturing carbon dioxide by choline chloride: urea-confined nanoporous silica. Arabian Journal for Science and Engineering, 45, 4621-4634.

Ghazali, Z., Yarmo, M. A., & Othaman, R. (2019). Confinement and characterization of deep eutectic solvent based on choline chloride: alcohol into nanoporous silica for CO2 capture. AIP Conference Proceedings,

Hiremath, V., Jadhav, A. H., Lee, H., Kwon, S., & Seo, J. G. (2016). Highly reversible CO2 capture using amino acid functionalized ionic liquids immobilized on mesoporous silica. Chemical Engineering Journal, 287, 602-617.

Huang, L., Jin, Y., Sun, L., Chen, F., Fan, P., Zhong, M., & Yang, J. (2017). Graphene oxide functionalized by poly (ionic liquid) s for carbon dioxide capture. Journal of Applied Polymer Science, 134(11).

Huang, Z., Karami, D., & Mahinpey, N. (2021). Study on the efficiency of multiple amino groups in ionic liquids on their sorbents performance for low-temperature CO2 capture. Chemical Engineering Research and Design, 167, 198-206.

Hussain, S., Dong, H., Duan, H., Ji, X., Asif, H. M., Liu, W., & Zhang, X. (2024). Efficient Selective Carbon Dioxide Separation via Task-Specific Ionic Liquids Incorporated in ZIF-8. Langmuir, 40(16), 8636-8644.

Isaacs-Páez, E., García-Pérez, A., Nieto-Delgado, C., Chazaro-Ruiz, L. F., & Rangel-Mendez, J. (2022). Enhanced CO2 capture kinetics by using macroporous carbonized natural fibers impregnated with an ionic liquid. Journal of Molecular Liquids, 350, 118602.

Kavak, S., Polat, H. M., Kulak, H., Keskin, S., & Uzun, A. (2019). MIL‐53 (Al) as a Versatile Platform for Ionic‐Liquid/MOF Composites to Enhance CO2 Selectivity over CH4 and N2. Chemistry–An Asian Journal, 14(20), 3655-3667.

Kinik, F. P., Altintas, C., Balci, V., Koyuturk, B., Uzun, A., & Keskin, S. (2016). [BMIM][PF6] incorporation doubles CO2 selectivity of ZIF-8: elucidation of interactions and their consequences on performance. ACS applied materials & interfaces, 8(45), 30992-31005.

Kolding, H., Fehrmann, R., & Riisager, A. (2012). CO2 Capture technologies: Current status and new directions using supported ionic liquid phase (SILP) absorbers. Science China Chemistry, 55(8), 1648-1656.

Koyuturk, B., Altintas, C., Kinik, F. P., Keskin, S., & Uzun, A. (2017). Improving gas separation performance of ZIF-8 by [BMIM][BF4] incorporation: interactions and their consequences on performance. The Journal of Physical Chemistry C, 121(19), 10370-10381.

Kulak, H., Polat, H. M., Kavak, S., Keskin, S., & Uzun, A. (2019). Improving CO2 Separation Performance of MIL‐53 (Al) by Incorporating 1‐n‐Butyl‐3‐Methylimidazolium Methyl Sulfate. Energy Technology, 7(7), 1900157.

Kurisingal, J. F., Rachuri, Y., Pillai, R. S., Gu, Y., Choe, Y., & Park, D.-W. (2019). Ionic-liquid-functionalized UiO-66 framework: an experimental and theoretical study on the cycloaddition of CO2 and epoxides. ChemSusChem, 12(5), 1033-1042.

Li, Y., Cheng, J., Hu, L., Liu, J., Zhou, J., & Cen, K. (2018). Graphene nanoplatelet and reduced graphene oxide functionalized by ionic liquid for CO2 capture. Energy & Fuels, 32(6), 6918-6925.

Liu, F., Huang, K., & Jiang, L. (2018). Promoted adsorption of CO2 on amine‐impregnated adsorbents by functionalized ionic liquids. AIChE Journal, 64(10), 3671-3680.

Liu, S.-H., & Sie, W.-H. (2016). CO 2 Capture on Mesocellular Silica Foam Supported Amino Acid-Functionalized Ionic Liquids. Water, Air, & Soil Pollution, 227, 1-8.

MacQueen, P. M., Bach, R. A., MacLean, C. T., & MacQuarrie, S. L. (2014). Effective one-step synthesis of silica supported 1, 3-dibutylimidazolium acetate for carbon dioxide capture. The Journal of Physical Chemistry C, 118(10), 5239-5242.

Marliza, T., Yarmo, M., Lahuri, A., & Taufiq-Yap, Y. (2022). CO2 capture using ionic liquid hybrid sorbent: Physical and chemical adsorption-desorption study. Materials Today: Proceedings, 64, 20-26.

Marliza, T. S., Yarmo, M. A., Hakim, A., Abu Tahari, M. N., & Taufiq-Yap, Y. H. (2017). Characterizations and application of supported ionic liquid [bmim][CF3SO3]/SiO2 in CO2 capture. Materials Science Forum,

Mi, W. M., Yue, Z. H., Yan, L. Y., Jing, M., Shuai, L., & Hua, Z. J. (2014). Novel CO2-Capture Derived from the Basic Ionic Liquids Orientated on Mesoporous Materials.

Mirzaei, M., Badiei, A. R., Mokhtarani, B., & Sharifi, A. (2017). Experimental study on CO2 sorption capacity of the neat and porous silica supported ionic liquids and the effect of water content of flue gas. Journal of Molecular Liquids, 232, 462-470.

Mirzaei, M., Hekmat Shoar, S., Sharifi, A., & Abaee, M. S. (2024). CO2 and N2 adsorption performance of [Rmim][NO3] ionic liquids impregnated onto mesoporous silica at ambient pressure. Journal of Porous Materials, 31(1), 165-175.

Mirzaei, M., Mokhtarani, B., Badiei, A., & Sharifi, A. (2018). Improving Physical Adsorption of CO2 by Ionic Liquids‐Loaded Mesoporous Silica. Chemical Engineering & Technology, 41(7), 1272-1281.

Mohamedali, M., Henni, A., & Ibrahim, H. (2019a). Investigation of CO 2 capture using acetate-based ionic liquids incorporated into exceptionally porous metal–organic frameworks. Adsorption, 25(4), 675-692.

Mohamedali, M., Henni, A., & Ibrahim, H. (2019b). Markedly improved CO2 uptake using imidazolium-based ionic liquids confined into HKUST-1 frameworks. Microporous and Mesoporous Materials, 284, 98-110.

Mohamedali, M., Ibrahim, H., & Henni, A. (2018). Incorporation of acetate-based ionic liquids into a zeolitic imidazolate framework (ZIF-8) as efficient sorbents for carbon dioxide capture. Chemical Engineering Journal, 334, 817-828.

Mohamedali, M., Ibrahim, H., & Henni, A. (2020). Imidazolium based ionic liquids confined into mesoporous silica MCM-41 and SBA-15 for carbon dioxide capture. Microporous and Mesoporous Materials, 294, 109916.

Nkinahamira, F., Su, T., Xie, Y., Ma, G., Wang, H., & Li, J. (2017). High pressure adsorption of CO2 on MCM-41 grafted with quaternary ammonium ionic liquids. Chemical Engineering Journal, 326, 831-838.

Nozari, V., Zeeshan, M., Keskin, S., & Uzun, A. (2018). Effect of methylation of ionic liquids on the gas separation performance of ionic liquid/metal–organic framework composites. CrystEngComm, 20(44), 7137-7143.

Peng, H., Zhou, Y., Liu, J., Zhang, H., Xia, C., & Zhou, X. (2013). Synthesis of novel amino-functionalized ionic liquids and their application in carbon dioxide capture. RSC Advances, 3(19), 6859-6864.

Philip, F. A., & Henni, A. (2022). Enhancement of post-combustion CO2 capture capacity by incorporation of task-specific ionic liquid into ZIF-8. Microporous and Mesoporous Materials, 330, 111580.

Polesso, B. B., Bernard, F. L., Ferrari, H. Z., Duarte, E. A., Dalla Vecchia, F., & Einloft, S. (2019). Supported ionic liquids as highly efficient and low-cost material for CO2/CH4 separation process. Heliyon, 5(7), e02183.

Polesso, B. B., Duczinski, R., Bernard, F. L., Ferrari, H. Z., Luz, M. d., Vecchia, F. D., Menezes, S. M. C. d., & Einloft, S. (2019). Imidazolium-based ionic liquids impregnated in silica and alumina supports for CO 2 capture. Materials Research, 22.

Ren, J., Li, Z., Chen, Y., Yang, Z., & Lu, X. (2018). Supported ionic liquid sorbents for CO2 capture from simulated flue-gas. Chinese Journal of Chemical Engineering, 26(11), 2377-2384.

Ren, J., Wu, L., & Li, B.-G. (2012). Preparation and CO2 sorption/desorption of N-(3-aminopropyl) aminoethyl tributylphosphonium amino acid salt ionic liquids supported into porous silica particles. Industrial & engineering chemistry research, 51(23), 7901-7909.

Rojas, M. F., Miranda, L. P., Ramirez, A. M., Quintero, K. P., Bernard, F., Einloft, S., & Díaz, L. A. C. (2017). New biocomposites based on castor oil polyurethane foams and ionic liquids for CO2 capture. Fluid Phase Equilibria, 452, 103-112.

Romanos, G., Vangeli, O., Stefanopoulos, K., Kouvelos, E., Papageorgiou, S., Favvas, E., & Kanellopoulos, N. (2009). Methods of evaluating pore morphology in hybrid organic–inorganic porous materials. Microporous and Mesoporous Materials, 120(1-2), 53-61.

Ruckart, K. N., O’Brien, R. A., Woodard, S. M., West, K. N., & Glover, T. G. (2015). Porous solids impregnated with task-specific ionic liquids as composite sorbents. The Journal of Physical Chemistry C, 119(35), 20681-20697.

S Aquino, A., O Vieira, M., Ferreira, A. S. D., Cabrita, E. J., Einloft, S., & O de Souza, M. (2019). Hybrid ionic liquid–silica xerogels applied in CO2 capture. Applied Sciences, 9(13), 2614.

Sang, Y., & Huang, J. (2020). Benzimidazole-based hyper-cross-linked poly (ionic liquid) s for efficient CO2 capture and conversion. Chemical Engineering Journal, 385, 123973.

Santiago, R., Lemus, J., Hospital-Benito, D., Moya, C., Bedia, J., Alonso-Morales, N., Rodriguez, J. J., & Palomar, J. (2019). CO2 capture by supported ionic liquid phase: highlighting the role of the particle size. ACS Sustainable Chemistry & Engineering, 7(15), 13089-13097.

Sezginel, K. B., Keskin, S., & Uzun, A. (2016). Tuning the gas separation performance of CuBTC by ionic liquid incorporation. Langmuir, 32(4), 1139-1147.

Shahrom, M. S. R., Nordin, A. R., & Wilfred, C. D. (2019). The improvement of activated carbon as CO2 adsorbent with supported amine functionalized ionic liquids. Journal of Environmental Chemical Engineering, 7(5), 103319.

Sheshkovas, A. Z., Veselovskaya, J. V., Rogov, V. A., & Kozlov, D. V. (2022). Thermochemical study of CO2 capture by mesoporous silica gel loaded with the amino acid ionic liquid 1-ethyl-3-methylimidazolium glycinate. Microporous and Mesoporous Materials, 341, 112113.

Silva, F. d., Magalhães, G., Jardim, E. d. O., Silvestre-Albero, J., Sepúlveda-Escribano, A., de Azevedo, D., & de Lucena, S. (2015). CO2 adsorption on ionic liquid—modified Cu-BTC: Experimental and simulation study. Adsorption Science & Technology, 33(2), 223-242.

Sistla, Y. S., & Khanna, A. (2022). Room Temperature CO2 Adsorption Studies Using Pure and Ionic Liquid Immobilized Zeolites. Journal of Chemical & Engineering Data, 67(11), 3503-3515.

Song, T., Avelar Bonilla, G. M., Morales-Collazo, O., Lubben, M. J., & Brennecke, J. F. (2019). Recyclability of encapsulated ionic liquids for post-combustion CO2 capture. Industrial & Engineering Chemistry Research, 58(12), 4997-5007.

Song, X., Yu, J., Wei, M., Li, R., Pan, X., Yang, G., & Tang, H. (2019). Ionic liquids-functionalized zeolitic imidazolate framework for carbon dioxide adsorption. Materials, 12(15), 2361.

Suhaili, N., Lim, L., Teh, L., Shahdan, S. N., & Manabu, Z. G. (2023). Effect of Arginine-Based Deep Eutectic Solvents on Supported Porous Sorbent for CO2. Sains Malaysiana, 52(5), 1419-1434.

Sun, L., & Tang, S. (2019). Synthesis of bi-functionalized ionic liquid—mesoporous alumina composite material and its CO2 capture capacity. Korean Journal of Chemical Engineering, 36(10), 1708-1715.

Sun, Y., Zhu, J., Huang, J., Xin, F., & Liu, J. (2017). Polymeric ionic liquid modified silica for CO2 adsorption and diffusivity. Polymer Composites, 38(4), 759-766.

Tamilarasan, P., & Ramaprabhu, S. (2016). Amine-rich ionic liquid grafted graphene for sub-ambient carbon dioxide adsorption. RSC Advances, 6(4), 3032-3040.

Tanaka, S., Kida, K., Fujimoto, H., Makino, T., & Miyake, Y. (2011). Self-assembling imidazolium-based ionic liquid in rigid nanopores induces anomalous CO2 adsorption at low pressure. Langmuir, 27(13), 7991-7995.

Uehara, Y., Karami, D., & Mahinpey, N. (2017). Effect of water vapor on CO2 sorption–desorption behaviors of supported amino acid ionic liquid sorbents on porous microspheres. Industrial & engineering chemistry research, 56(48), 14316-14323.

Uehara, Y., Karami, D., & Mahinpey, N. (2018). Roles of cation and anion of amino acid anion-functionalized ionic liquids immobilized into a porous support for CO2 capture. Energy & Fuels, 32(4), 5345-5354.

Uehara, Y., Karami, D., & Mahinpey, N. (2019a). Amino acid ionic liquid-modified mesoporous silica sorbents with remaining surfactant for CO 2 capture. Adsorption, 25(4), 703-716.

Uehara, Y., Karami, D., & Mahinpey, N. (2019b). CO2 adsorption using amino acid ionic liquid-impregnated mesoporous silica sorbents with different textural properties. Microporous and Mesoporous Materials, 278, 378-386.

Wan, M. M., Zhu, H. Y., Li, Y. Y., Ma, J., Liu, S., & Zhu, J. H. (2014). Novel CO2-capture derived from the basic ionic liquids orientated on mesoporous materials. ACS applied materials & interfaces, 6(15), 12947-12955.

Wang, L., Zhang, J., Tan, Z., Jiang, H., & Xiong, C. (2015). Development of ionic liquids tethered to coconut shell activated carbon for biogas upgrading in a packed bed. Energy Technology, 3(5), 509-517.

Wang, P., Zhu, J., Tang, J., Kang, J., & Shi, L. (2022). Morphology and CO2 adsorption performance of novel ionic liquid microcapsules containing [Bmim][PF6]. Chemical Engineering Research and Design, 187, 633-644.

Wang, T., Song, X., Luo, Q., Yang, X., Chong, S., Zhang, J., & Ji, M. (2018). Acid-base bifunctional catalyst: Carboxyl ionic liquid immobilized on MIL-101-NH2 for rapid synthesis of propylene carbonate from CO2 and propylene oxide under facile solvent-free conditions. Microporous and Mesoporous Materials, 267, 84-92.

Wang, X., Akhmedov, N. G., Duan, Y., Luebke, D., Hopkinson, D., & Li, B. (2013). Amino acid-functionalized ionic liquid solid sorbents for post-combustion carbon capture. ACS applied materials & interfaces, 5(17), 8670-8677.

Wang, X., Akhmedov, N. G., Duan, Y., Luebke, D., & Li, B. (2013). Immobilization of amino acid ionic liquids into nanoporous microspheres as robust sorbents for CO 2 capture. Journal of Materials Chemistry A, 1(9), 2978-2982.

Wang, Y., & Yang, R. T. (2020). Template removal from SBA-15 by ionic liquid for amine grafting: applications to CO2 capture and natural gas desulfurization. ACS Sustainable Chemistry & Engineering, 8(22), 8295-8304.

Wu, J., Yang, Z., Xie, J., Zhu, P., Wei, J., Jin, R., & Yang, H. (2023). Porous polymer supported amino functionalized ionic liquid for effective CO2 capture. Langmuir, 39(7), 2729-2738.

Xu, Q.-Q., Yin, J.-Z., Zhou, X.-L., Yin, G.-Z., Liu, Y.-F., Cai, P., & Wang, A.-Q. (2016). Impregnation of ionic liquids in mesoporous silica using supercritical carbon dioxide and co-solvent. RSC Advances, 6(103), 101079-101086.

Xu, W.-L., Zhang, J.-Y., Cheng, N.-N., Li, Z.-L., Lan, H.-C., Jiang, W.-J., Huang, K., Peng, H.-L., & Du, J. (2021). Facilely synthesized mesoporous polymer for dispersion of amino acid ionic liquid and effective capture of carbon dioxide from anthropogenic source. Journal of the Taiwan Institute of Chemical Engineers, 125, 115-121.

Xu, W.-L., Zhang, J.-Y., Cheng, N.-N., Li, Z.-L., Lan, H.-C., Jiang, W.-J., Peng, H.-L., Huang, K., & Du, J. (2021). Dispersing aminopolycarboxylate ionic liquids in mesoporous organic polymer for highly efficient and improved carbon capture from dilute source. Journal of Molecular Liquids, 338, 116653.

Xue, C., Feng, L., Zhang, Q., Huang, R., Hao, Y., Ma, X., Liu, G., Li, K., & Hao, X. (2019). High and fast carbon dioxide capture of hydroxypyridine-based ionogel depending on pore structure of mesoporous silica vesicle in the simulated flue gas. International journal of greenhouse gas control, 84, 111-120.

Xue, C., Feng, L., Zhu, H., Huang, R., Wang, E., Du, X., Liu, G., Hao, X., & Li, K. (2019). Pyridine-containing ionic liquids lowly loaded in large mesoporous silica and their rapid CO2 gas adsorption at low partial pressure. Journal of CO2 Utilization, 34, 282-292.

Xue, C., Zhu, H., Du, X., An, X., Wang, E., Duan, D., Shi, L., Hao, X., Xiao, B., & Peng, C. (2017). Unique allosteric effect-driven rapid adsorption of carbon dioxide in a newly designed ionogel [P 4444][2-Op]@ MCM-41 with excellent cyclic stability and loading-dependent capacity. Journal of Materials Chemistry A, 5(14), 6504-6514.

Ye, C.-P., Wang, R.-N., Gao, X., & Li, W.-Y. (2020). CO2 Capture Performance of supported phosphonium dual amine-functionalized ionic liquids@ MCM-41. Energy & Fuels, 34(11), 14379-14387.

Ye, N., Shen, Y., Chen, Y., Cao, J., Lu, X., & Ji, X. (2024). Enhanced CO2 Capture through SAPO-34 Impregnated with Ionic Liquid. Langmuir, 40(17), 9097-9107.

Yin, J.-Z., Zhen, M.-Y., Cai, P., Zhou, D., Li, Z.-J., Zhu, H.-Y., & Xu, Q.-Q. (2018). Supercritical CO2 preparation of SBA-15 supported ionic liquid and its adsorption for CO2. Materials Research Express, 5(6), 065060.

Yousefe, M., Ursano, B., Reina, J. A., & Puga, A. (2023). Readily regenerable amine-free CO2 sorbent based on a solid-supported carboxylate ionic liquid. Journal of Environmental Management, 334, 117469.

Yu, Y., Mai, J., Huang, L., Wang, L., & Li, X. (2014). Ship in a bottle synthesis of ionic liquids in NaY supercages for CO 2 capture. RSC Advances, 4(25), 12756-12762.

Yu, Y., Mai, J., Wang, L., Li, X., Jiang, Z., & Wang, F. (2014). Ship-in-a-bottle synthesis of amine-functionalized ionic liquids in NaY zeolite for CO2 capture. Scientific reports, 4(1), 1-8.

Yuan, J., Fan, M., Zhang, F., Xu, Y., Tang, H., Huang, C., & Zhang, H. (2017). Amine-functionalized poly (ionic liquid) brushes for carbon dioxide adsorption. Chemical Engineering Journal, 316, 903-910.

Yusuf, N. M., Masdar, M., Isahak, W., Nordin, D., Husaini, T., Majlan, E., Wu, S., Rejab, S., & Lye, C. (2019). Impregnated carbon–ionic liquid as innovative adsorbent for H2/CO2 separation from biohydrogen. International Journal of Hydrogen Energy, 44(6), 3414-3424.

Zeeshan, M., Keskin, S., & Uzun, A. (2018). Enhancing CO2/CH4 and CO2/N2 separation performances of ZIF-8 by post-synthesis modification with [BMIM][SCN]. Polyhedron, 155, 485-492.

Zeeshan, M., Nozari, V., Yagci, M. B., Isık, T., Unal, U., Ortalan, V., Keskin, S., & Uzun, A. (2018). Core–shell type ionic liquid/metal organic framework composite: an exceptionally high CO2/CH4 selectivity. Journal of the American Chemical Society, 140(32), 10113-10116.

Zeeshan, M., Yalcin, K., Oztuna, F. E. S., Unal, U., Keskin, S., & Uzun, A. (2021). A new class of porous materials for efficient CO2 separation: Ionic liquid/graphene aerogel composites. Carbon, 171, 79-87.

Zhang, W., Gao, E., Li, Y., Bernards, M. T., He, Y., & Shi, Y. (2019). CO2 capture with polyamine-based protic ionic liquid functionalized mesoporous silica. Journal of CO2 Utilization, 34, 606-615.

Zhang, W., Gao, E., Li, Y., Bernards, M. T., Li, Y., Cao, G., He, Y., & Shi, Y. (2019). Synergistic enhancement of CO2 adsorption capacity and kinetics in triethylenetetrammonium nitrate protic ionic liquid functionalized SBA-15. Energy & Fuels, 33(9), 8967-8975.

Zhou, Y., Chang, M., Zang, X., Zheng, L., Wang, Y., Wu, L., Han, X., Chen, Y., Yu, Y., & Zhang, Z. (2020). The polymeric ionic liquids/mesoporous alumina composites: synthesis, characterization and CO2 capture performance test. Polymer Testing, 81, 106109.

Zhu, J., He, B., Huang, J., Li, C., & Ren, T. (2018). Effect of immobilization methods and the pore structure on CO2 separation performance in silica-supported ionic liquids. Microporous and Mesoporous Materials, 260, 190-200.

Zhu, J., Xin, F., Huang, J., Dong, X., & Liu, H. (2014). Adsorption and diffusivity of CO2 in phosphonium ionic liquid modified silica. Chemical Engineering Journal, 246, 79-87.

Zhu, J., Xin, F., Sun, Y., & Dong, X. (2014). Phosphonium-based ionic liquids grafted onto silica for CO2 sorption. Theoretical Foundations of Chemical Engineering, 48(6), 787-792.

Zulkurnai, N., Ali, U. M., Ibrahim, N., & Manan, N. A. (2017). Carbon dioxide (CO2) adsorption by activated carbon functionalized with deep eutectic solvent (DES). IOP Conference Series: Materials Science and Engineering,