The impact of sorting quality on the properties of recycled flexible plastic packaging

J. Langwieser1, 2*, A. Hatmanstorfer2, N. Kuhn3, A. Tischberger-Aldrian3, J. Fischer2, 4

- Competence Center CHASE GmbH, Altenberger Strasse 69, 4040 Linz, Austria

- Johannes Kepler University Linz, Institute of Polymeric Materials and Testing, Altenberger Strasse 69, 4040 Linz, Austria

- Montanuniversitaet Leoben, Chair of Waste Processing Technology and Waste Management, Franz-Josef-Strasse 18, 8700 Leoben, Austria

- Johannes Kepler University Linz, Linz Institute of Technology (LIT) Factory, Altenberger Strasse 69, 4040 Linz, Austria

*Correspondence: johanna.langwieser@chasecenter.at

Oxidation onset temperature (OOT)

|  | OOT [°C] |  |
| --- | --- | --- |
|  | Mean | Standard deviation |
| Grade 1 | 223,9 | 1,1 |
| Grade 2 | 224,4 | 0,4 |
| Grade 3 | 219,0 | 0,4 |
| Grade 4 | 222,6 | 1,7 |
| P01 | 218,0 | 0,4 |
| P03 | 216,2 | 0,1 |
| P05 | 209,3 | 0,4 |

Ash Content

|  | Ash content [%] |  |
| --- | --- | --- |
|  | Mean | Standard deviation |
| Grade 1 | 2,4 | 0,02 |
| Grade 2 | 1,0 | 0,15 |
| Grade 3 | 2,8 | 0,03 |
| Grade 4 | 2,5 | 0,03 |
| P01 | 1,6 | 0,05 |
| P03 | 2,2 | 0,07 |
| P05 | 2,6 | 0,10 |

Density

|  | Density [g/cm3] |  |
| --- | --- | --- |
|  | Mean | Standard deviation |
| Grade 1 | 0,947 | 0,002 |
| Grade 2 | 0,923 | 0,006 |
| Grade 3 | 0,886 | 0,001 |
| Grade 4 | 0,877 | 0,008 |
| P01 | 0,830 | 0,001 |
| P03 | 0,819 | 0,006 |
| P05 | 0,826 | 0,005 |

Melt mass-flow rate (MFR)

|  | MFR [g/10 min] |  |
| --- | --- | --- |
|  | Mean | Standard deviation |
| Grade 1 | 0,6 | 0,01 |
| Grade 2 | 0,9 | 0,01 |
| Grade 3 | 0,7 | 0,01 |
| Grade 4 | 0,9 | 0,02 |
| P01 | 1,1 | 0,02 |
| P03 | 1,4 | 0,00 |
| P05 | 1,2 | 0,01 |