Table S-1 Characteristics of the metal standard stock solutions

| Standard | Matrix | Certified concentration of metal ± U | Producer |
| --- | --- | --- | --- |
| Cobalt (CoCl2) | water with HNO3 | (1.000 ± 0.002) g Co/dm3 | Merck (Titrisol), Germany |
| Cadmium (one-component, Cd) | 2% HNO3 | (1000 ± 3) μg Cd/cm3 | CPI International, USA |
| Copper (one-component, Cu) | 2% HNO3 | (1000 ± 3) μg Cu/cm3 | CPI International, USA |
| Lead (one-component, Pb) | 2% HNO3 | (1000 ± 3) μg Pb/cm3 | CPI International, USA |

U – expanded uncertainty for coverage factor k=2

Table S-2 Parameters of metal sorption isotherms in the Freundlich model

| Metal | Parameter | Sorbent |  |
| --- | --- | --- | --- |
|  |  | Subbituminous coal | UCG Char |
| Cadmium | KF ± Δ KF | 0.00074 ± 0.00008 | 0.0075 ± 0.0024 |
|  | n ± Δn | 0.813 ± 0.041 | 0.419 ± 0.055 |
|  | R2 | 0.9901 | 0.9346 |
| Cobalt | KF ± Δ KF | 0.00069 ± 0.00014 | 0.0129 ± 0.0033 |
|  | n ± Δn | 1.04 ± 0.13 | 0.468 ± 0.079 |
|  | R2 | 0.9447 | 0.8965 |
| Copper | KF ± Δ KF | 0.00405 ± 0.00016 | 0.8757 ± 1.1000 |
|  | n ± Δn | 0.862 ± 0.022 | 0.839 ± 0.170 |
|  | R2 | 0.9975 | 0.8588 |
| Lead | KF ± Δ KF | 0.01283 ± 0.00026 | 0.4656 ± 0.2100 |
|  | n ± Δn | 0.698 ± 0.010 | 0.6218 ± 0.0710 |
|  | R2 | 0.9991 | 0.9509 |