Supplementary Table 1 Summary of parameters from multivariate linear regression analysis for AF tensile modulus (Equation 8). represents regression coefficient and SE represents the standard error of the coefficient
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log(modulus) (log(MPa))

Variable I SE p-value

Constant 3.401 0.076 1.85X 103
log(length) (log (mm)) -1.106 0.075 5.05 X 10?%°
1/width (mm™) -2.733 0.089 2.78 X103
AR 0.058 0.008 2.58 X 10°











