Supporting Information

Visible light photocatalytic degradation of microplastic residuals with zinc oxide nanorods

Tajkia Syeed Tofa,1 Karthik Laxman Kunjali,2 Swaraj Paul,3 and Joydeep Dutta 2*

1Department of Sustainable development, Environmental Science and Engineering, School of Architecture and the Built Environment, KTH Royal Institute of Technology, Stockholm, Sweden

2Functional Materials, Department of Applied Physics, School of Engineering Sciences, KTH Royal Institute of Technology, Stockholm, Sweden

3PP Polymer AB, Krossgatan 15 , SE-162 50 Vällingby, Stockholm, Sweden

*Corresponding author:

Prof. Joydeep Dutta

Functional Materials, Dept. of Applied Physics

KTH Royal Institute of Technology

Isafjordsgatan 22, SE 164 40, Kista

Email: joydeep@kth.se

Ph: +46-8-790 81 42, Mb: +46-73-765 21 86

# Experimental set-up

Fig. S1: Experimental setup for conducting photocatalysis process.

# SEM Images

Fig. S2: SEM images of the top view demonstrate diameter and density of the hydrothermally prepared different concentration of ZnO nanorods on glass substrate. Also, side view shows the length of nanorods. a) 3 mM_5hrs, b) 5 mM_5hrs c) 10 mM_5hr, and d) 20 mM_5hr.

Table S1: Properties of ZnO catalysts of different concentrations

| Growth concentration | 3mM_5hrs | 5mM_5hrs | 10mM_5hrs | 20mM_5hrs |
| --- | --- | --- | --- | --- |
| avg. diameter, d (nm) | 34.5 | 40 | 55 | 65 |
| avg. side length, l (nm) | 263 | 511 | 960 | 1750 |
| avg. area of each nano rod (nm2) | 28766.68 | 63398.46 | 162329.59 | 346738.44 |
| avg. density of the nanorods on substrate (/nm2) | 0.000225 | 0.00035 | 0.0003 | 0.00015 |
| Total effective surface area on a substrate of sizes (1 cm X 1 cm) (cm2) | 6.5 | 22 | 49 | 55 |