[bookmark: _Hlk140215224]Table S2. Multi-comparison Tukey tests for deadwood basic density between species overall and for each decay class of Picea abies, Pinus sylvestris and Fagus sylvatica (p < 0.05; Tukey HSD method).

	Decay class
	Tree species
	difference
	lwr
	upr
	p adj

	All
	pine-beech
	-0.0594
	-0.1157
	-0.0032
	<0.05

	All
	spruce-beech
	-0.0502
	-0.0985
	-0.0019
	<0.05

	All
	spruce-pine
	0.0092
	-0.0352
	0.0537
	1

	1
	pine-beech
	-0.1278
	-0.1901
	-0.0656
	0

	1
	spruce-beech
	-0.1242
	-0.1775
	-0.071
	0

	1
	spruce-pine
	-0.0449
	0.0131
	0.0521
	1

	2
	pine-beech
	-0.0642
	-0.119
	-0.0093
	<0.05

	2
	spruce-beech
	-0.0447
	-0.0919
	0.0025
	<0.1

	2
	spruce-pine
	0.0194
	-0.0241
	0.063
	1

	3
	pine-beech
	-0.0273
	-0.0848
	0.0302
	1

	3
	spruce-beech
	-0.0099
	-0.0594
	0.0396
	1

	3
	spruce-pine
	0.0174
	-0.0282
	0.063
	1

	4
	pine-beech
	-0.0296
	-0.0897
	0.0306
	1

	4
	spruce-beech
	-0.0395
	-0.0913
	0.0123
	1

	4
	spruce-pine
	-0.0099
	-0.0577
	0.0378
	1


Confidence level used: 0.95

