# A priori predictions of Type I and Type V isotherms by the Rigid Adsorbent Lattice Fluid

Maarten C. Verbraeken and Stefano Brandani

School of Engineering, University of Edinburgh, The King’s Buildings, Robert Stevenson Road, EH9 3FB

### Supporting information

Figure S1 shows the comparison between the RALF model and a number of Frumkin-Fowler-Guggenheim (FFG) isotherm (equation 1 in the main text) for different values of ω. The FFG isotherm parameters are set to give the same Henry’s law constant and the same saturation capacity for both models (see Table S1), thus leaving only the energy parameter, ω, to be determined. The FFG isotherm can be rewritten as follows:

bp=nnsat-ne-2ωθRT										S1

nsat is the amount adsorbed as predicted by RALF, which can be calculated considering the system at ρ=1, ref.1:

ρ=ρρ*=jmjVsjwjρj*=1									S2

Which, for a single component, leads to

nsat,1=ρ1*ρsM11-ρsρs*										S3

The saturation capacity of water in silicalite-1 as determined through equation S3, i.e. nsat,H2O=10.03 mol kg–1 is in good agreement with the reported micropore volume of silicalite-1, Vp=0.185 cm3 g–1 (ref. 2). The Henry’s law constant can be calculated by expressing the compressibility as

lnz=ln1kgρsRT-lnN1msP										S4

and considering that in the low pressure limit:

limP→0 N1msP=KP											S5

Finally, the expression for the adsorbate’s chemical potential (equation 18 in the main text) can be rearranged to give:

lnKP=ln1kgρsRT+ρsRTr10v1*2P1s*-1-ρsln1-ρsρs+1r10-r10v1*vs*-ln1-ρsρs-1			S6

Table S1: Fowler-Guggenheim isotherm parameters used to match predicted isotherm for water on silicalite-1 at 300 K by RALF model

| Fowler Guggenheim isotherm parameters |  |  |
| --- | --- | --- |
| b | 3.9×10-5 | (Pa–1) |
| nsat | 10.03 | (mol kg–1) |
| ω2-phase | 4.88×103 | (J mol–1) |

Figure S1: Comparison of RALF prediction for water on silicalite-1 at 300 K and FFG isotherm for different values of ω.

Figure S2: Predicted ethanol isotherms on silicalite-1 with varying solid density at 300 K. Actual density for silicalite-1 is 1786 kg m–3, which corresponds to a porosity  = 0.31, indicated by the dashed line.

Figure S3: Predicted propane isotherms on silicalite-1 with varying solid density 300 K. Actual density for silicalite-1 is 1786 kg m–3, which corresponds to a porosity  = 0.31, indicated by the dashed line.

Figure S4: Ethanol isotherms for silicalite-1 (ε=0.31) at 300 K for different values of binary interaction parameter js

## References

(1) 	Brandani, S. The Rigid Adsorbent Lattice Fluid Model for Pure and Mixed Gas Adsorption. AIChE J. 2019, 65 (4), 1304–1314. https://doi.org/10.1002/aic.16504.

(2) 	Trzpit, M.; Soulard, M.; Patarin, J.; Desbiens, N.; Cailliez, F.; Boutin, A.; Demachy, I.; Fuchs, A. H. The Effect of Local Defects on Water Adsorption in Silicalite-1 Zeolite:  A Joint Experimental and Molecular Simulation Study. Langmuir 2007, 23 (20), 10131–10139. https://doi.org/10.1021/la7011205.