Supplemental Information to accompany:

“A Reference High-Pressure CH4 Adsorption Isotherm for Zeolite Y:
Results of an Interlaboratory Study”

H. G. T. Nguyen,1* C. M. Sims,1 B. Toman,1 J. Horn,1 R. D. van Zee,1 M. Thommes,2 R. Ahmed,3 J. F. M. Denayer,4 G. V. Baron,4 E. Napolitano,5 M. Bielewski,5 E. Mangano,6 S. Brandani,6 D. P. Broom,7 M. J. Benham,7 A. Dailly,8 F. Dreisbach,9 S. Edubilli,10 S. Gumma,10, † J. Möllmer,11 M. Lange,11 M. Tian,12, ‡ T. J. Mays,12 T. Shigeoka,13 S. Yamakita,13 M. Hakuman,13 Y. Nakada,13 K. Nakai,13 J. Hwang,14 R. Pini,14 H. Jiang,15 A. D. Ebner,15 M. A. Nicholson,15 J. A. Ritter,15 J. Farrando-Pérez,16 C. Cuadrado-Collados,16 J. Silvestre-Albero,16 C. Tampaxis,17 T. Steriotis,17 D. Řimnáčová,18 M. Švábová,18 M. Vorokhta,18 H. Wang,19 E. Bovens,20 N. Heymans,20 G. De Weireld20

*Corresponding author email: huong.nguyen@nist.gov

1National Institute of Standards and Technology, Gaithersburg MD, USA

2Friedrich-Alexander University Erlangen-Nuremberg, Nuremberg, Germany

3Anton Paar QuantaTec Inc. Boynton Beach FL, USA

4Vrije Universiteit Brussel, Brussels, Belgium

5European Commission, Joint Research Centre (JRC), Petten, Netherlands

6University of Edinburgh, Edinburgh, UK

7Hiden Isochema Limited, Warrington, UK

8General Motors, Warren MI, USA

9TA Instruments, Bochum, Germany

10Indian Institute of Technology Guwahati, Assam, India

11 Institute of Non-Classical Chemistry, Leipzig, Germany

12University of Bath, Bath, UK

13MicrotracBEL, Suminoe-ku, Osaka, Japan

14Imperial College London, London, UK

15University of South Carolina, Columbia SC, USA

16University of Alicante, Alicante, Spain

17National Centre for Scientific Research “Demokritos”, Greece

18Czech Academy of Sciences, Prague, Czech Republic

19National Institute of Metrology, Beijing, China

20University of Mons, Mons, Belgium

† Current affiliation: Indian Institute of Technology Tirupati, Andhra Pradesh, India

‡Current affiliation: University of Exeter, Exeter, UK

Table of Contents

S1. Surface and pore characterization of Zeolite Y

S2. ILS2 CO2/ZSM-5 isotherms (all datasets)

S3. ILS2 goodness-of-fit values

S4. ILS2 CO2/ZSM-5 isotherms (individual datasets #1-14, 16-18)

S5. ILS2 CH4/Zeolite Y isotherms (datasets #1-28)

S6. ILS2 CH4/Zeolite Y isotherms (all datasets > 2 MPa and ≥ 7.5 MPa)

S7. OpenBUGS codes (goodness-of-fit and methane fit)

S1. Surface and pore characterization of Zeolite Y

Figure S1. Ar isotherms at 87 K and pore volume and pore-size distribution for Zeolite Y (RM 8850). The BET surface area calculated from P/Po = 0.008 to 0.04 is 819 ± 13 m2/g. The pore volume (PV) and pore-size-distribution (PSD) was determined using NLDFT calculation model on the equilibrium branch of the Ar isotherm at 87 K for zeolites with spherical/cylindrical pores.

S2. ILS2 CO2/ZSM-5 isotherms (all datasets)

Figure S2. ILS2 CO2 adsorption isotherms at 20 °C for ZSM-5 for all submitted datasets.

S3. ILS2 goodness-of-fit values

Table S1. goodness-of-fit values for ILS2 CO2 adsorption isotherms at 20 °C for ZSM-5.

| dataset | goodness-of-fit value* |
| --- | --- |
| 1 | 0.13 |
| 2 | 0.07 |
| 3 | 0.12 |
| 4 | 0.18 |
| 5 | 0.08 |
| 6 | 0.06 |
| 7 | 0.03 |
| 8 | 0.12 |
| 9 | 0.09 |
| 10 | 0.15 |
| 11 | 0.08 |
| 12 | 0.11 |
| 13 | 0.07 |
| 14 | 0.38 |
| 16 | 0.07 |
| 17 | 0.02 |
| 18 | 0.07 |

*green = pass; orange = borderline; red = fail

S4. ILS2 CO2/ZSM-5 isotherms (individual datasets #1-18)

Figure S3. ILS2 CO2 adsorption isotherms at 20 °C for ZSM-5 for datasets 1-6.

Figure S4. ILS2 CO2 adsorption isotherms at 20 °C for ZSM-5 for datasets 7-12.

Figure S5. ILS2 CO2 adsorption isotherms at 20 °C for ZSM-5 for datasets 13-18. No data was submitted for dataset #15.

S5. ILS2 CH4/Zeolite Y isotherms (datasets #1-28)

Figure S6. ILS2 CH4 adsorption isotherms at 25 °C for Zeolite Y for datasets 1-6.

Figure S7. ILS2 CH4 adsorption isotherms at 25 °C for Zeolite Y for datasets 7-12.

Figure S8. ILS2 CH4 adsorption isotherms at 25 °C for Zeolite Y for datasets 13-18.

Figure S9. ILS2 CH4 adsorption isotherms at 25 °C for Zeolite Y for datasets 19-24.

Figure S10. ILS2 CH4 adsorption isotherms at 25 °C for Zeolite Y for datasets 25-28.

S6. ILS2 CH4/Zeolite Y isotherms (all datasets > 2 MPa and ≥ 7.5 MPa)

Figure S11. ILS2 CH4 adsorption isotherms at 25 °C for Zeolite Y for all datasets minus datasets only up to 2 MPa (datasets 5, 10, 11, 19, 23, and 25)

Figure S12. ILS2 CH4 adsorption isotherms at 25 °C for Zeolite Y for all datasets minus datasets not measured up to 7.5 MPa (datasets 5, 10, 11, 19, 23, 25, 3, 7, 9, 12, 18, 22, 24, 27, and 28)

S7. OpenBUGS codes

S7.1. OpenBUGS code for CH4/Zeolite Y isotherm at 25 °C reference fit

{

g~dunif(0,10)

a~dunif(-10,5)

b~dunif(0,5)

f~dunif(0,5)

for(i in 1:12){sig[i]~dgamma(1.0E-5,1.0E-5)}

T1~dcat(P1[])

P1[1:12]~ddirich(alpha1[])

alpha1[1]<-1

alpha1[2]<-0.1

alpha1[3]<-1

alpha1[4]<-1

alpha1[5]<-1

alpha1[6]<-1

alpha1[7]<-1

alpha1[8]<-1

alpha1[9]<-1

alpha1[10]<-0.1

alpha1[11]<-0.1

alpha1[12]<-1

sigp<-sig[T1]

for (i in 1:1079){lpress[i]<-log(press[i])

bot[i]<-1+exp((-lpress[i]+a)/b)

mean[i]<-g/pow(bot[i],f)

uptake[i]~dnorm(mean[i],sig[lab[i]])}

for(i in 1:1079){dif[i]<-uptake[i]-predy[i]

predy[i]~dnorm(mean[i],sigp)

}

for(i in 1:131){pressl[i]<--9.2+0.1*i

pressp[i]<-exp(pressl[i])}

for (i in 1:131){

lpredp[i]<-log(pressp[i])

botp[i]<-1+exp((-lpredp[i]+a)/b)

meanp[i]<-g/pow(botp[i],f)

pred[i]<-meanp[i]

predb[i]~dnorm(pred[i],sigp)}

a.cut<-cut(a)

b.cut<-cut(b)

f.cut<-cut(f)

g.cut<-cut(g)

for(i in 1:18){sign[i]~dgamma(1.0E-5,1.0E-5)}

for( i in 1:883){lpressn[i]<-log(pressn[i])

botn[i]<-1+exp((-lpressn[i]+a.cut)/b.cut)

meann[i]<-g.cut/pow(botn[i],f.cut)

meann.cut[i]<-cut(meann[i])

uptaken[i]~dnorm(meann.cut[i],sign[labn[i]])

predbn[i]~dnorm(meann.cut[i],sign[labn[i]])}

}

list(sig=c(1, 1,1,1,1,1,1,1,1,1,1,1),sign=c(1,1,1,1,1,1,1,1,1,1,1,1,1,1,1,1,1,1) )

S7.2. OpenBUGS code for goodness-of-fit determination for CO2/ZSM-5 isotherms at 20 °C.

{

g~dunif(0,10)

a~dunif(-10,5)

b~dunif(0,5)

f~dunif(0,5)

for(i in 1:12){sig[i]~dgamma(1.0E-5,1.0E-5)}

T1~dcat(P1[])

P1[1:12]~ddirich(alpha1[])

alpha1[1]<-1

alpha1[2]<-0.1

alpha1[3]<-1

alpha1[4]<-1

alpha1[5]<-1

alpha1[6]<-1

alpha1[7]<-1

alpha1[8]<-1

alpha1[9]<-1

alpha1[10]<-0.1

alpha1[11]<-0.1

alpha1[12]<-1

sigp<-sig[T1]

for (i in 1:1079){lpress[i]<-log(press[i])

bot[i]<-1+exp((-lpress[i]+a)/b)

mean[i]<-g/pow(bot[i],f)

uptake[i]~dnorm(mean[i],sig[lab[i]])}

for(i in 1:1079){dif[i]<-uptake[i]-predy[i]

predy[i]~dnorm(mean[i],sigp)

}

for(i in 1:131){pressl[i]<--9.2+0.1*i

pressp[i]<-exp(pressl[i])}

for (i in 1:131){

lpredp[i]<-log(pressp[i])

botp[i]<-1+exp((-lpredp[i]+a)/b)

meanp[i]<-g/pow(botp[i],f)

pred[i]<-meanp[i]

predb[i]~dnorm(pred[i],sigp)}

a.cut<-cut(a)

b.cut<-cut(b)

f.cut<-cut(f)

g.cut<-cut(g)

for(i in 1:18){sign[i]~dgamma(1.0E-5,1.0E-5)}

for( i in 1:883){lpressn[i]<-log(pressn[i])

botn[i]<-1+exp((-lpressn[i]+a.cut)/b.cut)

meann[i]<-g.cut/pow(botn[i],f.cut)

meann.cut[i]<-cut(meann[i])

uptaken[i]~dnorm(meann.cut[i],sign[labn[i]])

predbn[i]~dnorm(meann.cut[i],sign[labn[i]])}

}

list(sig=c(1, 1,1,1,1,1,1,1,1,1,1,1),sign=c(1,1,1,1,1,1,1,1,1,1,1,1,1,1,1,1,1,1) )