Supporting Information

Anticancer effects against Colorectal Cancer Models of chloro(triethylphosphine)gold(I) Encapsulated in PLGA-PEG Nanoparticles

Alessio Menconi,[a] Tiziano Marzo,*[b] Lara Massai,[c] Alessandro Pratesi,[d] Mirko Severi,[c] Giulia Petroni,[a] Lorenzo Antonuzzo,[e] Luigi Messori,[c] Serena Pillozzi,*[a,f]# Damiano Cirri*[d]#

[a]	A. Menconi, Dr. G. Petroni, Dr. S. Pillozzi, Department of Experimental and Clinical Medicine, University of Florence, Viale G.B. Morgagni 50, 50134 Firenze, Italy. E-mail: serena.pillozzi@unifi.it

[b]	Dr. T. Marzo orcid.org/0000-0002-2567-3637, Department of Pharmacy, University of Pisa, Via Bonanno Pisano 6, 56126, Pisa, Italy. E-mail: tiziano.marzo@unipi.it

[c]	Prof. L. Messori orcid.org/0000-0002-9490-8014, Dr. L. Massai orcid.org/0000-0003-0765-1802, Laboratory of Metals in Medicine (MetMed), Department of Chemistry “U. Schiff”, University of Florence, Via della Lastruccia 3, 50019 Sesto Fiorentino, Italy.

[d]	Dr. A. Pratesi orcid.org/0000-0002-9553-9943, Dr. D. Cirri orcid.org/0000-0001-9175-9562, Department of Chemistry and Industrial chemistry (DCCI), University of Pisa, Via G. Moruzzi 13, 56124, Pisa, Italy. E-mail: damiano.cirri@dcci.unipi.it

[e]	Dr. L. Antonuzzo, S.C. Oncologia Medica 1, Azienda Ospedaliero-Universitaria Careggi, Florence, Italy.

[f]	Dr. S. Pillozzi, DI.V.A.L Toscana S.R.L., Via Madonna del Piano, 6, 50019 Sesto Fiorentino, Italy. E-mail: serena.pillozzi@unifi.it

# These authors equally contributed

Index

1HNMR spectrum	2

DLS measurements	2

Spectroscopic properties	3

Et3PAuCl retention	4

# 1HNMR spectrum

Figure S1. 1HNMR spectrum of RhB-C=O-PLGA-C=O-NH-PEG-COOH.

# DLS measurements

| Batch | PDI | Size (nm) |
| --- | --- | --- |
| 1 | 0.17 | 87 |
| 2 | 0.17 | 72 |
| 3 | 0.17 | 71 |
| 4 | 0.22 | 52 |
| 5 | 0.27 | 55 |
| 6 | 0.23 | 74 |
| 7 | 0.18 | 66 |

Table S1. DLS measurements used for determining size and PDI index of nanoparticles.

# Spectroscopic properties

Figure S2. Spectroscopic properties of PLGA-PEG nanoparticles loaded with Et3PAuCl. A: Comparison of absorbance profiles recorded on the solution of nanoparticles (black line) and filtered solution (red line). B: Comparison of fluorescence profiles recorded on the solution of nanoparticles (black line) and filtered solution (red line). Spectra were recorded using the same samples of absorbance analysis after an eight-fold dilution with MilliQ water.

# Et3PAuCl retention

| Batch | [Gold] (g/L) | [Released Gold] (g/L) | Gold retention (%) |
| --- | --- | --- | --- |
| 1 | 7777.3 | 555.4 | 92.9 |
| 2 | 7836.2 | 485.1 | 93.8 |
| 3 | 7982.4 | 694.9 | 91.4 |

Table S2. Determination of the retained amount of Et3PAuCl after 24 h at 25° C.

Figure S3. IC50 evaluation of Et3PAuCl (dark grey) and its encapsulated form (light grey) on HCT-116. Determination performed through MTT assay.