Synthesis and active manipulation of magnetic liquid beads

Ajeet Singh Yadav1, Fariba Malekpour Galogahi1, Aditya Vashi1, Du Tuan Tran1, Gregor S Kijanka1, Haotian Cha1, Kamalalayam Rajan Sreejith1 and Nam-Trung Nguyen1, *

1Queensland Micro- and Nanotechnology Centre, Griffith University, 170 Kessels Road, Nathan, QLD 4111, Australia.

*Corresponding author

Table S1: Mass ratio of liquid bead and solid bead

| # Mass ratio of liquid bead and solid bead |  |
| --- | --- |
| # Density of TMPTMA (g/ cm3) | # = 1.1 |
| # Density of HFE 7500 oil(g/ cm3) | # = 1.6 |
| # Mass of solid bead(density×volume) (g) | # = 5.75959×10-7 |
| # Volume of solid bead (cm3) | # = 5.23599×10-7 |
| # Volume of shell (cm3) | # = 4.58149×10-7 |
| # Volume of core (cm3) | # = 6.54498×10-8 |
| # Mass of core-shell bead(density×volume) (g) | # = 6.08684×10-7 |
| # Mass Ratio(solid bead/liquid bead) | # = 0.946236559 |

Table S2: Ratio of volumes available in solid and core-shell beads for magnetite particles

| ## Volume ratio of a solid and liquid beads |  |  |
| --- | --- | --- |
| ## Solid bead | ## Liquid bead | Volume Ratio |
| ## Radius outer (mm)= 0.05 | ## Radius outer (mm)= 0.05 | Volume (solid): Volume (shell of the core-shell bead) = 0.875 |
| ## Radius inner (mm) = 0 | ## Radius inner (mm)= 0.025 |  |
| ## Volume(particle)(mm3) = 0.000523599 | ## Volume(shell)(mm3) =0.000458 |  |

Figure S3: Motion of magnetic liquid beds represented by (a) displacement versus distance from magnet, (b) velocity versus distance from magnet and (c) acceleration versus distance from magnet graphs.

Figure S3: Motion of magnetic liquid beads: (a) Displacement, velocity, and acceleration versus distance from magnet for 1 and 2%(wt) magnetite particle containing solid beads [2].  (b) Displacement, velocity, and acceleration versus distance from magnet for 1 and 2%(wt) magnetite particle containing core-shell beads

Video S4: Video demonstrating sorting of magnetic liquid beads from non-magnetic beads.

## Video S5: Video showing response of beads collected from outlet 1 in presence of the magnet.

## Video S6: Video showing response of beads collected from outlet 2 in presence of the magnet.

## Video S7: Video showing 2D self-assembly of magnetic liquid beads in presence of magnet.