Electronic Supplementary Information

For

Kinetic Investigation of η-Al2O3 Catalyst for Dimethyl Ether production

Ahmed I. Osman a,b*, Jehad K. Abu-Dahrieha*

aSchool of Chemistry and Chemical Engineering, Queen’s University Belfast, Belfast BT9 5AG, Northern Ireland, UK

bChemistry Department, Faculty of Science - Qena, South Valley University, Qena 83523 – Egypt

* Corresponding author

Jehad K. Abu-Dahrieh, Ahmed I. Osman

E-mail: j.abudahrieh@qub.ac.uk, aosmanahmed01@qub.ac.uk

Address: School of Chemistry and Chemical Engineering, Queen's University Belfast, David Keir Building, Stranmillis Road, Belfast BT9 5AG, Northern Ireland, United Kingdom

Fax: +44 2890 97 4687

Tel.: +44 2890 97 4412

Table S1:  Surface area, pore volume, total acidity and acid density along with the EDX results of pure η-Al2O3 catalyst.

| Support / Catalyst | SBET (m2 g-1) | Crystallite size (nm) | Pore volume (cm3 g-1) | Total aciditya, A(sites/g) | Acid density, B(sites/m2) | EDX results |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Al | O |
| η-Al2O3 | 223 | 5.5 | 0.5 | 8.56 | 3.8 | 51.9 | 48.1 |

a Total acidity = A x 1020.

b Acid density = B x 1018.

Figure S1: The Nitrogen adsorption-desorption isotherms of η-Al2O3 acidic support catalyst.