Supplementary Material

Parts-per-million (salen)Fe(III) homogeneous catalysts for the production of biodiesel from waste cooking oils.

Massimo Melchiorre,a,b Angela Amoresano,a Peter H.M. Budzelaar,a Maria E. Cucciolito,a,c Fabio Mocerino,a Gabriella Pinto,a Francesco Ruffo a,c, Angela Tuzi,a Roberto Esposito,a,c,*.

aDipartimento di Scienze Chimiche, Università di Napoli Federico II, Complesso Universitario di Monte S. Angelo, via Cintia 21, 80126 Napoli, Italy; bISUSCHEM, piazza Carità 32, 80134 Napoli, Italy; cConsorzio Interuniversitario di Reattività Chimica e Catalisi (CIRCC), via Celso Ulpiani 27, 70126 Bari, Italy.

Figure S1. IR spectrum of catalyst 5 in nujol mull.

Figure S2. HRMS (ESI/QTOF) of catalyst 5.

Figure S3. UV-Vis spectrum of catalyst 5 in methanol. Lmax 232 nm

Paragraph S1. Method to quantify the yield of the reaction through NMR spectroscopy.

Figure S4. 1H NMR spectrum in CDCl3 at 25°C and 400 MHz of biodiesel produced from neutral soybean oil according to entry 10 of Table 3 (methanol:oil 10:1 mol:mol, catalyst 5 loading 0.10 mol %, 160°C, 2 h).

Table S1. Crystal data and refinement details for complex 5.

Figure S5. ORTEP view of complex 5 with ellipsoids drawn at 30 % probability level. The two splitted positions of carbonyl group and CHCl3 molecule are drawn as bold bonds (0.89 refined occupancy factor) and dashed open bonds (0.11 refined occupancy factor).

Figure S6. Perspective view of complex 5 showing the highly deformed octahedral environment of Fe ion.

Figure S7. Crystal packing of complex 5 viewed along b axis direction showing sheets of complex and solvent chloroform molecules that alternate in the a axis direction.

Table S2. Bond lengths comparison in Fe(N,N’,O,O’)(OAc) complexes.

Figure S1. IR spectrum of catalyst 5 in nujol mull.

Figure S2. HRMS (ESI/QTOF) of catalyst 5.

Figure S3. UV-Vis spectrum of catalyst 5 in methanol. Lmax 232 nm

Paragraph S1. Method to quantify the yield of the reaction through NMR spectroscopy

The signals relevant to the quantification of the reaction yield are:

a) the singlet at d 3.7 ppm, attributed to the methoxyl group, present only in the product.

b) the triplet at d 2.3, attributed to the methylene group α to the carbonyl group, present both in the reagent and the product.

Thus, indicating with A1 the integration area of the signal of the methoxyl group, and with A2 the integration area of the signal of the methylene group, the yield is obtained using the following formula, where the ratio A1/A2 is multiplied by a factor 2/3, because areas A1 and A2 relates to 3 and 2 protons, respectively (see Figure S4 for reference).

Y(%)=100 × 2A13A2

Figure S4. 1H NMR spectrum in CDCl3 at 25°C and 400 MHz of biodiesel produced from neutral soybean oil according to entry 10 of Table 3 (methanol:oil 10:1 mol:mol, catalyst 5 loading 0.10 mol %, 160°C, 2 h).

Table S1. Crystal data and refinement details for complex 5    _______________________________________________________

Empirical formula                      C22H23FeN2O4 · (CHCl3)

Formula weight                          554.64

Temperature                               173(2) K

Wavelength                                 0.71073 Å

Crystal system, space group       Monoclinic, P21/c

Unit cell dimensions                   a = 12.346(3) Å       α = 90°

b = 10.2737(15) Å   β = 105.999(18)°

c = 19.704(6) Å        = 90°

Volume                                       2402.4(10) Å3

Z, Calculated density                 4, 1.533 Mg/m3

Absorption coefficient               0.994 mm–1

F(000)                                        1140

Crystal size                                 0.50 x 0.14 x 0.05 mm

Theta range for data collection   2.925 to 27.840°.

Reflections collected / unique    18918 / 5344 [R(int) = 0.0660]

Refinement method                     Full-matrix least-squares on F2

Data / restraints / parameters       5344 / 3 / 325

Goodness-of-fit on F^2                1.040

Final R indices [I>2sigma(I)]       R1 = 0.0652, wR2 = 0.1362

R indices (all data)                        R1 = 0.1178, wR2 = 0.1578

Largest diff. peak and hole           0.787 and –0.433 eA–3

______________________________________________________________

Figure S5. ORTEP view of complex 5 with ellipsoids drawn at 30 % probability level.  The two splitted positions of carbonyl group and CHCl3 molecule are drawn as bold bonds (0.89 refined occupancy factor) and dashed open bonds (0.11 refined occupancy factor).

Figure S6. Perspective view of complex 5 showing the highly deformed octahedral environment of Fe ion.

Figure S7. Crystal packing of complex 5 viewed along b axis direction showing sheets of complex and solvent chloroform molecules that alternate in the a axis direction.

Table S2. Bond lengths comparison in Fe(N,N’,O,O’)(OAc) complexes.

| Bonda | Rangea |  | Complex 5 |
| --- | --- | --- | --- |
| Fe–O1 | 1.8572 – 1.900 | Å | 1.889 Å |
| Fe–O2 | 1.859 – 1.9081 | Å | 1.895 Å |
| Fe–N1 | 2.0885 – 2.399 | Å | 2.106 Å |
| Fe–N2 | 2.058 – 2.177 | Å | 2.087 Å |
| Fe–O3 | 2.0652 – 2.1124 | Å | 2.084 Å |
| Fe–O4 | 2.142 - 2.353 | Å | 2.128 Å |

a From Ref: O. J. Driscoll et al. “The synthesis, characterisation and application of iron(III)–acetate complexes for cyclic carbonate formation and the polymerisation of lactide”, Dalton Trans., 2019, 48, 15049.