Supplementary Material

Effect of synthesis methods of ZnZrOx oxides associated with SAPO-34 on the production of light olefins by CO2 hydrogenation.

Ananda Vallezi Paladino Lino1*, Elisabete Moreira Assaf2, José Mansur Assaf1 (in memorian)

1Federal University of São Carlos, Chemical Engineering Department, São Carlos, SP 13565-905, Brazil

2University of São Paulo, São Carlos Institute of Chemistry, São Carlos, SP 13566-590, Brazil

*corresponding author: ananda.paladino@ufscar.br

Table S1 Main catalysts reported in literature for the CO2 hydrogenation to light olefins through the methanol mediate route

| Catalyst | T (oC) | P (bar) | H2/CO2 | GHSV (mL.gcat-1.h-1) | XCO2 (%) | SCO (%) | SCH4 (%) | SC2=-C4= (%) | O/P | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ZnO-Y2O3/ SAPO-34 | 390 | 40 | 4 | 1,800 | 27.6 | 85 | 0.3 | 12.6 | 6.5 | [S.1] |
| In2O3-ZrO2/SAPO-34 | 400 | 15 | 3 | 3,000 | 20 | 88 | 0.6 | 10 | 9 | [S.2] |
| CuZnZr@ (Zn-)SAPO-34 | 400 | 20 | 3 | 3,000 | 19.6 | 58.6 | 6 | 25 | 3 | [S.3] |
| ZnZrO2@ Al2O3@SAPO-34 | 380 | 30 | 3 | 3,500 | 13 | 78 | 0.9 | 16 | 4 | [S.4] |
| ZnZrO2@ SAPO-34 | 380 | 30 | 3 | 3,500 | 13 | 55 | 23 | 9.5 | 1.1 | [S.5] |
| ZnZrO2@ SAPO-34 | 380 | 30 | 3 | 3,500 | 20 | 27 | 1.6 | 58.4 | 3.3 | [S.5] |
| GaZrOx/ SAPO-34 | 390 | 30 | 3 | 3,000 | 26 | 52 | 2.5 | 42 | 14 | [S.6] |
| CuCeO2@ SAPO-34 | 360 | 20 | 3 | 18,600 | 8 | 41 | 1.5 | 41 | 2.8 | [S.7] |
| Mn2O3-ZnO/SAPO-34 | 380 | 30 | 3 | 3,600 | 25 | 55 | 1.3 | 36 | 6 | [S.8] |
| NiCu-CeO2/SAPO-34 | 375 | 20 | 3 | 12,000 | 15 | 65 | 0.7 | 27 | 4 | [S.9] |
| CuZn-Kaolin/ SAPO-34 | 400 | 30 | 3 | 1,800 | 50.4 | 7.5 | 12.6 | 65.3 | 4.5 | [S.10] |
| CuZnAl/ SAPO-34 | 380 | 20 | 3 | 3,600 | 30 | 98 | 1.3 | 0.10 | 0.2 | [S.11] |
| ZnZr/SAPO-34 | 380 | 20 | 3 | 3,600 | 15 | 47 | 1.3 | 43 | 5.5 | [S.11] |
| Zn0,3Ce0,2Zr1,8O0,4/ SAPO-34 | 280 | 1 | 3 | 4,800 | 3 | 7.5 | 2.8 | 66 | 70 | [S.12] |
| InCrOx/SAPO-34 | 350 | 35 | 3 | 1,140 | 30 | 60 | 1 | 30 | 4 | [S.13] |
| Ga0,15CrOx/SAPO-34 | 350 | 30 | 3 | 4,000 | 10 | 32 | 1.4 | 54 | 6 | [S.14] |
| ZnZrO2@ SAPO-34 | 380 | 20 | 3 | 4,800 | 15 | 53 | 2.4 | 32.9 | 3.5 | [S.15] |
| ZnZrOx&bio SAPO | 380 | 30 | 3 | 6,000 | 13.4 | 40.2 | 3 | 48.7 | 5 | [S.16] |

Fig. S1 X ray diffraction pattern of the ZZ(CI) sample, as prepared and after calcination, and the respective phase patterns

Fig. S2 O1s XPS spectra of the ZZ samples

Fig. S3 SEM image of the CZA sample

Fig.S4 N2 adsorption/desorption isotherm and pore size distribution (inset) of CZA sample

Fig. S5 Catalysts performances along TOS. P= 20 bar, T= 380o C, GHSV= 2,400 mL.h-1.g-1. ZZ or CZA/ SAPO-34 weight ratio: 3/1.  Activation condition: 150o C, 1 h, N2 (30 mL.min-1), followed by reduction at 400o C, 1 h, H2 (30 mL.min-1).

Fig. S6 Relationship between O/P ratio and physic-chemical properties.

Reference list

[S.1]  Li J, Yu T, Miao D, Pan X, Bao X (2019) Carbon dioxide hydrogenation to light olefins over ZnO-Y2O3 and SAPO-34 bifunctional catalysts. Catal. Comm.. https://doi.org/10.1016/j.catcom.2019.105711

[S.2] Gao J, Jia C, Liu B (2017) Direct and selective hydrogenation of CO2 to ethylene and propene by bifunctional catalysts. Catal Sci. Technol. https://doi.org/10.1039/C7CY01549F

[S.3] Chen J,Wang X, Wu D, Zhang J, Ma Q, Gao X, Lai X, Xia H, Fan S, Zhao TS (2019) Hydrogenation of CO2 to light olefins on CuZnZr@(Zn-)SAPO-34 catalysts: Strategy for product distribution. Fuel. 44-52. https://doi.org/10.1016/j.fuel.2018.10.148

[S.4] Wang G, Wang Y, Cao J, Wang X, Yi Y, Liu F (2020) Fabrication of ZnZrO2@Al2O3@SAPO-34 tandem catalyst for CO2 conversion to hydrocarbons. Microporous Mesoporous Mater. https://doi.org/10.1016/j.micromeso.2019.109693

[S.5] Wang G, Zeng L, Cao J, Liu F, Lin Q, Yi Y, Pan H (2019) Highly selective conversion of CO2 to hydrocarbons over composite catalysts of ZnO-ZrO2 and SAPO-34. Microporous Mesoporous Mater. 284. https://doi.org/10.1016/j.micromeso.2019.04.023

[S.6] Zhang P, Ma L, Meng F, Wang L, Zhang R, Yang G, Li Z (2021) Boosting CO2 hydrogenation performance for light olefin synthesis over GaZrOx combined with SAPO-34. Appl. Catal. B: Environ. https://doi.org/10.1016/j.apcatb.2021.121042

[S.7] Sedighi M, Mohammadi M (2020) CO2 hydrogenation to light olefins over Cu-CeO2/SAPO-34 catalysts: Product distribution and optimization. J. CO2 Util. https://doi.org/10.1016/j.jcou.2019.10.002

[S.8] Mou J, Fan X, Li F, Wang X, Zhao T, Chen P, Li Z, Yang C, Cao J (2021) CO2 hydrogenation to lower olefins over Mn2O3-ZnO/SAPO-34 tandem catalysts. Chem. Eng. J. https://doi.org/10.1016/j.cej.2021.129978

[S.9] Ghasemi M, Mohammadi M, Sedighi M (2020) Sustainable production of light olefins from greenhouse gas CO2 over SAPO-34 supported modified cerium oxide. Microporous Mesoporous Mater. https://doi.org/10.1016/j.micromeso.2020.110029

[S.10] Wang P, Zha F, Yao L, Chang Y (2018) Synthesis of light olefins from CO2 hydrogenation over (CuO-ZnO)-kaolin/SAPO-34 molecular sieves, Appl. Clay Sci. https://doi.org/10.1016/j.clay.2018.06.038

[S.11] Li Z, Wang J, Qu Y, Liu H, Tang C, Miao S, Feng Z, An H,  Li C (2017) Highly Selective Conversion of Carbon Dioxide to Lower Olefins. ACS Catal. https://doi.org/10.1021/acscatal.7b03251

[S.12] Zhang L, Geng B, Wang P, Kang H, Xiao H, Jia J, Wu H (2023) Highly efficient ZnCeZrOx/SAPO-34 catalyst for the direct conversion of CO2 into light olefins under mild reaction conditions. Appl. Catal. A: Gen. https://doi.org/10.1016/j.apcata.2023.119141

[S.13] Wang S, Wang P, Qin Z, Yan W, Dong M, Li J, Wang J, Fan W (2020) Enhancement of light olefin production in CO2 hydrogenation over In2O3-based oxide and SAPO-34 composite. J. Catal. https://doi.org/10.1016/j.jcat.2020.09.010

[S.14] Zhang W, Wang S, Guo S, Qin Z, Dong M, Fan W, Wang J (2022) GamCrOx/H-SAPO-34(F), a highly efficient bifunctional catalyst for the direct conversion of CO2 into ethene and propene. Fuel. https://doi.org/10.1016/j.fuel.2022.125475

[S.15] Lu P, Chang X, Yu W, Hu Q, Ali KM, Xing C, Du C, Yang Z, Chen S (2023) Synergistic effects of ZnO–ZrO2@SAPO-34 core-shell catalyst in catalyzing CO2 hydrogenation for the synthesis of light olefins. Renew. Energy. https://doi.org/10.1016/j.renene.2023.03.111

[S.16] Yang S, Song J, Yue Y, Chen B, Ali S, Tan KB, Tian J, Huang J, Li Q, Zhan G (2026) Tuning zeolite crystal size in bifunctional catalysts assembled on bio-SiO2 for enhanced CO2 hydrogenation to light olefins. Chem. Eng. Sci. https://doi.org/10.1016/j.ces.2025.122468