Supporting information for:

The relationship between fibre composition and material properties following periodate oxidation and borohydride reduction of a range of wood-based fibres

Verónica López Durán1,2, Per A. Larsson1,2, Lars Wågberg1,2,3

1Fibre and Polymer Technology, KTH Royal Institute of Technology, SE-10044 Stockholm, Sweden

2 BiMaC Innovation, KTH Royal Institute of Technology, SE-10044, Sweden

3 Wallenberg Wood Science Center, KTH Royal Institute of Technology, SE-10044, Sweden

- Crystallinity index (%) and crystalline width (nm) of fibres:

|  |  | Crystallinity index (%) | FWHM | Crystalline width (nm) |
| --- | --- | --- | --- | --- |
| Bleached chemical | 0 | 82,8 | 2,0 | 4,1 |
|  | 6 | 76,2 | 2,2 | 3,6 |
|  | 6+1 | 80,6 | 2,1 | 3,9 |
|  | 12 | 61,4 | 2,7 | 3,0 |
|  | 12+1 | 74,6 | 2,2 | 3,7 |
| Dissolving grade | 0 | 82,3 | 1,9 | 4,2 |
|  | 6 | 77,3 | 2,1 | 3,9 |
|  | 6+1 | 80,5 | 2,0 | 4,0 |
|  | 12 | 73,4 | 2,2 | 3,6 |
|  | 12+1 | 81,3 | 2,0 | 4,1 |
| Unbleached chemical | 0 | 79,3 | 2,3 | 3,5 |
|  | 6 | 70,0 | 2,6 | 3,1 |
|  | 6+1 | 77,0 | 2,4 | 3,4 |
|  | 12 | 60,6 | 2,9 | 2,8 |
|  | 12+1 | 72,5 | 2,5 | 3,3 |
| CTMP fibres | 0 | 78,5 | 2,1 | 3,9 |
|  | 6 | 73,2 | 2,3 | 3,6 |
|  | 6+1 | 77,0 | 2,1 | 3,8 |
|  | 12 | 68,3 | 2,4 | 3,3 |
|  | 12+1 | 73,6 | 2,3 | 3,6 |
|  | 24 | 55,8 | 2,9 | 2,8 |
|  | 24+1 | 63,9 | 2,5 | 3,2 |

- SEM images:

| Sample | Reference | 6 h oxidation | 6 h oxidation and 1 h reduction | 12 h oxidation | 12 h oxidation and 1 h reduction |
| --- | --- | --- | --- | --- | --- |
| Bleached chemical |  |  |  |  |  |
| Dissolving grade |  |  |  |  |  |
| Unbleached chemical |  |  |  |  |  |

| Sample | Reference | 6 h oxidation | 6 h oxidation and 1 h reduction | 12 h oxidation | 12 h oxidation and 1 h reduction |
| --- | --- | --- | --- | --- | --- |
| CTMP fibres |  |  |  |  |  |
|  | 24 h oxidation | 24 h oxidation and 1 h reduction |  |  |  |