Tailoring Flame-Retardancy and Strength of Papers via Layer-by-Layer Treatment of Cellulose Fibers

Oruç Köklükaya*, †, Federico Carosio‡ and Lars Wågberg*, †, ᵮ

†Fiber and Polymer Technology, KTH Royal Institute of Technology,

Teknikringen 56, SE-100 44 Stockholm, Sweden

‡Dipartimento di Scienza Applicata e Tecnologia, Politecnico di Torino, Alessandria Site

Viale Teresa Michel 5, 15121, Alessandria, Italy

ᵮWallenberg Wood Science Center, KTH Royal Institute of Technology,

SE-100 44 Stockholm, Sweden

Corresponding authors:

Oruҫ Köklükaya

ORCID ID 0000-0001-9856-6536

E-mail: oruc@kth.se

Phone: +46-8-790 82 96

Lars Wågberg

ORCID ID 0000-0001-8622-0386

E-mail: wagberg@kth.se

Phone: +46-8-790 82 94

Supplementary material

Fig. S 1 The density of papers prepared from untreated and LbL-treated fibers

Fig. S 2 Nitrogen analysis calibration curves for a) low molecular mass PEI and b) high molecular mass PEI

Fig. S 3 SEM images of  a) cellulose fibers and b) carboxymethylated fiber and corresponding high magnification images.

Table S 1 The average roughness value (Rq) of PEI/SHMP thin films deposited on model cellulose and CM-cellulose surfaces as a function of bilayer number

| Sample | Model cellulose surface roughness [nm] | Model CM-cellulose surface roughness [nm] |
| --- | --- | --- |
| Reference | 8.5 ± 0.4 | 8.0 ± 0.1 |
| LMw-PEI/SHMP-3.5BL | 8.0 ± 0.0 | 11.8 ± 2.0 |
| HMw-PEI/SHMP-3.5BL | 8.7 ± 0.3 | 25.5 ± 0.8 |