Direct sulfation of cellulose fibers using a reactive deep eutectic solvent to produce highly charged cellulose nanofibers

Juho Antti Sirviö,* Jonne Ukkola, Henrikki Liimatainen

Fibre and Particle Engineering Research Unit, University of Oulu, P.O. Box 4300, 90014 Oulu, Finland E-mail: juho.sirvio@oulu.fi

Figure S1. The size distribution of SCNF calculated from TEM image

Figure S2. Viscosities of the SCNFs 0.3% solutions in the presence of various metal salts (1 mM) as a function of shear rate (0.1-1000 s-1).

Table S2. Viscosities of the SCNFs 0.3% solutions in the presence of various metal salts (1 mM) at shear rate of 1 s-1 and ration between viscosities with and without the presence of metal salts.

|  | Viscosity (Pa s) | Viscositya/Viscosityb |  |
| --- | --- | --- | --- |
| SCNF 0.3% | 2.52 |  |  |
| NaCl | 1.52 | 0.6 |  |
| CaCl2 | 1.75 | 0.7 |  |
| AlCl3 | 1.35 | 0.8 |  |
| FeCl3 | 1.98 | 0.8 |  |
| FeSO4 | 1.52 | 0.6 |  |
| CuSO4 | 1.46 | 0.6 |  |

a = Viscosity of 0.3% SCNF solution in presence of 1 mM salt

b = Viscosity of 0.3% solution without addition of salt