Title

# Development and mining of a database of historic European paper properties

Authors

Matija Strlič, Yun Liu, Dirk Lichtblau, Gerrit De Bruin, Barry Knight, Thea Winther, Irena Kralj Cigić, Richard G. Brereton

Supplementary Material

Spearman’s correlation coefficients have been calculated to account to possible non-linear relationships between data. Tables. S.1-4 present the coefficients on pairwise sets of variables. Tabs. S.5-8 present the number of samples used for the calculation of the corresponding coefficients. Figs. S.1-41 present scatterplots for pairs of variables where ρ2 > 0.25. All the plots are colour coded as follows: blue for bleached, red for gelatin and green for groundwood.

Table S.1: Spearman’s correlation coefficients on pairwise sets of variables for all samples.

|  | dat | lig | pH | dp | MW | ash | Al | car | ros | pro | grm | TS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| dat | 1 | 0.1598 | 0.1802 | 0.4525 | 0.4183 | -0.0172 | -0.0847 | -0.2568 | -0.2125 | -0.4072 | 0.0764 | 0.3013 |
| lig |  | 1 | -0.4717 | -0.3145 | -0.2405 | 0.4969 | 0.1023 | 0.5325 | 0.5054 | -0.5563 | -0.3594 | -0.4224 |
| pH |  |  | 1 | 0.6209 | 0.4547 | -0.2505 | -0.2466 | -0.5942 | -0.461 | 0.2188 | 0.1842 | 0.3802 |
| dp |  |  |  | 1 | 0.7805 | -0.3712 | -0.3710 | -0.7606 | -0.5066 | 0.1936 | -0.0643 | 0.6130 |
| MW |  |  |  |  | 1 | -0.2915 | -0.2859 | -0.5690 | -0.4387 | 0.1501 | 0.0172 | 0.3132 |
| ash |  |  |  |  |  | 1 | 0.1729 | 0.3675 | 0.4957 | -0.5427 | 0.0887 | -0.1985 |
| Al |  |  |  |  |  |  | 1 | 0.2978 | 0.4020 | -0.1148 | 0.0623 | -0.0146 |
| car |  |  |  |  |  |  |  | 1 | 0.5934 | -0.4442 | -0.1471 | -0.4257 |
| ros |  |  |  |  |  |  |  |  | 1 | -0.5331 | -0.1369 | -0.2077 |
| pro |  |  |  |  |  |  |  |  |  | 1 | 0.0971 | 0.2347 |
| grm |  |  |  |  |  |  |  |  |  |  | 1 | 0.5326 |
| TS |  |  |  |  |  |  |  |  |  |  |  | 1 |

Table S.2: Spearman’s correlation coefficients on pairwise sets of variables for all bleached samples.

|  | dat | lig | pH | dp | MW | ash | Al | car | ros | pro | grm | TS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| dat | 1 | 0.0372 | 0.3655 | 0.6832 | 0.6239 | -0.1296 | -0.1296 | -0.5615 | -0.3656 | NaN | 0.065 | 0.5504 |
| lig |  | 1 | -0.3082 | -0.1396 | -0.0686 | 0.2775 | 0.2024 | 0.1548 | 0.2934 | NaN | 0.0001 | -0.1353 |
| pH |  |  | 1 | 0.6049 | 0.4406 | -0.1904 | -0.2750 | -0.5534 | -0.5213 | NaN | -0.0663 | 0.3736 |
| dp |  |  |  | 1 | 0.7468 | -0.3448 | -0.2775 | -0.7151 | -0.4744 | NaN | -0.0821 | 0.5742 |
| MW |  |  |  |  | 1 | -0.2243 | -0.1367 | -0.6268 | -0.4111 | NaN | 0.0222 | 0.3566 |
| ash |  |  |  |  |  | 1 | 0.0912 | 0.1557 | 0.2275 | NaN | 0.1300 | -0.1558 |
| Al |  |  |  |  |  |  | 1 | 0.3363 | 0.3367 | NaN | 0.0006 | -0.1328 |
| car |  |  |  |  |  |  |  | 1 | 0.5239 | NaN | 0.1016 | -0.3567 |
| ros |  |  |  |  |  |  |  |  | 1 | NaN | 0.0209 | -0.1373 |
| pro |  |  |  |  |  |  |  |  |  | NaN | NaN | NaN |
| grm |  |  |  |  |  |  |  |  |  |  | 1 | 0.4123 |
| TS |  |  |  |  |  |  |  |  |  |  |  | 1 |

Table S.3: Spearman’s correlation coefficients on pairwise sets of variables for gelatine samples.

|  | dat | lig | pH | dp | MW | ash | Al | car | ros | pro | grm | TS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| dat | 1 | 0.0668 | -0.5858 | -0.4108 | -0.0933 | 0.0805 | 0.6306 | 0.2525 | 0.3164 | -0.0868 | 0.0490 | -0.2994 |
| lig |  | 1 | -0.1568 | -0.1955 | -0.1644 | -0.1582 | -0.0275 | 0.0797 | 0.2618 | -0.0172 | -0.2199 | -0.4688 |
| pH |  |  | 1 | 0.5230 | 0.2300 | 0.0811 | -0.2563 | -0.2587 | -0.5029 | -0.1563 | 0.5263 | -0.1085 |
| dp |  |  |  | 1 | 0.7820 | 0.1054 | -0.3056 | -0.6154 | -0.2944 | -0.0138 | -0.0572 | 0.3429 |
| MW |  |  |  |  | 1 | 0.0238 | -0.3461 | -0.6252 | -0.0173 | 0.0783 | -0.1681 | 0.6321 |
| ash |  |  |  |  |  | 1 | 0.1968 | -0.0251 | -0.0356 | -0.0815 | 0.0614 | 0.5128 |
| Al |  |  |  |  |  |  | 1 | 0.1623 | -0.0143 | 0.4330 | -0.3446 | 0.2000 |
| car |  |  |  |  |  |  |  | 1 | 0.0131 | -0.2776 | 0.3033 | -0.2460 |
| ros |  |  |  |  |  |  |  |  | 1 | 0.0999 | -0.4290 | 0.0255 |
| pro |  |  |  |  |  |  |  |  |  | 1 | -0.1807 | 0.5623 |
| grm |  |  |  |  |  |  |  |  |  |  | 1 | 0.5385 |
| TS |  |  |  |  |  |  |  |  |  |  |  | 1 |

Table S.4: Spearman’s correlation coefficients on pairwise sets of variables for groundwood samples.

|  | dat | lig | pH | dp | MW | ash | Al | car | ros | pro | grm | TS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| dat | 1 | 0.1678 | 0.0308 | 0.0714 | 0.2663 | -0.1791 | -0.1952 | -0.1917 | -0.4722 | -0.1444 | -0.0459 | 0.0958 |
| lig |  | 1 | -0.3471 | -0.5714 | 0.1826 | -0.2613 | -0.3094 | 0.2102 | -0.2844 | -0.0278 | -0.3466 | -0.274 |
| pH |  |  | 1 | -0.3571 | 0.2981 | 0.1343 | -0.0718 | -0.4842 | -0.0632 | -0.0515 | 0.1042 | 0.3099 |
| dp |  |  |  | 1 | -0.0357 | 0.1190 | 0.6905 | 0.0476 | 0.2381 | NaN | 0.4000 | 0.5000 |
| MW |  |  |  |  | 1 | -0.1538 | -0.3788 | -0.2933 | -0.3798 | -0.1450 | -0.1586 | 0.1297 |
| ash |  |  |  |  |  | 1 | 0.0195 | -0.1671 | 0.0587 | -0.1089 | 0.3584 | 0.0211 |
| Al |  |  |  |  |  |  | 1 | 0.1353 | 0.4802 | 0.0811 | 0.1695 | -0.0228 |
| car |  |  |  |  |  |  |  | 1 | 0.1697 | 0.1025 | -0.1223 | -0.2942 |
| ros |  |  |  |  |  |  |  |  | 1 | 0.1100 | -0.0319 | -0.0955 |
| pro |  |  |  |  |  |  |  |  |  | 1 | -0.1148 | NaN |
| grm |  |  |  |  |  |  |  |  |  |  | 1 | 0.5924 |
| TS |  |  |  |  |  |  |  |  |  |  |  | 1 |

Table S.5: Number of samples used in the Spearman’s correlation analysis on pairwise sets of variables for all samples.

|  | dat | lig | pH | dp | MW | ash | Al | car | ros | pro | grm | TS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| dat | 597 | 467 | 593 | 332 | 518 | 573 | 566 | 587 | 585 | 597 | 444 | 300 |
| lig |  | 556 | 553 | 300 | 462 | 543 | 534 | 553 | 550 | 534 | 389 | 266 |
| pH |  |  | 725 | 443 | 616 | 699 | 693 | 713 | 711 | 695 | 499 | 330 |
| dp |  |  |  | 446 | 375 | 427 | 424 | 441 | 438 | 428 | 254 | 175 |
| MW |  |  |  |  | 616 | 598 | 589 | 609 | 609 | 588 | 442 | 287 |
| ash |  |  |  |  |  | 702 | 678 | 697 | 694 | 673 | 482 | 322 |
| Al |  |  |  |  |  |  | 697 | 691 | 687 | 668 | 483 | 316 |
| car |  |  |  |  |  |  |  | 717 | 708 | 688 | 494 | 326 |
| ros |  |  |  |  |  |  |  |  | 715 | 686 | 495 | 328 |
| pro |  |  |  |  |  |  |  |  |  | 699 | 481 | 316 |
| grm |  |  |  |  |  |  |  |  |  |  | 501 | 311 |
| TS |  |  |  |  |  |  |  |  |  |  |  | 330 |

Table S.6: Number of samples used in the Spearman’s correlation analysis on pairwise sets of variables for bleached samples.

|  | dat | lig | pH | dp | MW | ash | Al | car | ros | pro | grm | TS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| dat | 301 | 195 | 299 | 281 | 269 | 285 | 279 | 295 | 292 | NaN | 205 | 147 |
| lig |  | 208 | 207 | 195 | 186 | 201 | 192 | 205 | 203 | NaN | 134 | 98 |
| pH |  |  | 321 | 301 | 289 | 305 | 299 | 314 | 311 | NaN | 215 | 154 |
| dp |  |  |  | 303 | 274 | 287 | 284 | 300 | 295 | NaN | 210 | 151 |
| MW |  |  |  |  | 289 | 275 | 268 | 284 | 284 | NaN | 199 | 140 |
| ash |  |  |  |  |  | 306 | 287 | 302 | 300 | NaN | 205 | 149 |
| Al |  |  |  |  |  |  | 301 | 296 | 293 | NaN | 206 | 147 |
| car |  |  |  |  |  |  |  | 316 | 309 | NaN | 213 | 152 |
| ros |  |  |  |  |  |  |  |  | 313 | NaN | 212 | 153 |
| pro |  |  |  |  |  |  |  |  |  | NaN | NaN | NaN |
| grm |  |  |  |  |  |  |  |  |  |  | 216 | 149 |
| TS |  |  |  |  |  |  |  |  |  |  |  | 154 |

Table S.7: Number of samples used in the Spearman’s correlation analysis on pairwise sets of variables for gelatine samples.

|  | dat | lig | pH | dp | MW | ash | Al | car | ros | pro | grm | TS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| dat | 46 | 40 | 46 | 44 | 34 | 43 | 43 | 44 | 46 | 46 | 12 | 8 |
| lig |  | 98 | 98 | 97 | 60 | 97 | 97 | 98 | 98 | 98 | 23 | 20 |
| pH |  |  | 137 | 135 | 96 | 134 | 134 | 135 | 137 | 137 | 40 | 21 |
| dp |  |  |  | 135 | 94 | 132 | 132 | 133 | 135 | 135 | 40 | 21 |
| MW |  |  |  |  | 96 | 95 | 95 | 95 | 96 | 96 | 33 | 15 |
| ash |  |  |  |  |  | 134 | 134 | 134 | 134 | 134 | 38 | 20 |
| Al |  |  |  |  |  |  | 134 | 134 | 134 | 134 | 38 | 20 |
| car |  |  |  |  |  |  |  | 135 | 135 | 135 | 38 | 20 |
| ros |  |  |  |  |  |  |  |  | 137 | 137 | 40 | 21 |
| pro |  |  |  |  |  |  |  |  |  | 137 | 40 | 21 |
| grm |  |  |  |  |  |  |  |  |  |  | 40 | 13 |
| TS |  |  |  |  |  |  |  |  |  |  |  | 21 |

Table S.8: Number of samples used in the Spearman’s correlation analysis on pairwise sets of variables for groundwood samples.

|  | dat | lig | pH | dp | MW | ash | Al | car | ros | pro | grm | TS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| dat | 250 | 232 | 248 | 7 | 215 | 245 | 244 | 248 | 247 | 250 | 227 | 145 |
| lig |  | 250 | 248 | 8 | 216 | 245 | 245 | 250 | 249 | 238 | 232 | 148 |
| pH |  |  | 267 | 7 | 231 | 260 | 260 | 264 | 263 | 254 | 244 | 155 |
| dp |  |  |  | 8 | 7 | 8 | 8 | 8 | 8 | NaN | 4 | 3 |
| MW |  |  |  |  | 231 | 228 | 226 | 230 | 229 | 219 | 210 | 132 |
| ash |  |  |  |  |  | 262 | 257 | 261 | 260 | 250 | 239 | 153 |
| Al |  |  |  |  |  |  | 262 | 261 | 260 | 250 | 239 | 149 |
| car |  |  |  |  |  |  |  | 266 | 264 | 254 | 243 | 154 |
| ros |  |  |  |  |  |  |  |  | 265 | 253 | 243 | 154 |
| pro |  |  |  |  |  |  |  |  |  | 256 | 233 | NaN |
| grm |  |  |  |  |  |  |  |  |  |  | 245 | 149 |
| TS |  |  |  |  |  |  |  |  |  |  |  | 155 |

| Figure S.1 |  |
| --- | --- |
| Figure S.2 |  |
| Figure S.3 |  |
| Figure S.4 |  |
| Figure S.5 |  |
| Figure S.6 |  |
| Figure S.7 |  |
| Figure S.8 |  |
| Figure S.9 |  |
| Figure S.10 |  |
| Figure S.11 |  |
| Figure S.12 |  |
| Figure S.13 |  |
| Figure S.14 |  |
| Figure S.15 |  |
| Figure S.16 |  |
| Figure S.17 |  |
| Figure S.18 |  |
| Figure S.19 |  |
| Figure S.20 |  |
| Figure S.21 |  |
| Figure S.22 |  |
| Figure S.23 |  |
| Figure S.24 |  |
| Figure S.25 |  |
| Figure S.26 |  |
| Figure S.27 |  |
| Figure S.28 |  |
| Figure S.29 |  |
| Figure S.30 |  |
| Figure S.31 |  |
| Figure S.32 |  |
| Figure S.33 |  |
| Figure S.34 |  |
| Figure S.35 |  |
| Figure S.36 |  |
| Figure S.37 |  |
| Figure S.38 |  |
| Figure S.39 |  |
| Figure S.40 |  |
| Figure S.41 |  |