Supporting information

Superbase-Based Protic Ionic Liquids for Cellulose Filament Spinning

Sherif Elsayed, Michael Hummel, Daisuke Sawada, Chamseddine Guizani, Marja Rissanen and Herbert Sixta

Department of Bioproducts and Biosystems, Aalto University, P.O. Box 16300, FI-00076 Aalto, Finland.

E-mail: sherif.elsayed@aalto.fi, michael.hummel@aalto.fi, daisuke.sawada@aalto.fi, chamseddine.guizani@aalto.fi, marja.rissaned@aalto.fi, herbert.sixta@aalto.fi.

Contents

X-ray diffraction	2

Rheological properties	2

Tensile properties	5

Number of pages: 05

Number of figures: 03

Number of tables: 02

NMMO - fibers

[DBNH]OAc - fibers

[DBUH]OAc - fibers

a

b

c

Fig. S1  X-ray diffraction patterns of the fibers at DR 12 a. Raw scattering profiles from 5° to 60° 2θ b. Amorphous scattering c. Fittings of corrected profiles showing the crystalline peaks

[mTBDH]OAc - fibers

(1-10)

(002)

(020)

(110)

Intensity (a.u.)

Intensity (a.u.)

Intensity (a.u.)

Intensity (a.u.)

Intensity (a.u.)

Intensity (a.u.)

Intensity (a.u.)

Intensity (a.u.)

Corrected data for empty scattering

Amorphous BKG

Subtracted data

Corrected data for empty scattering

Amorphous BKG

Subtracted data

Corrected data for empty scattering

Amorphous BKG

Subtracted data

Corrected data for empty scattering

Amorphous BKG

Subtracted data

2θ (°)

2θ (°)

X-ray diffraction

Table S1  Crystal width of the equatorial lattice of the measured fibers

| Draw ratio | NMMO | [DBNH]OAc | [DBUH]OAc | [mTBD]OAc |
| --- | --- | --- | --- | --- |
|  | Crystal width (CWhkl), Å |  |  |  |
| 2 | 30.0 | 34.8 | 35.5 | 35.0 |
| 5 | 32.0 | 34.7 | 34.2 | 35.2 |
| 12 | 33.5 | 34.9 | 35.6 | 35.2 |

# Rheological properties

Fig. S2 shows a higher zero-shear viscosity for the NMMO and [DBUH]OAc solutions followed by the [mTBDH]OAc solution, while [DBNH]OAc solution depicted the lowest zero shear viscosity.

Fig. S2  Zero-shear viscosity (η0) of the NMMO, [DBUH]OAc, [mTBDH]OAc and [DBNH]OAc cellulose solutions at different measured temperatures

Table S2  Zero-shear viscosity (η0). cross-over points (COP) and angular frequencies for the cellulose solutions at different measured temperatures

| [DBUH]OAc |  |  |  | [mTBD]OAc |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Temperature | η0 | Angular frequency | COP | Temperature | η0 | Angular frequency | COP |
| °C | Pa.s | 1/s | Pa | °C | Pa.s | 1/s | Pa |
| 80 | 60800 | 0.27 | 3500 | 85 | 28400 | 0.83 | 3900 |
| 85 | 40800 | 0.47 | 3600 | 70 | 66500 | 0.26 | 4100 |
| 90 | 29100 | 0.72 | 3700 | 80 | 37700 | 0.59 | 3800 |
| 95 | 21900 | 1.02 | 3600 | 85 | 28400 | 0.83 | 3900 |
| 100 | 16800 | 1.38 | 3600 | 90 | 21500 | 1.14 | 3900 |
| 105 | 13400 | 1.81 | 3700 | 95 | 16300 | 1.56 | 4000 |
| 110 | 12400 | 2.26 | 3800 | 105 | 9700 | 2.76 | 4100 |
| NMMO |  |  |  | [DBNH]OAc |  |  |  |
| Temperature | η0 | Angular frequency | COP | Temperature | η0 | Angular frequency | COP |
| °C | Pa.s | 1/s | Pa | °C | Pa.s | 1/s | Pa |
| 80 | 52100 | 0.43 | 4100 | 70 | 49000 | 0.4 | 3500 |
| 90 | 30400 | 0.86 | 4400 | 80 | 29000 | 0.8 | 3800 |
| 95 | 22800 | 1.17 | 4400 | 90 | 16700 | 1.46 | 3800 |
| 100 | 17500 | 1.58 | 4500 | 100 | 9700 | 2.65 | 3900 |
| 105 | 13500 | 2.08 | 4500 |  |  |  |  |
| 110 | 10200 | 2.78 | 4500 |  |  |  |  |
| 115 | 8200 | 3.61 | 4600 |  |  |  |  |
| [emim]OAc |  |  |  |  |  |  |  |
| Temperature | η0 | Angular frequency | COP |  |  |  |  |
| °C | Pa.s | 1/s | Pa |  |  |  |  |
| 40 | 42700 | 0.35 | 2800 |  |  |  |  |
| 45 | 31700 | 0.51 | 2800 |  |  |  |  |
| 50 | 22500 | 0.75 | 2800 |  |  |  |  |
| 55 | 15700 | 1.13 | 2900 |  |  |  |  |
| 60 | 11000 | 1.68 | 2900 |  |  |  |  |
| 65 | 7900 | 2.45 | 3000 |  |  |  |  |
| 70 | 5600 | 3.49 | 3100 |  |  |  |  |
| 80 | 4100 | 4.90 | 3100 |  |  |  |  |
| 85 | 3000 | 6.80 | 3200 |  |  |  |  |
| 90 | 2100 | 9.60 | 3200 |  |  |  |  |
| 95 | 1500 | 13.73 | 3300 |  |  |  |  |
| 105 | 1126 | 19.45 | 3363 |  |  |  |  |

# Tensile properties

Fig. S3  Titer of the fibers spun from NMMO, [DBUH]OAc, [mTBDH]OAc and [DBNH]OAc

The development of the fiber titers as they are stretched from DR 3 to 12 is depicted in Fig. S3. One can observe that upon increasing DR the diameter of the fibers spun from different solvents (illustrated as titer) reached similar values in the range of 1.2 – 1.3 dtex at DR 12.