Molecular and Crystal Structures of Cellulose in Severely Deteriorated Archaeological Wood

Juan Guoa, Jiabao Chena, Qiulu Menga,e, Leon Ploszczanskib, Jian’an Liuc, Rupeng Luoc, Tao Jind, Philipp Siedlaczekb, Helga C. Lichteneggerb, Yafang Yina*, Harald Rennhoferb*

aResearch Institute of Wood Industry, Chinese Academy of Forestry, Beijing 100091, China; Wood Collection of Chinese Academy of Forestry, Beijing 100091, China

bInstitute of Physics and Materials Science, Department of Material Sciences and Process Engineering, University of Natural Resources and Life Sciences (BOKU), Vienna 1180, Austria

cZhejiang Provincial Institute of Cultural Relics and Archaeology, Jiaogong road No.71, Hangzhou 310012, Zhejiang, China

dNingbo Municipal Institute of Cultural Heritage Management, Baoshan Road No. 180, Ningbo 315012, Zhejiang, China

eSchool of Resources, Environment and Materials, Guangxi University, No. 100 Daxue East Road, Nanning 530004, China

Table S1 Peak assignments for FTIR spectra of recent wood (Faix 1991; Pandey and Pitman 2003; Darwish et al 2013; Guo et al. 2019; Pozhidaev et al 2019)

| Peak position (cm-1) | Peak assignments |
| --- | --- |
| 3700-3000 | different inter- and intramolecular hydrogen bonds among cell wall components |
| 3000-2800 | C-H stretch in methyl and methylene groups |
| 1740 | C=O stretching of acetyl and carbonyl groups in hemicelluloses |
| 1660 | conjugated C=O stretch in lignin |
| 1592 | aromatic skeletal vibrations, together with C=O stretch in lignin |
| 1505 | aromatic skeletal vibrations in lignin |
| 1462 | aromatic C-H deformation in lignin and carbohydrates |
| 1420 | C-H deformation in lignin and carbohydrates |
| 1416 | aromatic skeletal vibrations combined with C-H in-plane deform |
| 1374 | C-H bending in carbohydrates |
| 1330 | C-H vibration in cellulose and C1-O vibration in syringyl derivatives |
| 1315 | wagging (out of the plane) of CH2 groups in crystalline cellulose |
| 1270 | aromatic C-O stretching vibrations of methoxyl and phenyl propane guaiacol ring units of lignin |
| 1214 | aromatic C-O stretching vibration in syringol rings of lignin |
| 1158 | asymmetric bridge C-O-C stretch mode in carbohydrates |
| 1126 | C-H in plane deformation in syringyl monomer |
| 1052 | C-O stretching in carbohydrates |
| 1032 | C-H deformation in guaiacyl unit, with C-O deformation in prim. alc. |
| 896 | C-H vibrational mode in carbohydrates |

Table S2 Sugar composition (%)a of benzene ethanol extracted archaeological and non-degraded wood samples as determined by HPLCb

|  | Fuc | Rha | Gal-UA | Gul-UA | Glc-UA |
| --- | --- | --- | --- | --- | --- |
| C1 | 0.05±0.003 | 0.2±0.02 | 0.6±0.04 | 0.04±0.0002 | 0.02±0.0003 |
| C2 | 0.04±0.002 | 0.3±0.01 | 0.6±0.01 | 0.1±0.004 | 0.02±0.0004 |
| C3 | 0.04±0.0004 | 0.2±0.0005 | 0.5±0.005 | 0.03±0.002 | 0.02±0.0005 |
| C4 | 0.03±0.002 | 0.4±0.06 | 0.7±0.003 | 0.2±0.002 | 0.03±0.003 |
| C6 | 0.08±0.003 | 0.3±0.02 | 0.7±0.02 | 0.05±0.0004 | 0.02±0.0004 |
| C8 | ndd | 0.1±0.004 | 0.3±0.02 | 0.3±0.005 | 0.04±0.001 |
| C9 | 0.02±0.00008 | 0.4±0.006 | 0.4±0.007 | 0.5±0.007 | 0.03±0.0003 |
| C10 | nd | 0.5±0.003 | 0.9±0.01 | 0.6±0.02 | 0.06±0.001 |
| C12 | nd | 0.03±0.002 | 0.2±0.01 | 0.2±0.01 | nd |

a Data are expressed as a percentage based on dry weight of benzene ethanol extracted wood samples;

b Data are mean values of duplicate analysis ± standard deviation;

c Fuc: fucose; Rha: rhamnose; Gal-UA: galacturonic acid; Gul-UA: guluronic acid; Glc-UA: glucuronic acid;

d nd: not detected

Table S3 Resonance assignments of solid state 13C CP/MAS NMR spectra of recent wood (Alesiani et al. 2005; Bardet et al. 2002; Preston et al. 2009; Proietti et al 2011; Łucejko et al. 2012; Zoia et al. 2017; Zborowska et al. 2019; Lucejko et al. 2021; Spinella et al 2021; Wikberg and Maunu 2004)

| Resonance number | Chemical shift (ppm) | assignmentsa |
| --- | --- | --- |
| 16 | 175 | Carboxyl region includes carboxylic acids, amides and esters |
| 15 | 172 | Carbohydrates: -COO-R, CH3-COO- |
| 14 | 154 | Lignin: S3 (e), S5 (e) |
| 13 | 148 | Lignin: S3 (ne), S5 (ne), G1, G4 |
| 12 | 137-133 | Lignin: S1 (e), S4 (e), G1 (e), S1 (ne), S4 (ne), G1 (e) |
| 11 | 121 | Lignin: G6 |
| 10 | 114-106 | Lignin: G6, G5, S2, S6 |
| 9 | 105 | Carbohydrate: C1 |
| 8 | 89 | Carbohydrates: C4 |
| 7 | 84 | Lignin: Cβ in β-O-4 linked side chain; Carbohydrates: C4 |
| 6 | 75 | Lignin: Cα-OH in β-O-4 linked side chain of lignins; Carbohydrates: C2,3,5 |
| 5 | 72 | Carbohydrates: C2,3,5 |
| 4 | 65 | Carbohydrates: C6 |
| 3 | 62 | Lignins: Cγ |
| 2 | 56 | Lignin: OCH3 |
| 1 | 21 | Polysaccharides: CH3-COO- [methyl carbon in hemicellulose acetyl groups] |

a S: syringyl (aromatic unit with two methoxyl groups); G: guaiacyl (aromatic unit with only one methoxyl); ne: in non-etherified arylglycerol β-aryl ethers; e: in etherified arylglycerol β-aryl ethers.

Fig. S1 Scattering curves I(χ) of (A, B) C7, (C, D) C8, (E, F) C9, (G, H) C10, (I, J) C11, and (K, L) C12

Fig. S2 The results from the spectral fitting of the solid state 13C CP/MAS NMR spectra of wood samples (A, B) C1, (C, D) C2, (E, F) C3, (G, H) C4, (I, J) C9, and (K, L) C10. The black lines represent the experimental spectra. The fitted lines are shown as green solid lines, and cumulative fitting lines are depicted in red dotted lines.

Fig. S3 SAXS curve fit results using the software SASfit (Breβler, Kohlbrecher, Thünemann 2015) in order to obtain values of mean fibril diameter (D0), diameter distribution (σ) and the inter-fibril distance DF. The fit was applied to data of C7 – C12 in the range of about q = 0.7 to 5 nm-1. The dots are measured data of the scattering intensity of dried C7 (A) and dried C12 (B). Whereas the line is the corresponding curve fitting profile.