S2 supplementary information

Determination of A and K parameters for the calculation of the IPDT values

IPDT=A.KTf-Ti+Ti

A=S1+S2S1+S2+S3

K=S1+S2S1

where Ti and Tf are the initial and final experimental temperatures of the TGA curve, respectively. Graphical representations of the areas S1, S2, and S3 are depicted in the following figure.

| Sample | Doyle’s Parameters |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | S1 | S2 | S3 | A | K | Tf | Ti |
| Xa | 8170 | 12819 | 15393 | 0.5769 | 2.57 | 600 | 180 |
| CMC | 7069 | 16352 | 15600 | 0.6002 | 3.31 | 600 | 180 |
| CMC/Xa | 7620 | 14586 | 15496 | 0.5890 | 2.91 | 600 | 180 |
| ZnO-NPs | 1957 | 33595 | 4945 | 0.8779 | 18.16 | 600 | 180 |
| CMC/Xa/1ZnO | 6966 | 18551 | 12781 | 0.6663 | 3.66 | 600 | 180 |
| CMC/Xa/3ZnO | 6464 | 20864 | 11317 | 0.7072 | 4.23 | 600 | 180 |
| CMC/Xa/5ZnO | 6066 | 23073 | 9845 | 0.7475 | 4.80 | 600 | 180 |