S2 supplementary information

Determination of A and K parameters for the calculation of the IPDT values



where Ti and Tf are the initial and final experimental temperatures of the TGA curve, respectively. Graphical representations of the areas S1, S2, and S3 are depicted in the following figure.
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	Sample
	Doyle’s Parameters

	
	S1
	S2
	S3
	A
	K
	Tf
	Ti

	Xa
	8170
	12819
	15393
	0.5769
	2.57
	600
	180

	CMC
	7069
	16352
	15600
	0.6002
	3.31
	600
	180

	CMC/Xa
	7620
	14586
	15496
	0.5890
	2.91
	600
	180

	ZnO-NPs
	1957
	33595
	4945
	0.8779
	18.16
	600
	180

	CMC/Xa/1ZnO
	6966
	18551
	12781
	0.6663
	3.66
	600
	180

	CMC/Xa/3ZnO
	6464
	20864
	11317
	0.7072
	4.23
	600
	180

	CMC/Xa/5ZnO
	6066
	23073
	9845
	0.7475
	4.80
	600
	180
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