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Description automatically generated]Fig S1. BC production in 10 L glass vessel through traditional static fermentation. (a) BC formation feeding after 21 days of culturing; (b) Harvested BC pellicles; (c) Dried BC pellicle

Table 1. Culturing time and harvested BC physical characteristics obtained from MDV2, 3, and 4.
	 
	Culturing time (days)
	Wet thickness (mm)
	Wet weight (g)
	Dry thickness (mm)
	Dry weight/Yield (g)
	Dry density (kg/m3)

	
	
	
	
	
	
	
	

	MDV2
	96
	80
	4929.12
	0.14
	70.16
	91.55
	

	MDV3
	66
	60
	2319.32
	0.05
	42.73
	156.12
	

	MDV4
	48
	40
	2599.00
	0.04
	30.26
	138.2
	

	Control
	21
	5
	322.81
	0.0005
	3.37
	1231.28
	





image1.png




