Electronic Supplementary Material

Water repellency of cotton knitted fabrics treated with alkyl ketene dimers

Satoru Onodera • Chiaki Tanaka • Akira Isogai

S. Onodera  A. Isogai ()

Department of Biomaterials Science, Graduate School of Agricultural and Life Sciences, The University of Tokyo, Tokyo 113-8657, Japan

e-mail: akira-isogai@g.ecc.u-tokyo.ac.jp

S. Onodera  C. Tanaka

R&D Division, Gunze Limited, 1 Ishiburo, Inokurashin-machi, Ayabe, Kyoto 623-8512, Japan

Laundry treatment conditions

The AKD-treated CF samples were subjected to laundry treatment up to 30 cycles according to Japanese Industrial Standard entitled “Textiles-Domestic washing and drying procedures for textile testing” (JIS L 1930 F C4M, 2020). The details of the laundry conditions were as follows: the water temperature at 40 °C, and one laundry treatment time of 20 min including the following sequences, washing for 6 min, dehydration for 3 min, rinsing for 2 min, dehydration for 3 min, rinsing for 2 min, dehydration for 3 min, and drying at 40 °C for 30min. A commercial detergent (Attack®, Kao, Tokyo, Japan) was used in laundry treatment at a concentration of 0.67 g/L..

Fig. S1 SEM images of fiber surfaces of (a) AKD-treated and air-dried, and (b) AKD-treated and cured cotton fabrics, prepared by soaking in a weakly cationic 10 g/L AKD dispersion. The contents of the AKD-related compounds in the fabrics were determined by FTIR, and are expressed as wt% on the dry mass of fabric (odmf)

Fig. S2 Pyrolysis–gas chromatograms of the AKD-treated and cured cotton fabrics, prepared by soaking the cotton fabrics in weakly cationic (a) 1.0, (b) 5.0, (c) 10.0, and (d) 15.0 g/L AKD dispersions

Fig. S3 Relationships between the content of AKD-related compounds in the AKD-treated and cured cotton fabrics, and the relative peak ratio obtained from the pyrolysis–gas chromatograms. The contents of the AKD-related compounds are expressed as wt% on the dry mass of fabric (% odmf). A weakly cationic AKD dispersion was used to soak the fabric

Fig. S4 Relationships between the content of AKD-related compounds in the AKD-treated and cured cotton fabrics, and the relative AKD/total and AKD/levoglucosan peak ratios obtained from the pyrolysis–gas chromatograms. Weakly cationic AKD dispersions were used for fabric soaking. The contents of the AKD-related compounds are expressed as wt% on the dry mass of fabric (% odmf)

Fig. S5 FTIR spectra of the AKD-treated and cured cotton fabrics after one cycle of laundry treatment (see Fig. 1, Fig. 3, and Fig. 4 in the main text). Weakly cationic AKD dispersions were used for fabric soaking

Fig. S6 Photographs of water droplets on the AKD-treated and cured cotton fabrics with different water-absorption times, and the contents of the AKD-related compounds. Weakly cationic AKD dispersions were used for fabric soaking at different pHs of 4.5 and 10 for the upper and lower samples, respectively

### Fig. S7 FTIR spectra of the original CF, and the AKD-treated and cured CF before and after extractions with CHCl3, hot water, and 1% Tween 80

### Fig. S8 SEM images of the original AKD-treated and cured cotton fabrics, and the fabrics after extraction with CHCl3, hot water, or 1% Tween 80. A weakly cationic AKD dispersion was used for fabric soaking. The contents of the AKD-related compounds are expressed as wt% on the dry mass of fabric (% odmf)

Fig. S9 Water-absorption times and contents of AKD-related compounds of the AKD-treated and cured cotton fabrics, prepared by soaking in weakly cationic AKD dispersions at various pH values controlled by adding 0.1 M NaOH. The AKD concentration of the dispersion used for soaking was 6.7 g/L

Fig. S10 Relationships between the AKD concentration of the weakly and highly cationic AKD dispersions used for fabric soaking, and the content of AKD-related compounds in the AKD-treated and cured cotton fabrics, calculated from their FTIR spectra. The contents of AKD-related compounds are expressed as wt% on the dry mass of fabric (% odmf)