Supporting information for

Low-cost preparation of photocatalytic hydrolyzed cellulose composites, activated with one-step synthesized graphene oxide-metal oxide for dye degradation

Huseyin Gumus1*, Bulent Buyukkidan2,

1*Osmaneli Vocational School, Bilecik Seyh Edebali University, 11500, Osmaneli, Bilecik/Turkey

huseyin.gumus@bilecik.edu.tr (corresponding author) ORCID No: 0000-0002-2029-7978

2 Department of Chemistry, Kutahya Dumlupinar University, Kutahya/Turkey

bulent.buyukkidan@dpu.edu.tr  ORCID No: 0000-0001-9619-3246

Fig. S1 Schematic representation of photocatalysis preparation (a) and photocatalytic process (b)

Table S1 Properties of model pollutant MO

| Dye |  | Methyl Orange (MO) |  |
| --- | --- | --- | --- |
| Structure [24] |  |  |
| Synonym(s) | 4-[4-(Dimethylamino) phenylazo] benzenesulfonic acid sodium salt, Acid Orange 52/Orange III |  |
| Molecular formula | C14H14N3NaO3S |  |
| Molecular weight (g/mol) | 327.33 |  |
| Type | Anionic dye |  |

Table S2 Equations for adsorption kinetic and isotherms

| Adsorption isotherm |  |  |  |  |
| --- | --- | --- | --- | --- |
| Freundlich | Qe=KFCe1n | KF: Freundlich constant/Ln∙mg1–n∙g−1 1/n: adsorption intensity |  |
| Langmuir | Qe=QmKLCe1+KLCe | Qm: Maximum adsorption capacity of monolayer/mg∙g−1 KL: binding strength/L∙mg−1 |  |
| Pseudo-first order (PFO) | InCt=-k1t+InC0 | k1: PFO rate constant/min−1 |  |
| Pseudo-second order (PSO) | tQt= 1k2Qe2+ tQe | k2:PSOrate constant/mg∙g−1∙min−1 |  |

Fig. S2 XRD patterns of TiO2

Fig. S3 XRD patterns of textile waste-based cellulose

Fig. S4 XRD patterns of PVDF

Fig. S5 Ft-IR spectrum of GO-Fe- TiO2

Fig. S6 Pseudo second order isotherm plots for removal of MO onto P and PFb composites (MO amount: 50 mL (50 mg/L), pH= 7.0, temperature: 298 K, adsorbent: 0.3 g, stirring rate: 150 rpm for 110 min.)

Fig.S7 Infrared spectrums of Phc-20; MO adsorbed and UV radiated with air oxygen

Table S3 Photocatalytic dye removal studies with different adsorbent-photocatalyst (Gumus and Buyukkidan 2024)

| Catalyst-Biochar precursor |  | Amount or surface area (for membranes) |  |  | Substrat and amount |  |  | Power (W) |  |  | Time |  |  |  | Removal Mechanism and efficiency |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ZnO/biochar |  |  | 100 mg |  |  | 160 mg/L methylene blue |  |  | 250 |  |  | 200 min. |  |  |  | Degradation 95.19% |  |  |  |  |  |
| TiO2-biochar |  |  | 10 mg |  |  | 20 mg/L Methyl orange |  |  | 500 |  |  | 150 min. |  |  |  | Degradation 96.98% |  |  |  |  |  |
| FCF-pDA-PVDF (Fe-biochar-) composite beads |  |  | 1.0 g |  |  | 10 mg/L Methyl orange |  |  | 300 |  |  | 75 min. |  |  |  | Degradation 100% |  |  |  |  |  |
| MIL-53(Fe)/PVDF |  |  | 4.7 cm diameter |  |  | 20 ppm of tetracycline |  |  | 100 W Xe lamp, UV light |  |  | 30 min. |  |  |  | Degradation 93 % |  |  |  |  |  |
| Fe (III)-TiO2/ PVDF composite membrane |  |  | 13 cm -5 cm |  |  | 10 mg/L 250mL bisphenol-A (BPA) |  |  | 500 W sunlight Xenon lamp- |  |  | 180 min |  |  |  | Degradation 69.9% |  |  |  |  |  |
| TiO2-PVDF-co-HFP matrix |  |  | 0.10 m × 0.15 m |  |  | 100 mg/L Congo red (CR) and methylene blue (MB) |  |  | 8W UV light |  |  | 4 h. |  |  |  | Degradation-cleaning 100% |  |  |  |  |  |
| MCU-C3N4/PVDF membrane |  |  | (0.22 µm, 47 mm) |  |  | 5 mg/L rhodamine B (RhB) 5mg/L tetracycline hydrochloride (TC) |  |  | 300W Xe lamp |  |  | 60 min. |  |  |  | Degradation 84.24% 71.26% |  |  |  |  |  |
| Bi2WO6 @MIL-100(Fe)-PVDF |  |  | 14.6 cm2 |  |  | 10 mg/L 100 mL Pirimicarb |  |  | 70 W visible light |  |  | 240 |  |  |  | Degradation 86% |  |  |  |  |  |
| Fe-CTW (FeCl2 treated Waste Textile based) biochar |  |  | 50 mg |  |  | 75 mg/L methyl orange |  |  | 30 W |  |  | 35 + 10 min. |  |  |  | Degradation 87.4% |  |  |  |  |  |
| PFb-10 |  |  | 0.3 g |  |  | 75 mg/L Methyl orange |  |  | 30 W |  |  | 75+30+5 min. |  |  |  | Removal** 97.41% |  |  |  |  |  |
| Phc Phc-5 Phc-10 Phc-20 Phc-30 (G-TiO2-Fe-PVDF-Hcell) |  |  | 0.3 g |  |  | 50 mg/L Methyl orange |  |  | 30 W |  |  | 75+30+5* min. |  |  |  | Removal** 23.2% 62.5% 85.59% 91.8% 83.52% (This study) |  |  |  |  |  |

*   :	30W UV radiation for 30 min. (after the 75th minute) and, 30 W UV radiation for 5 min. with 0.01 mol/L (after the 105th minute)

**  :	Total removal by adsorption and degradation