SUPPLEMENTARY INFORMATION FOR:

„BIO-BASED LEATHER ALTERNATIVES: AN EVALUATION OF ELASTIC PROPERTIES”

Authors: Christoph Hahn1,2, Beatrice Steck3, Abhimanyu Tharayil2, André Matthes1, Holger Cebulla1

Journal Submission ID: 61933973-2e1a-4290-8fa1-303d1db6c637

Corresponding Author: Christoph Hahn

Mail: christoph.ch.hahn@mercedes-benz.com

1 Chemnitz University of Technology

Faculty of Mechanical Engineering

Chair of Textile Technologies

Reichenhainer Str. 70

09126 Chemnitz

Germany

2 Mercedes-Benz AG

Leibnizstraße 2

71032 Böblingen

Germany

3 Reutlingen University

Faculty of Textile – Textoversum

Alteburgstraße 150

72762 Reutlingen

Germany

Content: Additional Mechanical Data (MD and CD values)

Table S1: Additional mechanical data (MD and CD values) for Fig 6: Overview of the elongation at low forces on average of MD and CD. The reference materials, leather and artificial leather are highlighted by the grey area

Table S2: Additional mechanical data (MD and CD values) for Fig 7: IER in comparison to elongation qualitatively and quantitatively on average of MD and CD

Table S3: Additional mechanical data (MD and CD values) for Fig 8: IER at different elongation limits qualitatively on average of MD and CD

Table S4: Additional mechanical data (MD and CD values) for Fig 9: Loss of IER with increase in cycles qualitatively on average of MD and CD

Table S5: Additional mechanical data (MD and CD values) for Fig 11: Proportions of IER, DR and PS qualitatively and quantitatively on average of MD and CD

Table S1: Additional mechanical data (MD and CD values) for Fig 6: Overview of the elongation at low forces on average of MD and CD. The reference materials, leather and artificial leather are highlighted by the grey area

|  |  | 25 N | cV | 50N | cV | 100 N | cV |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | [N] | [%] | [N] | [%] | [N] | [%] |
| NGM2 | Average | 0,75 | 11,49 | 1,52 | 16,06 | 3,59 | 19,98 |
|  | MD | 0,80 | 2,61 | 1,60 | 3,48 | 3,60 | 4,29 |
|  | CD | 0,69 | 13,83 | 1,43 | 24,09 | 3,00 | 28,95 |
| NGM3 | Average | 0,96 | 14,76 | 1,46 | 12,15 | 2,25 | 9,78 |
|  | MD | 0,84 | 6,02 | 1,31 | 6,56 | 2,06 | 5,11 |
|  | CD | 1,09 | 6,02 | 1,62 | 6,56 | 2,44 | 5,11 |
| CT1 | Average | 0,87 | 17,96 | 1,63 | 16,49 | 2,95 | 15,91 |
|  | MD | 0,87 | 18,99 | 1,57 | 16,89 | 2,66 | 9,49 |
|  | CD | 0,87 | 20,61 | 1,68 | 18,75 | 3,24 | 14,46 |
| CT2 | Average | 15,37 | 42,21 | 39,01 | 56,48 | 64,47 | 59,36 |
|  | MD | 21,28 | 2,38 | 59,12 | 0,91 | 99,39 | 0,92 |
|  | CD | 9,46 | 4,72 | 18,90 | 2,85 | 29,54 | 1,67 |
| NWPF1 | Average | 1,36 | 60,11 | 2,28 | 62,56 | 3,97 | 68,77 |
|  | MD | 0,62 | 7,03 | 0,99 | 5,34 | 1,54 | 3,96 |
|  | CD | 2,10 | 8,75 | 3,56 | 8,67 | 6,40 | 11,54 |
| NWPF2 | Average | 0,39 | 39,34 | 0,79 | 30,69 | 1,72 | 26,54 |
|  | MD | 0,26 | 11,6 | 0,59 | 4,92 | 1,36 | 6,24 |
|  | CD | 0,51 | 16,05 | 0,99 | 15,55 | 2,08 | 16,97 |
| NWPF3 | Average | 0,15 | 37,11 | 0,26 | 49,42 | 0,57 | 53,88 |
|  | MD | 0,10 | 10 | 0,15 | 20,83 | 0,29 | 18,78 |
|  | CD | 0,19 | 5,26 | 0,37 | 4,09 | 0,84 | 2,38 |
| NWPF4 | Average | 0,17 | 34,81 | 0,41 | 11,12 | 0,91 | 38,43 |
|  | MD | 0,20 | 19,88 | 0,40 | 14,34 | 1,22 | 7,29 |
|  | CD | 0,14 | 54,19 | 0,41 | 9,78 | 0,59 | 0,97 |
| Bovine Leather | Average | 3,68 | 17,93 | 6,63 | 21,77 | 11,17 | 22,29 |
|  | MD | 4,12 | 14,98 | 7,63 | 16,35 | 12,85 | 15,41 |
|  | CD | 3,23 | 10,47 | 5,63 | 14,12 | 9,49 | 18,49 |
| Synthetic Leather | Average | 4,12 | 24,53 | 9,04 | 35,7 | 20,21 | 48,12 |
|  | MD | 3,20 | 3,8 | 6,10 | 2,89 | 11,34 | 2,92 |
|  | CD | 5,03 | 2,93 | 11,97 | 2,26 | 29,07 | 2,1 |

Table S2: Additional mechanical data (MD and CD values) for Fig 7: IER in comparison to elongation qualitatively and quantitatively on average of MD and CD

|  | MD |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | IER |  | PS |  | Elongation |  |
|  | [mm] | cV [%] | [mm] | cV [%] | [mm] | cV [%] |
| NGM1 | 2,21 | 66,84 | 3,86 | 12,42 | 6,07 | 30,44 |
| NGM2 | 2,57 | 3,06 | 1,19 | 6,77 | 3,75 | 0,15 |
| NGM3 | 6,21 | 1,05 | 4,55 | 1,25 | 10,75 | 0,16 |
| CT1 | 6,06 | 1,59 | 4,93 | 1,77 | 11,00 | 0,11 |
| CT2 | 32,35 | 1,55 | 22,65 | 2,20 | 55,00 | 0,01 |
| NWPF1 | 2,42 | 1,86 | 3,31 | 1,99 | 5,73 | 0,52 |
| NWPF2 | 4,69 | 12,89 | 11,78 | 5,06 | 16,47 | 0,19 |
| NWPF3 | 1,29 | 0,97 | 0,46 | 3,33 | 1,75 | 0,34 |
| NWPF4 | 2,30 | 1,76 | 3,22 | 0,55 | 5,51 | 0,49 |
| Bovine Leather | 7,93 | 2,62 | 9,74 | 2,12 | 17,67 | 0,11 |
| Synthetic Leather | 14,63 | 0,47 | 9,15 | 0,87 | 23,78 | 0,13 |

|  | CD |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | IER |  | PS |  | Elongation |  |
|  | [mm] | cV [%] | [mm] | cV [%] | [mm] | cV [%] |
| NGM1 | 0,81 | 31,44 | 6,08 | 6,68 | 6,89 | 2,34 |
| NGM2 | 1,82 | 4,37 | 0,60 | 13,75 | 2,42 | 0,23 |
| NGM3 | 3,30 | 1,21 | 3,70 | 1,09 | 7,00 | 0,08 |
| CT1 | 9,04 | 0,96 | 9,04 | 0,90 | 18,09 | 0,06 |
| CT2 | 12,70 | 1,95 | 9,05 | 2,72 | 21,76 | 0,02 |
| NWPF1 | 4,95 | 3,55 | 11,29 | 1,50 | 16,24 | 0,06 |
| NWPF2 | 3,40 | 7,02 | 9,27 | 2,58 | 12,67 | 0,06 |
| NWPF3 | 2,17 | 3,30 | 2,58 | 2,84 | 4,75 | 0,06 |
| NWPF4 | 1,78 | 3,09 | 1,73 | 2,93 | 3,50 | 0,22 |
| Bovine Leather | 6,40 | 2,60 | 7,78 | 2,32 | 14,18 | 0,20 |
| Synthetic Leather | 31,87 | 0,37 | 22,14 | 0,56 | 54,00 | 0,01 |

Table S3: Additional mechanical data (MD and CD values) for Fig 8: IER at different elongation limits qualitatively on average of MD and CD

|  | MD |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | IER at 40% | cV | IER at 50% | cV | IER at 60% | cV |
|  | [%] | [%] | [%] | [%] | [%] | [%] |
| NGM1 | 33,82 | 37,66 | -30,81 | 208,80 | -19,49 | 216,93 |
| NGM2 | 66,78 | 3,18 | 61,70 | 4,07 | 61,21 | 3,29 |
| NGM3 | 55,09 | 1,01 | 52,03 | 0,57 | 49,36 | 0,5 |
| CT1 | 52,65 | 1,57 | 59,26 | 3,03 | 59,40 | 5,7 |
| CT2 | 56,61 | 1,60 | 57,58 | 2,47 | 58,25 | 1,49 |
| NWPF1 | 40,80 | 2,26 | 35,96 | 3,82 | 31,99 | 1,47 |
| NWPF2 | 26,83 | 13,65 | 20,78 | 37,48 | 20,28 | 9,44 |
| NWPF3 | 71,60 | 1,14 | 65,35 | 2,03 | 58,31 | 5,36 |
| NWPF4 | 39,60 | 1,37 | 37,05 | 2,40 | 33,46 | 5,69 |
| Bovine Leather | 43,19 | 2,71 | 43,95 | 2,52 | 39,78 | 3,8 |
| Synthetic Leather | 61,53 | 0,51 | 59,27 | 0,98 | 57,84 | 0,37 |

|  | CD |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | IER at 40% | cV | IER at 50% | cV | IER at 60% | cV |
|  | [%] | [%] | [%] | [%] | [%] | [%] |
| NGM1 | 11,77 | 33,08 | -101,67 | 122,15 | -94,25 | 49,46 |
| NGM2 | 75,11 | 4,50 | 72,19 | 2,93 | 67,91 | 1,34 |
| NGM3 | 47,17 | 1,21 | 41,24 | 0,49 | 36,93 | 0,42 |
| CT1 | 50,00 | 0,93 | 47,57 | 1,85 | 55,30 | 7,63 |
| CT2 | 58,39 | 1,94 | 55,30 | 0,10 | 56,88 | 0,56 |
| NWPF1 | 30,50 | 3,51 | 24,96 | 0,90 | 19,82 | 5,4 |
| NWPF2 | 26,83 | 7,03 | 24,08 | 4,73 | 23,51 | 10,09 |
| NWPF3 | 45,61 | 3,34 | 36,29 | 0,23 | 33,61 | 0,77 |
| NWPF4 | 50,74 | 2,96 | 44,55 | 1,57 | 40,82 | 3,88 |
| Bovine Leather | 45,13 | 2,69 | 43,53 | 1,53 | 43,06 | 9,85 |
| Synthetic Leather | 59,01 | 0,39 | 55,28 | 0,69 | 52,70 | 0,76 |

Table S4: Additional mechanical data (MD and CD values) for Fig 9: Loss of IER with increase in cycles qualitatively on average of MD and CD

|  | MD |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cycle 1 to 2 | cV [%] | Cycle 2 to 3 | cV [%] | Cycle 3 to 4 | cV [%] | Cycle 4 to 5 | cV [%] |
| NGM1 | 0,02 | 6569,70 | 0,01 | 16686,57 | -0,27 | -137,35 | 0,47 | 458,28 |
| NGM2 | 3,47 | 29,78 | 2,34 | 10,17 | 1,39 | 112,95 | 3,82 | 25,77 |
| NGM3 | 5,22 | 7,79 | 2,77 | 11,76 | 1,69 | 15,86 | 2,26 | 9,39 |
| CT1 | 4,87 | 7,26 | 2,52 | 15,30 | 1,80 | 20,04 | 2,16 | 11,87 |
| CT2 | 4,32 | 4,67 | 2,55 | 7,99 | 1,64 | 10,59 | 1,49 | 7,80 |
| NWPF1 | 2,91 | 3,81 | 1,39 | 8,78 | 1,44 | 7,19 | 2,85 | 9,22 |
| NWPF2 | 3,52 | 2,77 | 1,59 | 10,69 | 1,02 | 3,00 | 1,37 | 8,25 |
| NWPF3 | 3,42 | 28,53 | 2,71 | 56,35 | 1,61 | 182,16 | 6,41 | 23,42 |
| NWPF4 | 4,27 | 6,62 | 1,50 | 45,53 | 1,90 | 24,12 | 2,63 | 13,20 |
| Bovine Leather | 3,55 | 5,96 | 1,71 | 10,43 | 1,11 | 27,23 | 1,47 | 10,54 |
| Synthetic Leather | 4,63 | 3,42 | 2,65 | 6,47 | 1,62 | 12,86 | 1,65 | 10,48 |

|  | CD |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cycle 1 to 2 | cV [%] | Cycle 2 to 3 | cV [%] | Cycle 3 to 4 | cV [%] | Cycle 4 to 5 | cV [%] |
| NGM1 | -0,11 | 2062,83 | 0,28 | 276,74 | 0,14 | 942,11 | 0,78 | 180,4 |
| NGM2 | 3,21 | 8,87 | 1,85 | 89,24 | 0,75 | 153,54 | 6,21 | 8,90 |
| NGM3 | 4,38 | 11,85 | 2,42 | 6,76 | 1,17 | 32,04 | 2,64 | 12,59 |
| CT1 | 4,94 | 4,65 | 2,40 | 7,87 | 1,66 | 16,76 | 1,71 | 11,21 |
| CT2 | 4,28 | 7,59 | 2,31 | 9,52 | 1,53 | 2,64 | 1,79 | 16,43 |
| NWPF1 | 3,09 | 2,28 | 1,63 | 9,46 | 1,02 | 24,13 | 1,45 | 18,27 |
| NWPF2 | 3,25 | 2,64 | 1,75 | 18,34 | 1,30 | 6,27 | 1,37 | 10,12 |
| NWPF3 | 3,99 | 18,32 | 1,88 | 23,24 | 1,68 | 38,73 | 3,71 | 16,50 |
| NWPF4 | 3,48 | 39,15 | 2,29 | 12,33 | 0,88 | 111,78 | 4,19 | 19,58 |
| Bovine Leather | 3,40 | 7,02 | 1,77 | 0,56 | 1,06 | 30,58 | 1,50 | 13,99 |
| Synthetic Leather | 4,43 | 24,91 | 2,32 | 9,50 | 1,62 | 8,25 | 1,30 | 6,67 |

Table S5: Additional mechanical data (MD and CD values) for Fig 11: Proportions of IER, DR and PS qualitatively and quantitatively on average of MD and CD

| MD |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | IER |  |  | DR |  |  | PS |  |  | Elongation |
|  | [mm] | cV [%] | [%] | [mm] | cV [%] | [%] | [mm] | cV [%] | [%] | [mm] |
| NGM2 | 2,20 | 1,03 | 64,71 | 0,6 | 0,87 | 17,65 | 0,60 | 0,83 | 17,65 | 3,4 |
| NGM3 | 3,60 | 0,97 | 54,55 | 1,6 | 0,00 | 24,24 | 1,40 | 1,07 | 21,21 | 6,6 |
| CT1 | 3,40 | 2,05 | 60,71 | 0,7 | 2,50 | 12,50 | 1,50 | 1,94 | 26,79 | 5,6 |
| CT2 | 30,50 | 4,14 | 19,23 | 3,75 | 2,31 | 11,54 | 2,75 | 1,59 | 69,23 | 37,0 |
| NWPF1 | 1,25 | 1,02 | 38,96 | 0,75 | 0,90 | 22,08 | 4,50 | 1,06 | 38,96 | 6,5 |
| NWPF2 | 6,00 | 2,32 | 82,43 | 3,4 | 1,92 | 10,14 | 6,00 | 1,26 | 7,43 | 15,4 |
| NWPF3 | 0,40 | 1,07 | 28,57 | 0,6 | 0,00 | 42,86 | 0,40 | 0,44 | 28,57 | 1,4 |
| NWPF4 | 1,50 | 0,81 | 28,57 | 1,25 | 1,66 | 23,81 | 2,50 | 2,09 | 47,62 | 5,3 |
| Bovine Leather | 4,60 | 0,95 | 62,16 | 0,8 | 0,85 | 10,81 | 2,00 | 1,36 | 27,03 | 7,4 |
| Synthetic Leather | 13,00 | 1,98 | 82,28 | 1,6 | 2,47 | 10,13 | 1,20 | 0,87 | 7,59 | 15,8 |

| CD |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | IER |  |  | DR |  |  | PS |  |  | Elongation |
|  | [mm] | cV [%] | [%] | [mm] | cV [%] | [%] | [mm] | cV [%] | [%] | [mm] |
| NGM2 | 1,00 | 0,00 | 50,00 | 0,8 | 0,00 | 40,00 | 0,20 | 0,55 | 10,00 | 2,0 |
| NGM3 | 3,40 | 1,49 | 54,19 | 0,8 | 0,85 | 13,05 | 2,00 | 0,00 | 32,76 | 6,2 |
| CT1 | 6,00 | 1,72 | 75,95 | 2 | 1,92 | 9,01 | 1,30 | 2,35 | 15,04 | 9,3 |
| CT2 | 13,60 | 2,11 | 80,97 | 1,8 | 1,70 | 13,28 | 0,80 | 0,88 | 5,75 | 16,2 |
| NWPF1 | 4,60 | 1,72 | 33,33 | 1,6 | 1,41 | 11,48 | 7,60 | 0,95 | 55,19 | 13,8 |
| NWPF2 | 2,60 | 1,50 | 27,23 | 2 | 1,75 | 20,75 | 5,00 | 1,29 | 52,02 | 9,6 |
| NWPF3 | 0,80 | 0,84 | 25,00 | 0,4 | 1,05 | 13,33 | 2,00 | 1,36 | 61,67 | 3,2 |
| NWPF4 | 2,00 | 1,00 | 43,00 | 0,4 | 1,04 | 9,00 | 2,20 | 0,86 | 48,00 | 4,6 |
| Bovine Leather | 4,40 | 1,59 | 69,33 | 0,4 | 1,36 | 6,19 | 1,60 | 1,06 | 24,48 | 6,4 |
| Synthetic Leather | 28,20 | 1,26 | 76,61 | 6,2 | 0,93 | 16,84 | 2,40 | 1,05 | 6,55 | 36,8 |