Supplementary Information

Fabrication of sisal fiber-derived beads from sustainable solvents: Investigating their potential for pH-responsive sorption of bovine serum albumin

Thamiris Voltarelli Ferracini a,b, Pieter De Wever b, Roberta Teixeira Polez c, Xiaoyan Qing b, Elisabete Frollini a, Pedro Fardim b

a Macromolecular Materials and Lignocellulosic Fibers Group, Center for Research on Science and Technology of BioResources, São Carlos Institute of Chemistry, University of São Paulo, São Paulo, São Carlos, Brazil

b Department of Chemical Engineering, Chemical and Biochemical Reactor Engineering and Safety, KU Leuven, Leuven, Belgium

c Department of Bioproducts and Biosystems, School of Chemical Engineering, Aalto University, Espoo, Finland

Figure S1. Standard calibration curve absorbance (λ = 595 nm) of bovine serum albumin (BSA) at different concentrations used for quantification of protein adsorption.

Figure S2. SEM surface images at different magnifications of the sisal beads: (a) NaOH-urea/4g/HNO3, (b) NaOH-urea/6g/HNO3, (c) ZnCl₂/1g/CaCl₂, (d) ZnCl₂/0.5g/CaCl₂, and (e) ZnCl₂/0.5g/EtOH.

| (c) | pH 3 |  |  | pH 4.6 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qe (mg/g)A | k1 (1/min) B | R2 | qe (mg/g) | k1 (1/min) | R2 |
| NaOH/4g/HNO3 | 34.50 ± 2.88 | 0.18 ± 0.06 | 0.961 | 7.98 ± 0.76 | 0.44 ± 0.15 | 0.928 |
| NaOH/6g/HNO3 | 39.08 ± 5.78 | 0.30 ± 0.16 | 0.879 | 6.41 ± 0.23 | 0.46 ± 0.06 | 0.990 |
| ZnCl2/1g/CaCl2 | 40.23 ± 6.33 | 1.19 ± 0.92 | 0.791 | 8.79 ± 1.14 | 0.40 ± 0.18 | 0.872 |
| ZnCl2/0.5g/CaCl2 | -0.26 ± 0.23 | -0.24 ± 0.04 | 0.989 | 3.87 ± 0.46 | 0.43 ± 0.18 | 0.896 |
| ZnCl2/0.5g/EtOH | 108.17 ± 6.68 | 0.13 ± 0.03 | 0.990 | 9.23 ± 0.35 | 1.06 ± 0.19 | 0.985 |

A qe is the amount id BSA adsorbed at the equilibrium.

B k1 is the pseudo first-order rate constant.

Figure S3. Sorption capacity of BSA as a function of time plots and pseudo-first-order kinetic model fitting at (a) pH 3 and (b) pH 4.6. (c) Kinetic model parameters of pseudo first order for BSA sorption on sisal beads.

| (c) | pH 3 |  |  | pH 4.6 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qe (mg/g) A | k2 (1/min) B | R2 | qe (mg/g) | k2 (1/min) | R2 |
| NaOH/4g/HNO3 | 8.75 ± 0.90 | 0.07 ± 0.03 | 0.9453 | 42.28 ± 4.82 | 0.004 ± 0.002 | 0.9715 |
| NaOH/6g/HNO3 | 7.01 ± 0.53 | 0.08 ± 0.03 | 0.9705 | 46.14 ± 10.33 | 0.006 ± 0.006 | 0.8696 |
| ZnCl2/1g/CaCl2 | 9.66 ± 1.36 | 0.05 ± 0.03 | 0.9034 | 43.57 ± 7.03 | 0.037 ± 0.041 | 0.8338 |
| ZnCl2/0.5g/CaCl2 | 4.28 ± 0.60 | 0.12 ± 0.08 | 0.9061 | 202494.06 ± 1.21 | 5x10-11 ± 7x10-7 | 0.7583 |
| ZnCl2/0.5g/EtOH | 9.62 ± 0.57 | 0.20 ± 0.08 | 0.9735 | 145.46 ± 13.99 | 7 x10-4 ± 2 x10-4 | 0.9923 |

A qe is the amount id BSA adsorbed at the equilibrium.

B k2 is the PSO rate constant.

Figure S4. Sorption capacity of BSA as function of time plots and pseudo second order kinetic model fitting at (a) pH 3 and (b) pH 4.6. (c) Kinetic model parameters of pseudo second order for BSA sorption on sisal beads.

| (c) | pH 3 |  |  | pH 4.6 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | C (mg/g) A | kdiff (mg/g min0.5) B | R2 | C (mg/g) | kdiff (mg/g min0.5) | R2 |
| NaOH/4g/HNO3 | 1.57 ± 0.31 | 1.23 ± 0.95 | 0.8922 | 7.100 ± 0.39 | 1.38 ± 1.18 | 0.9909 |
| NaOH/6g/HNO3 | 1.23 ± 0.32 | 1.04 ± 0.99 | 0.8243 | 8.55 ± 2.316 | 1.10 ± 7.02 | 0.8197 |
| ZnCl2/1g/CaCl2 | 1.75 ± 0.34 | 1.27 ± 1.04 | 0.8963 | 7.68 ± 2.81 | 11.36 ± 8.53 | 0.7134 |
| ZnCl2/0.5g/CaCl2 | 0.77 ± 0.18 | 0.54 ± 0.55 | 0.8574 | 10.28 ± 3.43 | 9x10-27 ± 23.30 | 0.6241 |
| ZnCl2/0.5g/EtOH | 1.49 ± 0.66 | 3.10 ± 2.02 | 0.6266 | 21.82 ± 1.19 | 8 x10-25 ± 8.07 | 0.9796 |

A C is a constant related to the boundary layer thickness.

B kdiff is the intraparticle diffusion rate constant.

Figure S5. Sorption capacity of BSA as function of time plots and intraparticle diffusion kinetic model fitting at (a) pH 3 and (b) pH 4.6. (c) Kinetic model parameters of intraparticle diffusion model for BSA sorption on sisal beads.